Biomimetic matrices for rapidly forming mineralized bone tissue based on stem cell-mediated osteogenesis

Marta S. Carvalho1,2, Atharva A. Poundarik1, Joaquim M.S. Cabral2,3, Cláudia L. da Silva2,3 and Deepak Vashishth1

1Center for Biotechnology and Interdisciplinary Studies, Department of Biomedical Engineering, Rensselaer Polytechnic Institute, Troy, NY, USA

2Department of Bioengineering and iBB – Institute of Bioengineering and Biosciences, Instituto Superior Técnico, Universidade de Lisboa, Lisboa, Portugal.

3The Discoveries Centre for Regenerative and Precision Medicine, Lisbon Campus, Instituto Superior Técnico, Universidade de Lisboa, Lisboa, Portugal

Supplementary Figure 1. Relative gene expression (collagen I [Col I], runt-related transcription factor 2 [Runx2], osteopontin [OPN], osteocalcin [OC] and alkaline phosphatase [ALP]) by BM MSC upon culture for 7, 15 and 21 days on control collagen gels, OPN - enhanced collagen gels, OC – enhanced collagen gels and OC/OPN – enhanced collagen gels. Data are expressed as mean ± s.e.m.; **P<0.01;  *P<0.05, relative to day 21 (Col I, Runx2, OPN, OC) and day 7 (ALP).

Supplementary Figure 2. SDS-PAGE protein gel of collagen gel, OC- collagen gel, OPN- collagen gel and OC/OPN- collagen gel confirms the presence of OC/OPN in the matrices. White box shows bands referred to molecular weight of OPN. White dashed box shows bands referred to molecular weight of OC.

Supplementary Figure 3.  In vitro OC and OPN release from OC/OPN-enhanced collagen gels. OC and OPN levels in PBS were determined by ELISA measurements after 24 h and 21 days. Results demonstrated that the biomimetic gels did not release OC and OPN proteins, being able to maintain the proteins on the gel.