Experimental Observation of the High Pressure Induced Substitutional Solid Solution and Phase Transformation in Sb2S3

Yingying Wang1, Yanmei Ma1＊, Guangtao Liu2, Jianyun Wang1, Yue Li1, Quan Li1, Jian Zhang1＊, YanmingMa1, Guangtian Zou1

# 1College of Physics, State Key Laboratory of Superhard Materials, Jilin University, Changchun 130012, China

2National Key Laboratory of Shock Wave and Detonation Physics, Institute of Fluid Physics, Chinese Academy of Engineering Physics, Mianyang 621900, China

Supplementary Materials

Supplementary Fig.1.  two-dimensional X-ray diffraction images of Sb2S3 at pressure of 42.5 GPa and ambient temperatures obtained in an angle-dispersive mode. Each Q(d) value corresponds to a diffraction ring. The scale for Q and d-spacing are given, and they correspond to each other.

(a)                          (b)                        (c)

Supplementary Fig.2. The morphological studies of the sample powders via SEM (a) and TEM (b,c) techniques. The select area electron beam diffractions (SAED) indicate each particle is a single crystalline grain. The particle size of the sample is about 2-3 μm in diameter.

Supplementary Fig.3.  XRD patterns collected at 0.7GPa, 50.2 GPa and after pressure release for Sb2S3 with an incident wavelength λ = 0.6199 Å. The existing peaks in the released pattern match those in the starting pattern very well.  Apparently, there is not  bcc phase quenched