Supporting Information

Rapid and selective recovery of palladium from platinum group metals and base metals using a thioamide-modified calix[4]arene extractant in environmentally friendly hydrocarbon fluids

Manabu Yamada 1†, Muniyappan Rajiv Gandhi 2†§ & Atsushi Shibayama 2

1 Research Center of Advanced Materials for Breakthrough Technology, Graduate School of Engineering Science, Akita University, Akita 010-8502, Japan.

2 Graduate School of International Resource Sciences, Akita University, Akita 010-8502, Japan.

†These authors contributed equally to this work. §Current address: Quality Control Department, Panipat Refinery & Petrochemical Complex, Indian Oil Corporation Limited, Haryana 132140, India. Correspondence and requests for materials should be addressed to M.Y. (email: myamada@gipc.akita-u.ac.jp)

Contents

Preliminary data of X-ray crystallography measurement of crystals 1

Supporting Tables

Table S1. The concentrations of metal ions in the leached liquors of automotive catalysts                   after 5 times dilution.

Table S2. Stripping of Pd(II) from the automotive leached solution extracted in  kerosene +                20% n-octanol  phase of  1 by 1 M HCl,  1 M HNO3,  10% (v/v) NH3 aqueous                solution and 0.5 M thiourea + 1.0 M HCl solution.

Supporting figures

Figure S1. Extraction of Pd(II) by 1 in kerosene, kerosene + 20%  n-octanol and extraction

of  Pd(II) by 2 in kerosene.

Figure S2. The FT-IR spectra of native 1 and acid treated 1.

Figure S3. Metal ions E% of 1 in ExxalTM 10 from catalyst leach liquors.

Conditions: shaking time = 30 min; [1] = 1.0 mM in ExxalTM 10; pH = 1.22

(~0.06 M HCl); O/A = 1; shaking speed = 300 rpm.

Figure S4. (a) Stripping of Pd(II) using 0.1 M thiourea/HCl (TU), (b) stripping of Pd(II)

using 10%  (v/v) NH3.

Figure S5. Stick diagram of 1. S = yellow, O = red, N = pale purple, C = dark grey (The H

atoms have been omitted for clarity).

Preliminary data of X-ray crystallography measurement of crystals 1

Single crystals of 1 for X-ray diffraction studies were grown from CHCl3 by slow evaporation at room temperature.  The crystals in mother liquid were picked up with a pipette, and dropped in Paratone-N oil. The single crystals coated with oil were isolated on MicroMountsTM, and the crystals were placed in a cold nitrogen steam at 93 K. X-ray diffraction data were collected a Rigaku Saturn 724 CCD diffractometer with Mo-Kα radiation (λ = 0.71073 Å). The structures were solved by direct methods using SHELXT-2014,1 and refined using the full-matrix least-squares method on F2 using SHELXL-2014.2 All materials for publication were prepared by Yadokari-XG 2009 software.3,4

Crystal data. C85.5H132.5Cl1.50N4O5S4, M =1477.95, colorless, crystal dimensions 0.35 × 0.35 × 0.10 mm3, triclinic, space group P -1, crystal description block, a = 13.4706(4), b = 18.5354(5), c = 19.9039(6) Å, α = 112.967(3)°, β = 91.894(2)o, γ = 97.076(2)°, V = 4522.9(2) Å3, Z = 1, Mo Kα radiation (λ = 0.71075 Å), ρcalcd = 1.082 g/cm3, T = 93 K, µ(Mo Kα) = 0.197 mm-1, 60181 measured reflections, 20511 unique reflections (Rint = 0.0373), 15535 observed reflections (I > 2σ(I)), 966 parameters, R = 0.1402, wR = 0.4487, refined against |F|, GOF = 1.884.

References

(1) Sheldrick, G. SHLEXT ‒ Integrated space-group and crystal-structure determination. Acta Crystallogr. Sect. A Found. Adv.  2015, 71, 3-8.

(2) Sheldrick, G. Crystal structure refinement with SHELXL. Acta Crystallogr. Sect. C Struct. Chem. 2015, 71, 3-8.

(3) Wakita, K. Yadokari-XG, software for crystal structure analyses. 2001.

(4) Kabuto, C.; Akine, S.; Nemoto, T.; Kwon, E. Release of software (Yadokari-XG 2009) for crystal structure analyses. Nippon Kessho Gakkaishi 2009, 51, 218-224.

Supporting Table

Table S1. The concentrations of metal ions in the leached liquors of automotive catalysts

after 5 times dilution.

| Metal ions | [M]aq,init (mg/L) |
| --- | --- |
| Pd Pt Rh La Ce Y Zr Ba Al | 92.8 54.2 37.2 86.7 608.8 3.8 25.6 289.3 320.9 |

Table S2. Stripping of Pd(II) from the automotive leached solution extracted in  kerosene + 20% n-octanol  phase of  1 by 1 M HCl,  1 M HNO3,  10% (v/v) NH3 aqueous solution and 0.5 M thiourea + 1.0 M HCl solution.

| Stripping reagent | Pd(II) S% |
| --- | --- |
| 0.1 M thiourea + 1.0 M HCl solution | 99.9 |
| 10% (v/v) NH3 aqueous solution | 20.1 |
| 1 M HNO3 | 16.4 |
| 1 M HCl | 15.3 |

Shaking time = 30 min; shaking speeds = 300 rpm; O/A= 1; temperature = 20 ± 1 °C.

Figure S1. Extraction of Pd(II) by 1 in kerosene, kerosene + 20%  n-octanol and extraction                    of Pd(II) by 2 in kerosene.

Figure S2. The FT-IR spectra of native 1 and acid treated 1.

Figure S3. Metal ions E% of 1 in ExxalTM 10 from catalyst leach liquors. Conditions: shaking time = 30 min; [1] = 1.0 mM in ExxalTM 10; pH = 1.22 (~0.06 HCl); O/A = 1; shaking speed = 300 rpm.

Figure S4. (a) Stripping of Pd(II) ion using 0.1 M thiourea/HCl (TU), (b) Stripping of Pd(II) ion using 10%  (v/v) NH3.

Figure S5. Stick diagram of 1. S = yellow, O = red, N = pale purple, C = dark grey (The H                  atoms have been omitted for clarity).