Fluorescent Biocompatible Platinum-Porphyrin–Doped Polymeric Hybrid Particles for Oxygen and Glucose Biosensing

Gaurav Pandey 1 , ζ, Rashmi Chaudhari 2, ζ, Bhavana Joshi 1, ζ, Sandeep Choudhary1 , Jaspreet Kaur1, Abhijeet Joshi 1, *

Supplementary Information

A)

B)

Figure S1: AFM images of PLGA nanoparticles, PEI-PLGA nanoparticles and PLA nanoparticles and CLSM images of PEI-PLGA nanoparticles embedded in alginate microspheres (A) and CLSM images of PLGA nanoparticles embedded alginate microspheres (B)

a)

b)

Fig S2: a) Calibration curve for Pt-Porphyrin for quantifying the encapsulation efficiency. b) Reversibility of response of Pt-Porphyrin when exposed to different concentrations of oxygen ranging from 0-10 mM

Fig S3. Response time curves for Glucose sensing using GPP-AM using a concentration of 6 mM Glucose, (Y error bars represent standard deviation of intensities of triplicate measurement

Table S1.  Effect of Pressure and flow rate of droplet generator for production of PP-AM and GPP-AM carriers

| Pressure (mbar) | Flow rate (ml/hr) | Concentration nanoparticles: alginate | Size of Hybrid microparticles (µm) |
| --- | --- | --- | --- |
| 70 (5) | 20 (2) | - | 60 (10) |
| 60 (5) | 10 (2) | 25 % w/v | 60 (10) |
| 120 (5) | 10 (2) | 25% w/v | 25 (7) |
| 300 (5) | 15 (2) | 75 % w/v | 15 (5) |
| 400 (5) | 15 (2) | 75 % w/v | 8 (5) |

The standard sample parameters used were concentration of alginate (2%w/v), Concentration of CaCl2 (250 mM), Nozzle size (0.35 mm) and distance for crosslinking (10 cm). Values in parenthesis represent the standard deviation; All the experiments were conducted for triplicate