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 EosFit parameter file
 
 This is a fixed-format file. If you edit this file, make sure you do not move anything!
 It is safer to change the parameters by loading the file to EosFit, and saving the file after making changes
 ____________________________________________________________________________________________________________
 
Title = Magnesiochromite (Ac139 sample) BM2-HP EoS to P-V-T data
Savedate = 27-MAR-2019 at 19:51
Comment =Fitted to P-V data of Nestola et al. (2018); Pmax = 7.85 GPa;
Comment =Fitted to T-V data of Singh et al. (1975), Grimes and Al-Ajaj (1992), Wang et al. (2012); Tmax = 1273 K; 
Comment =Volume data rescaled to its own V0 and V/V0 = 1 kept fixed during the fit;
Comment =gamma0 and q kept fixed during the fit (not relevant for the Holland-Powell model);
Comment = K' fixed from the EoS model used (BM2);
Comment =All the other EoS parameters were refined;
Comment =EoS obtained by Gabriele Zaffiro (University of Pavia).
 
Model =  2,  (Birch-Murnaghan)                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                            
Order =  2
Thermal =  6,  (HP Thermal Pres)                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                            
Cross =  0,  (none)                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                       
Trans =  0,  (none)                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                       
Shear =  0,  (none)                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                       
Type = Volume
Pref =   0.00000
Tref = 298.00000
Pscale =GPa
Vscale =V/V0
Stoich =   1.00000
 
Param = 1 1.00000         (V0   ,  Reference pressure volume: units are V/V0)
Param = 2 183.255         (K0   ,  Bulk modulus: units are GPa)
Param = 3 4.00000         (Kp   ,  dK/dP: dimensionless)
Param = 4 -0.0212         (Kpp  ,  d2K/dP2: units are inverse GPa)
Param = 5 0.00000    
Param = 6 0.00000    
Param = 7 0.00000    
Param = 8 0.00000    
Param = 9 0.00000    
Param =10 1.66188         (alph0,  Constant of thermal expansion at Tref x10^5 K^-1)
Param =11 683.340         (Th_E ,  Einstein temperature in K)
Param =12 0.00000    
Param =13 0.00000    
Param =14 0.00000    
Param =15 0.00000    
Param =16 0.00000    
Param =17 0.00000    
Param =18 1.00000         (Gamm0,  Gruneisen parameter at Tref,Pref)
Param =19 0.00000         (q    ,  Gruneisen power law in V/V0)
Param =20 0.00000    
Param =21 0.00000    
Param =22 0.00000    
Param =23 0.00000    
Param =24 0.00000    
Param =25 0.00000    
Param =26 0.00000    
Param =27 0.00000    
Param =28 0.00000    
Param =29 0.00000    
Param =30    Inf     
Param =31 0.00000    
Param =32 0.00000    
Param =33 0.00000    
Param =34 0.00000    
Param =35 0.00000    
Param =36 0.00000    
Param =37 0.00000    
Param =38 0.00000    
Param =39 0.00000    
Param =40 0.00000    
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