Supporting information

Efficient Degradation of Poly(ethylene terephthalate) with Thermobifida fusca Cutinase Exhibiting Improved Catalytic Activity Generated using Mutagenesis and Additive-based Approaches

# Makoto Furukawa, Norifumi Kawakami,* Atsushi Tomizawa and Kenji Miyamoto*

Department of Biosciences and Informatics, Keio University, 3-14-1 Hiyoshi, Kohoku-ku, Yokohama, Kanagawa 223-8522, Japan

E-mail

N.K.: norikawakami@bio.keio.ac.jp

K.M.: kmiyamoto@bio.keio.ac.jp

Figure S1. a)–f) The lcPET (1.2 cm2 mL-1) hydrolysis activity of 1 µM TfCut2 at 40°C–70°C in the presence of Cn-N(CH3)3+ (n=10 magenta, n=12 orange, n=14 green and n=16 blue in panels a to f). The error bars denote the standard deviation calculated from three different experiments.

Figure S2. Relative pNPB hydrolysis activity of 10 nM TfCut2 in the presence of 250 ppm C12-N(CH3)3+. The error bars denote the standard deviation calculated from three different experiments.

Figure S3. Three-hour lcPET degradation rates (1.2 cm2 mL-1) of 1 µM TfCut2 mutants in the absence of surfactant. Each mutation was introduced at F209. The error bars denote the standard deviation calculated from three different experiments.

Figure S4. The effect of Bicine buffer concentration on 24-h lcPET degradation (1.2 cm2 mL-1) by 1 µM G62A/F209A mutant in the presence of 30 ppm C12-N(CH3)3+ at 65°C. The error bars denote the standard deviation calculated from three different experiments.

Figure S5. Three-hour hcPET degradation rates (1.2 cm2 mL-1) of 1 µM enzyme in the presence or absence of 30 ppm C12-N(CH3)3+ at 65°C. The error bars denote the standard deviation calculated from three different experiments.

Table S1. The optimum concentration of each surfactant at 40°C–70°C. These data were experimentally determined (Figure S1).

|  | C10 (ppm) | C12 (ppm) | C14 (ppm) | C16 (ppm) |
| --- | --- | --- | --- | --- |
| 70°C | 100 | 5 | 1 | 0.5 |
| 65°C | 300 | 30 | 3 | 2 |
| 60°C | 500 | 50 | 7 | 2 |
| 55°C | 500 | 50 | 10 | 2 |
| 50°C | 1000 | 100 | 10 | 5 |
| 40°C | 1000 | 100 | 10 | 5 |

Table S2. The product distribution of the 24-h reaction by 1 μM mutant G62A/F209A in 500 μL of reaction solution.

|  | Yield (%)a |
| --- | --- |
| TPA | 62.5 ± 0.8 |
| MHET | 37.5 ± 0.8 |
| BHET | Not detected. |

a Values are averages ± standard deviation calculated from three different experiments.

Table S3. The DNA sequence of TfCut2 (PDBID: 4CG1) for expression in Escherichia coli.

| N-terminus (NdeI) | CATATG |
| --- | --- |
| Sequence of TfCut2 | GCGAACCCCTATGAACGCGGGCCGAATCCTACAGATGCGCTTCTGGAAGCGCGTTCTGGCCCGTTTAGTGTGTCGGAGGAAAACGTTTCGCGTCTGTCAGCGTCTGGATTTGGCGGTGGTACGATTTACTATCCGCGTGAGAACAACACCTATGGTGCAGTCGCCATTTCGCCGGGCTATACCGGAACTGAGGCCTCCATTGCCTGGTTAGGGGAACGCATTGCCTCTCATGGGTTTGTGGTCATCACGATTGATACGATCACCACCCTTGATCAGCCCGATAGTCGGGCAGAACAGCTGAATGCCGCTCTGAACCACATGATCAATCGCGCGTCTAGTACCGTTCGTAGCCGCATTGACAGCAGTCGCTTAGCGGTAATGGGCCATTCCATGGGTGGTGGTGGTAGCTTACGTTTGGCGAGTCAACGGCCAGACCTGAAAGCGGCCATTCCGCTGACACCCTGGCACTTGAACAAGAATTGGTCCTCCGTCACTGTGCCAACCCTGATTATTGGCGCCGACCTCGATACTATCGCACCGGTTGCAACGCATGCCAAACCGTTCTACAATTCGCTGCCTTCAAGCATTTCAAAAGCCTACCTCGAACTGGATGGCGCTACGCACTTTGCGCCTAATATCCCGAATAAGATTATCGGCAAATACTCGGTAGCGTGGTTGAAACGCTTCGTGGACAACGATACCCGCTATACCCAGTTTCTGTGTCCAGGACCGCGTGACGGCCTGTTCGGTGAAGTTGAGGAATATCGCTCAACATGCCCGTTCTATCCGAACAGCAGCAGCGTGGACAAACTCGCAGCTGCTCTGGAA |
| C-terminus (XhoI, His6-tag) | CTCGAGCACCACCACCACCACCACTGA |

Table S4. Primer sequences for site-directed mutagenesis.

| G62A forward | GGCTATACCGCAACTGAGGCC |
| --- | --- |
| G62A reverse | GGCCTCAGTTGCGGTATAGCC |
| H129A forward | GCGGTAATGGGCGCGTCCATGGGT |
| H129A reverse | ACCCATGGACGCGCCCATTACCGC |
| H129W forward | GCGGTAATGGGCTGGTCCATGGGT |
| H129W reverse | ACCCATGGACCAGCCCATTACCGC |
| F209A forward | GGCGCTACGCACGCTGCGCCTAAT |
| F209A reverse | ATTAGG CGCAGCGTGCGTAGCGCC |
| F209S forward | GGCGCTACGCACAGTGCGCCTAAT |
| F209S reverse | ATTAGGCGCACTGTGCGTAGCGCC |
| F209L forward | TGGCGCTACGCACCTGGCGCCTAATA |
| F209L reverse | CGGGATATTAGGCGCCAGGTGCGTAG |
| F209V forward | TGGCGCTACGCACGTGGCGCCTAATA |
| F209V reverse | CGGGATATTAGGCGCCACGTGCGTAG |
| F209W forward | GGCGCTACGCACTGGGCGCCTAAT |
| F209W reverse | ATTAGGCGCCCAGTGCGTAGCGCC |