Near ideal synaptic functionalities in Li ion synaptic transistor using Li3POxSex electrolyte with high ionic conductivity

Revannath Dnyandeo Nikam1,2, Myonghoon Kwak1,2, Jongwon Lee1,2, Krishn Gopal Rajput1,2,

Writam Banerjee, Hyunsang Hwang1,2,*

1Center for Single Atom-based Semiconductor Device, 2Department of Material Science and Engineering, Pohang University of Science and Technology (POSTECH), Pohang 790-784, Republic of Korea

* Authors to whom correspondence should be addressed

Email: hwanghs@postech.ac.kr

Section S1: Simulation for time-dependent calculation of Li ion distribution

To know the amount of Li+ transported from LiCoO2 channel to Si reservoir via electrolyte (Li3PO4 OR Li3POxSex), we have constructed the one dimensional (1D) simulation model. The model geometry used in this simulation is as shown below.

The model geometry consisted 3 domains (channel, electrolyte and Si reservoir).

On the channel side under the electric field the LiCoO2 is dissociating as,

LiCoO2 ↔ Li1-xCoO2 + xLi+ + e-

On the Si reservoir side Li+ associate as,

Si + Li+  SiLi

The hysteresis behavior (volatility or nonvolatility) in lithium ion transistor is determined by the dissociation reaction rate in LiCoO2 (kLCO), association rate in Si reservoir (kSi) and ionic mobility (µion) in electrolyte defined by ionic conductivity of electrolyte.

The reaction kinetics in LiCoO2 channel and in Si reservoir are described using the Butler-Volmer equation as,

i0, LiCoO2 =FkLiCoO2 CLi,max-CLi)CLiCLi,max-CLi,min⁡)CLiLiCoO2 CLi,-CLi,min)CLi,max-CLi,min⁡)1-LiCoO2

Where CLi,max and CLi,min are the maximum and minimum amount of Li+ ion in LiCoO2 channel.

And                                                   --------------(1)

i0, Si =FkSi CLi,max-CLi)CLiCLi,max-CLi,min⁡)CLiSi CLi,-CLi,min)CLi,max-CLi,min⁡)1-Si

During the potentiation, a negative gate pulses initiate the oxidation reaction at the surface of LiCoO2 and produces the Li+ ions. Under the electric field this Li+ migrate toward Si reservoir via electrolyte.

The chemical reaction in electrolyte is as,

Li+  Li0 + n-

The transport Li+ kinetic in electrolyte are described by the Nernst-Plank equation as,

Ni = -Di 𝐷𝑖∇𝑐 +ZiFRT DiCi ∇𝜙l      ----------------(2)

The hysteresis behavior (volatility or nonvolatility) of Li3PO4 and Li3POxSex electrolytes consisted synaptic transistor devices can have explained by knowing the Li+ ion concertation with time in LiCoO2 after the potentiation. To know the Li+ ion concertation with time in LiCoO2, we solve the Equation (1) and (2) using COMSOL multiphysic simulation platform with experimentally know parameters such as thickness of LiCoO2 channel, electrolyte and Si reservoir.

We first experimentally obtained the voltage decay curve with time for device with constant current. Then we simulate the device by tuning the various parameter to know which parameters were the most important in governing the time decay behavior. We finally concluded that the diffusion rate and reaction rates are the important parameter. Then we tuned the parameters during simulation until we obtain better fit to our experimental result.

Figure S1: Experimental and simulation voltage decay curves for Li3PO4 and Li3POxSex electrolytes.

Figure S2: Li+ ion concentration in LiCoO2 after removal of current bias in Li3PO4 and Li3POxSex consisted devices.

Table S1: The parameter used in simulation is given in below table.

| L | Thickness of electrolyte | 200 [nm] |
| --- | --- | --- |
| M | Thickness of electrode | 100 [nm] |
| c0_Li_ion | Total concentration of Li ions in Li3PO4 or Li3POxSex | 6.01×104 [mol/mm3] |
| kr | Li ion recombination reaction rate | 0.9×10-8 -[m^3/(mol*s)] |
| delta | Fraction of free Li ions in equilibrium | 0.18 |
| D_Li_ion | Diffusion coefficient for Li ions in electrolyte | 0.9e-15[m^2/s] |
| D_n | Diffusion coefficient for n in electrolyte | 5.1e-15[m^2/s] |
| c_Li_max | Selected maximal activity of Li, positive electrode | 2.33e4[mol/m^3] |
| D_Li | Diffusion coefficient for Li, positive electrode | 1.76e-15[m^2/s] |
| alpha_pos | Charge transfer coefficient | 0.6 |
| k_LCO | Rate constant charge transfer reaction, positive electrode | 5.1e-4[mol/m^2/s] |
| T | Temperature | 298.15[K] |
| kd | Dissociation rate constant in electrolyte | kr*c0_Li_ion*delta^2/(1-delta) |
| c_Li_ion_init | Initial Li ion electrolyte concentration | c0_Li_ion*delta |
| i_1C | 1C current | 10e-6[A/cm^2] |
| c_Li_init | Initial Li concentration, positive electrode | c_Li_max/2*1.01 |
| C_rate | C rate parameter in parametric sweep | 1 |
| c_Li_min | Minimum Li concentration, positive electrode | c_Li_max/2 |
| alpha_neg | Charge transfer coefficient, negative electrode | 0.5 |
| k_neg | Rate constant charge transfer reaction, negative electrode | 1e-2[mol/m^2/s] |

Section S3: XPS analysis of Li3PO4 and Li3POxSex

Figure S3. Survey XPS spectra of Li3PO4 deposited at 300C.

Figure S4. Survey XPS spectra of Li3POxSex deposited at 300C.

Table S2. Fractional % elemental analysis in Li3PO4 electrolyte from the XPS spectra

| Element | B.E. | Height CPS | FWHM | Area CPS | Atomic % | Structure |
| --- | --- | --- | --- | --- | --- | --- |
| Li (1s) | 56.48 | 1969.19 | 1.97 | 4532.53 | 53.06 | Li3PO4 |
| C (1S) | 290.83 | 3498.82 | 1.37 | 7218.24 | 5.05 |  |
| P (2p) | 134.31 | 5061.2 | 1.91 | 10262.37 | 5.83 |  |
| O (1s) | 532.41 | 68024.47 | 1.78 | 141568.23 | 36.06 |  |

# Fractional % element calculated from %  = (the peak area under (XPS elemental peak)/the sensitivity factor of element ) × 100.

Table S3. Fractional % elemental analysis in Li3POxSex electrolyte from the XPS spectra

| Element | B.E. | Height CPS | FWHM | Area CPS | Atomic % | Structure |
| --- | --- | --- | --- | --- | --- | --- |
| Li1s | 56.22 | 4143.09 | 1.71 | 7725.61 | 53.74 | Li3POxSex |
| P2p | 134.11 | 1476.59 | 1.77 | 2835.43 | 0.96 |  |
| C1s | 291 | 16956.21 | 1.24 | 27941.82 | 11.61 |  |
| Se3p | 161.87 | 1112.28 | 2.37 | 2957.83 | 0.26 |  |
| O1s | 532.81 | 125313.05 | 1.59 | 220876.01 | 33.44 |  |

# Fractional % element calculated from % = (the peak area under (XPS elemental peak)/the sensitivity factor of element) × 100

Section S5: Surface and thickness analysis of Li3PO4 and Li3POxSex using AFM

Figure S5: (A-B) Surface analysis of as grown electrolytes film by atomic force microscopy (AFM). (B-D) Depth profile to demine the exact thickness of as deposited electrolyte.

Section S6:  EIS circuit model

Figure S6: EIS circuit model used to fit the raw data.

Section S7: Se content dependnt swtching behavior of Li3POxSex consisted LIST device.

Figure S7: LTP and LTD characteristics Li3POxSex with varying Se content

The obtained synaptic property with varying Se content in Li3POxSex is summarized in below table.

| % Se content | Initial conductance (nS) | On/off ratio | Asymmetric ratio |
| --- | --- | --- | --- |
| 0.13 | 2.7 | 11 | 1.5 |
| 0.26 | 2.6 | 13 | 0.15 |
| 0.52 | 4.1 | 1.8 | 0.95 |

Note: In ideal symmetric switching the asymmetric ratio is zero.

To change the Se content Li3POxSex electrolyte, we have change the RF power of Se target during deposition. To correlate the RF power and Se content in Li3POxSex we use high resolution XPS analysis. First we fabricated a reference sample of Li3POxSex by giving 10 W RF power to Se target and analyzed with XPS. The obtained XPS result on Li3POxSex reference samples is as below.

Section S8: Individual pulse scheme for endurance test

Figure S8. Schematic of individual pulse scheme used for potentiation and depression during endurance test. During each potentiation and depression cycle 90 pulses with (±1.5 V, 1 s) with 1 s space were used.

Table S4:  Comaparision of ionic conductiviyt of various electrolytes with present study.

| Solid-State electrolyte | Thickness | Li+ conductivity (S cm−1) | Composition | Method | References |
| --- | --- | --- | --- | --- | --- |
| Li3PO4 | 1000 nm | 7 × 10−8 (25°C) | Li2.7PO3.9 | RF sputtering | [1] |
| Li3PO4 | 130 ± 10 nm | 3.3 × 10−8 (25°C) | Li2.8PO2 | ALD | [2] |
| Li3PO4 | 1000 nm | 6.6 × 10−8 (25°C) | Li2.7PO3.9 | RF sputtering | [3] |
| Li3PO4 | 2000 nm | 4 × 10−7 (25°C) | Li3PO4 | PLD | [4] |
| Li3PO4 | 1500 nm | 3.3 × 10−7 (25°C) | Li3PO4 | PLD | [5] |
| Li3PO4 (polycrystalline) | 0.2 cm | 4.2 × 10−18 (25°C) | Li3PO4 | Solid state reaction | [6] |
| Li3PO4 (N2 doping) | 2000 nm | 2.1 × 10−6 (25°C) | Li2.9 PO2.6 N0.91 | RF sputtering | [7] |
| Li3PO4 (N2 doping) | 2000 nm | 1.7 × 10−6 (25°C) | Li1.8 PO1.2 N1.5 | RF sputtering | [7] |
| Li3PO4 (N2 doping) | 2000 nm | 3.1 × 10−6 (25°C) | Li3.3 PO2.9 N0.83 | RF sputtering | [7] |
| Li3PO4 (N2 doping) | 12 nm | 2.71 × 10−10 (25°C) | 0% N content | ALD | [8] |
| Li3PO4 (N2 doping) | 10 nm | 3.36 × 10−7 (25°C) | 10 % N content | ALD | [8] |
| Li3PO4 (Si doping) | 1000 nm | 1.49 × 10−6 (25°C) | Li2.40 Si0.88P0.12O2.28 | RF sputtering | [9] |
| Li3PO4 (Si and N2 doping) | 1000 nm | 2.06 × 10−5 (25°C) | Li1.35 Si0.79P0.21O1.98N0.98 | RF sputtering | [9] |
| Li3PO4 | 200 nm | 1.2 × 10-7 (25°C) |  | RF sputtering | This study |
| Li3PO4 (Se doping) | 200 nm | 2.0 × 10-6 (25°C) |  | RF sputtering | This study |

[1] J. Electrochem. Soc., 144 (1997), pp. 524-532; [2] Nanotechnology 25 (2014) 504007; [3] J. Power Sources 44 103–10; [4] Journal of The Electrochemical Society, 157 (4) A521-A527 (2010); [5] ECS Transactions, 16 (26) 53-60 (2009); [6] J. Solid State Chem. 115 313–23; [7] Solid State Ionics 191 (2011) 49–54; [8] Chemistry of Materials 2015 27 (15), 5324-5331; [9] ACS Appl. Energy Mater. 2019, 2, 4782−4791