SUPPLEMENTARY INFORMATION

Novel multimodal MRI and MicroCT imaging approach to quantify angiogenesis and 3D vascular architecture of biomaterials

Anna Woloszyk, Petra Wolint, Anton S. Becker, Andreas Boss, Weston Fath, Yinghua Tian, Simon P. Hoerstrup, Johanna Buschmann and Maximilian Y. Emmert

Figure S1. Histological analysis of H&E-stained sections of Optimaix and DegraPol samples. a, Number of vessels per mm2 of scaffold area. b, Total branch length in mm per mm2 of scaffold area. c, Mean branch length in mm per mm2 of scaffold area. d, Mean radius in μm. e, Vessel area in %. f, Angle difference from 90°. g, H&E staining of an Optimaix scaffold. Asterisks indicate collagen fibers of the scaffold. Dashed line highlights a pore within the scaffold. Black arrows show the direction of the ingrowing blood vessels. h, H&E staining of a DegraPol scaffold. Asterisks indicate the scaffold material. Abbreviations: DP - DegraPol, OM -  Optimaix. All measurements were taken from distinct samples. Mean ± SE, n = 4, scale bar = 200 μm.

Table S1. Correlation coefficients R for the comparison of MicroCT readouts with perfusion capacity assessed by MRI for the interface, middle, and surface. Key: white -0.25<R<0.25 (no correlation); light grey -0.5<R<-0.25 & 0.25<R<0.5 (weak correlation); medium grey -0.75<R<-0.5 & 0.5<R<0.75 (moderate correlation); dark grey -1<R<-0.75 & 0.75<R<1 (strong correlation).

|  |  | Optimaix |  | DegraPol |  |
| --- | --- | --- | --- | --- | --- |
|  | MRI vs. MicroCT parameters | before despeckle | after despeckle | before despeckle | after despeckle |
| INTERFACE | Total vessel volume (mm3) | 0.3854 | 0.4187 | 0.1142 | -0.2418 |
|  | # Branches | 0.7585 | 0.2541 | -0.6152 | 0.378 |
|  | # Junctions | 0.6975 | 0.5827 | -0.602 | -0.3631 |
|  | # Branches/Junction | -0.752 | -0.5934 | 0.3878 | 0.5933 |
|  | Total branch length (mm) | 0.7384 | 0.601 | 0.05386 | -0.1565 |
|  | Mean branch length (mm) | 0.4959 | 0.47 | 0.9479 | -0.5765 |
|  | Mean vessel radius (mm) | -0.7879 | -0.6766 | 0.6114 | -0.03088 |
| MIDDLE | Total vessel volume (mm3) | 0.09595 | 0.8414 | 0.9094 | -0.574 |
|  | # Branches | -0.1859 | 0.8128 | 0.07018 | -0.8033 |
|  | # Junctions | -0.5539 | 0.5221 | 0.02697 | -0.7783 |
|  | # Branches/Junction | 0.8876 | 0.8173 | -0.2345 | -0.03226 |
|  | Total branch length (mm) | -0.4538 | 0.9724 | 0.3066 | -0.7749 |
|  | Mean branch length (mm) | -0.08257 | -0.805 | 0.3716 | 0.911 |
|  | Mean vessel radius (mm) | 0.002442 | 0.562 | 0.7922 | 0.8467 |
| SURFACE | Total vessel volume (mm3) | 0.7551 | 0.9276 | -0.2136 | -0.6925 |
|  | # Branches | -0.6577 | 0.9276 | -0.3181 | 0.8947 |
|  | # Junctions | -0.6719 | 0.5319 | -0.2887 | 0.8798 |
|  | # Branches/Junction | -0.3863 | -0.1897 | 0.4522 | 0.1122 |
|  | Total branch length (mm) | 0.6456 | 0.8298 | -0.2426 | 0.8203 |
|  | Mean branch length (mm) | 0.6388 | -0.8854 | 0.8476 | -0.4949 |
|  | Mean vessel radius (mm) | 0.6348 | 0.832 | -0.1624 | 0.01373 |

Video S1: MicroFil perfusion of the CAM.