# A new nonlinear viscoelastic model and mathematical solution of solids for improving prediction accuracy

Qinwu Xu1,2, Björn Engquist12,3,*, Mansour Solaimanian4, Kezhen Yan1,*

# Supplementary Material

# Senstivity analysis of model parameters

We applied the proposed model to agar and bone materials for sensitivity analysis of model parameters. Model results show that a higher μ value results in higher E(t) value without changing other model parameters (see Fig. 1a for the agar material); while a higher α value induces a higher modulus variation rate such that ∂E(t)/∂t∝α (see Fig. 1b for the bone material).

1School of Civil Engineering, Yango University, Fuzhou, Fujian 350015 China. 2Institute for Computational Engineering and Sciences and 3Department of Mathematics, the University of Texas at Austin, Austin, TX 78712 USA. 4Civil and Environmental Engineering, Penn State, State College, PA 16801 USA. Correspondence and requests for materials should be addressed to K. Yan (email:yankz2004@163.com) and B. Engquist (email: engquist@oden.utexas.edu).

Supplementary Fig. 1. Model parameter sensitivity analysis for: (a) agar material (experimental data was reproduced from [41]. and (b) bone materials using proposed model (experimental data was reproduced from [1]). Note: τ=1s for constant temperature.

# Model derivation for complex modulus

According the model format shown in Fig. 2, the stress and strain equilibrium satisfies the following (all in frequency domain):

εeiω=ε0eiω                                                        (1)

ε0eiω=ε1eiω+ε2eiω                                  (2)

σeiω=E∞ε0eiω+ERε1eiω                          (3)

σ1eiω=ERε1eiω=σ2eiω=

e+iϕμτ(ωτ)1-αε2eiω                                               (4)

ε1eiω+ε2eiω=ε0eiω                                   (5)

η,μ,τ, ση, ε2

E0-E∞, σ1, ε1

E∞, σ0, ε0

σeiω,εeiω

σeiω

Supplementary Fig. 2. Model format in spring-dashpot system.

From Equation 4, the strain of ε2eiω can be derived as:

ε2eiω=ERe-iϕτμ(ωτ)α-1ε1eiω                    (6)

Substitute Equation 6 into 5 to attain the ratio of ε1/ε0:

ε1eiωε0eiω=11+ERe-iϕτμ(ωτ)α-1                                (7)

Substitute Equation 7 to 3 and divide it by εeiω to attain the model expression for complex modulus as follows:

E*ω=σeiωεeiω=σeiωε0eiω=E∞+ERERe-iϕτμ(ωτ)α-1+1=E∞+ERμ/τeiϕ(ωτ)1-αER+μ/τeiϕ(ωτ)1-α             (8)

# Thermodynamic consistency

To ensure thermodynamic consistency, the Calusius-Duhem inequality shall be satisfied [2] as follows:

ρcT=-ρ∂Π∂t+σ∂ε∂t-ρs∂T∂t+c∂T∂x2≥0            (9)

where ρTc is a specific energy dissipation term, c is thermal conductivity, Π is the specific free energy, ε is the total strain of the model system, and s is the specific entropy.

The possibility of this inequality can be proven in the following.

The total strain can be decomposed into two parts as follows:

ε=ε0+εT=ε1+ε2+εT=ε1+ε2+αTΔT                    (10)

where ε0 is the total mechanical strain of the model - the same as the strain posed by E∞, εT is the thermal strain equals to αTΔT, αT is the coefficient of thermal expansion, and ΔT is temperature variation of the model system.

The total stress can be decomposed into two parts:

σ=σ0+σ1=σ0+ση                                          (11)

where σ0 is the elastic stress at infinite time posed by E∞, and ση is the stress posed by the dashpot – the same as that posed by spring network ER=E0-E∞.

The free energy of the model system can be given as:

Π=Π0ε0,T+Π1ε1,T+πT                     (12)

Π0ε0,T is the energy stored by E∞, Π1εe,T is the energy stored by the elastic network ER, and π(T) is a heat capacity related energy.

Substitute Equation 10 and Equation 12 into Equation 9 to reach the following equilibrium:

ρcT=-ρ∂Π0∂tε0,T+∂Π1∂tε1,T+∂π∂tT+σ∂ε0∂t+∂εT∂t-ρs∂T∂t+c∂T∂x2                                (13)

Substitute Equation 9 to 11 into Equation 13, and apply the chain rule to achieve the following:

ρcT=-ρ∂Π0∂ε0∂ε0∂t+∂Π0∂T∂εT∂t+∂Π1∂ε1∂ε1∂t+∂Π1∂T∂εT∂t+∂π∂T∂T∂t+σ0∂ε0∂t+ση∂ε1∂t+∂ε2∂t+σαT∂T∂t-ρs∂T∂t+c∂T∂x2                           (14)

This can ber rearranged as follows:

ρcT=σ0-ρ∂Π0∂ε0∂ε0∂t+ση-ρ∂Π1∂ε1∂ε1∂t

+σαT+∂Π0∂T+∂π∂T-ρs-ρ∂Π1∂T∂T∂t+ση∂ε2∂t+c∂T∂x2                            (15)

∂ε0∂t,∂ε1∂t,∂T∂t can be arbitrary, and thus the coefficients of the terms of ∂ε0∂t,∂ε1∂t,∂T∂t have to vanish to satisfy ρTγ≥0. Therefore, Equation 15 may be reduced to:

ρcT=ση∂ε2∂t+c∂T∂x2                                          (16)

The stress of the viscous dashpot can be expressed as ση=η∂ε2∂t (η is viscosity of the dashpot) and thus Equation 16 satisfies:

ρcT=η∂ε2∂t2+γ∂T∂x2≥0                         (17)

# Experimental validation

The model parameters are determined by fitting on experimental data using optimization skills. The nonlinear reduced gradient method was used to fit the model parameters by minimizing the objective function fx1,x2,….,xm  ∀ xi>0:

fx1,x2,….,xm =iNEix1,x2,….,xm-Ei2       (18)

where xi is the model parameters, e.g., for generalized Maxwell (GM) model xi=Ei and ηi, N is the total number of experimental data points, Ei and Ei is the ith modeled and measured modulus value, respectively.

For this optimization method, the gradients (derivatives with respect to each model parameter) are calculated based on the central finite difference (CFD) method. The iteration goal is to satisfy the first order essential optimal condition (i.e. the gradient is or close to zero).

It is known that inverse computation is generally dependent on seed values and it may turn out multiple results of model parameters which all satisify the optimization objective. This is especially true for the model with higher number of parameters such as GM model and its Prony series (PS) formula. Fig. 3 illustrates the optimization results for the PS with n=2 (standard solid model) and the proposed model (both have five model parameters) using different seed values that consdier three general cases: 1) modulus valus are higher, 2) lower, and 3) close to as compared to true values. The seeds and output values of model parametr are listed in Table 1. Results have shown that the proposed model yilds more unique solutions and E(t) shapes than the PS when using different seed values, indicating its higher stability (see Fig. 3a vs. 3b). When using a relatively large term number for the PS, its variability (e.g. different combinations of Ei and ηi values) can be larger, and it could be difficult to estimate property seed values for achiving more unique solutions. In comparison, the porposefd model uses much leass model parameters , but it is still able to caputure the full time range. It is also easier to estimate proper seed values such as E∞ and E0 values according to the expeimrental data range.

Supplementary Fig. 3. Optimization analysis: (a) Prony series with n=2 with 5 model parameters and (b) proposed model for polyurethane polymer materials.

Supplementary Table 1. Model seed and output after optimization to fit experimental data.

- GM model (n=1) or standard solid model

- Proposed model

Note: τ=1 for constant temperature.

We present model fitting and prediction results of an agar material in Supplementary Fig. 4. Result shows that the proposed model for agar material attained relatively close results for fitting and predictions (see Supplementary Fig. 4a). In comparison, the GM model has slightly over-predicted E(t) at high time range and produced less stability in the low time ranges (Supplementary Fig. 4b).

Supplementary Fig. 4. Model fit and prediction of agar material: (a) proposed model and (b) proposed model versus the GM model and Prony series (experimental data of agar was reproduced from [3]).

We present model fitting and prediction results of a bovine bone material in Supplementary Fig. 5. Result shows that the proposed model produces a smoother and still accurate curve fitting. The PS over-predicts E(t) at the high time range and produced gaps to measurement values as it intends to rapidly converge to E∞ once it is outside of the time range of fitted data.

Supplementary Fig. 5. Model fit and prediction of bovine femoral bones (experimental data of bone was reproduced from ([4]).

Table 2 lists the fitted model parameters of the GM model for the agarose gel, vaginal tissue, bone and agar materials.

Supplementary Table 2. Fitted model parameters of GM model (n=14): a). agarose gel; b) vaginal tissue; c) bone; and d) agar materials.

- b)

- d)

- N. Sasaki and M. Yoshikawa (1993) Stress relaxation in native and EDTA-treated bone as a function of mineral content. Journal of Biomechanics 26, 77-83.

- Haupt P. 1993 Non-equilibrium thermodynamics with applications to solids. In CISM-Course 336 (ed. W. Muschik), pp. 138–140. New York, NY: Springer.

- Shen J, Cheng P, Gu W, Hao Z. 2013 Stress relaxation measurement of viscoelastic materials using a polymer-based microfluidic device. Sens. Actuators, A 203, 119–130. (doi:10.1016/j.sna.2013.08.038)

- Sasaki N. 2012 Viscoelastic properties of biological materials. In Viscoelasticity - From theory to biological applications (ed. JD Vincente), pp. 99–122. Intech.