Supplementary Information

Title

Controlling oxygen coordination and valence of network forming cations

Takuya Aoyagi, Shinji Kohara, Takashi Naito, Yohei Onodera, Motomune Kodama, Taigo Onodera, Daiko Takamatsu, Shuta Tahara, Osami Sakata, Tatsuya Miyake, Kentaro Suzuya, Koji Ohara, Takeshi Usuki, and Yamato Hayashi and Hirotsugu Takizawa

Figure S1 Normalized XANES spectra at V K-edge in VPx glasses. Absorption-energy at normalized intensity of 0.5 shifted to low energy as amount of P2O5 increased which means that vanadium was reduced by adding P2O5.

Figure S2 Comparison between neutron/synchrotron X-ray data and RMC model for VPx glasses. a, Neutron total structure factor SN(Q). b, X-ray total structure factor SX(Q). c, EXAFS k3χ(k). EXAFS k3χ(k) data were obtained by back Fourier transformation of |FT(R)| of first correlation peak. Black curve, experimental data; Coloured curve, RMC model.

Figure S3  Raman spectra of VPx glasses. Peaks attributable to Q2 and Q3 sites appearing at more than 1150 cm−1 were not observed.

Figure S4  51V MAS-NMR spectra of VPx glass samples.

Figure S5  Relationship between normalized weight loss in water and fraction of V5+O4 units in all cations.

Figure S6  Atomic packing density of VPx glasses. The density was calculated in accordance with literature50. Ionic radius of tetravalent vanadium in V4+O4 was assumed by linear approximation from ionic radius of V4+O5 and V4+O6 since it was not in data. Black point, calculated from literature data24; Blue point, experimental data.

Figure S7  Fraction of -M-O-ring distribution in VPx glasses. Purple, amorphous-VP0; Red, VP10 glass; Green, VP28 glass; Blue, VP44 glass.

Table S1  Fraction of V5+O4, V5+O5 and V5+O6 units in VPx glasses obtained with 51V MAS-NMR spectra.

| Composition | Fraction of V5+ structural units |  |  |  |
| --- | --- | --- | --- | --- |
|  | VO5 (−300 ppm) | VO6 (−490 ppm) | d-VO4 (−540 ppm) | s-VO4 (−750 ppm) |
| VP10 | 0.27 | 0.08 | 0.12 | 0.53 |
| VP28 | 0.45 | 0.05 | 0.47 | 0.03 |
| VP44 | 0.81 | 0.10 | 0.08 | 0.02 |