Supplementary Information

Controlling Electronic States of Few-walled Carbon Nanotube Yarn via Joule-annealing and p-type Doping Towards Large Thermoelectric Power Factor

May Thu Zar Myinta,b, Takeshi Nishikawaa, Kazuki Omotoa, Hirotaka Inouea, Yoshifumi Yamashitaa, Aung Ko Ko Kyawc*,Yasuhiko Hayashia*

a Graduate School of Natural Science and Technology, Okayama University, Okayama, 700-8530, Japan.

b Faculty of Advanced Materials Engineering, University of Technology (Yatanarpon Cyber City), Pyin Oo Lwin District, Mandalay Division, Myanmar.

c Department of Electrical and Electronic Engineering, Southern University of Science and Technology, Shenzhen 518055, P. R. China.

E-mail: hayashi.yasuhiko@okayama-u.ac.jp and aung@sustech.edu.cn

Contents

Figures

Figure S1:	SEM images of pristine, Joule-annealed and Joule-annealed followed by F4TCNQ doped CNT yarn.

Figure S2:	Fitted curves of the temperature dependence Seebeck coefficient for pristine, Joule-annealed and Joule-annealed followed by F4TCNQ doped CNT yarn.

Figure S3:	Relationship between the amount of joule-annealing and the intensity of 2D band to G band.

Figure S4: 	Possible mechanism of morphology-change after Joule-annealing and doping.

Figure S5:	Raman spectrum of F4TCNQ.

Figure S6:	TEM images of pristine, Joule-annealed and Joule-annealed followed by   
  		F4TCNQ doped CNT yarn.

Figure S7:	TGA analysis of the CNT yarn before and after Joule-annealing.

Tables

Table S1:	The values of the intensity ratio of IG/ID and I2D/IG.

Pristine

(a)

Joule-annealing

(b)

2.5 mg/ml F4TCNQ doped

(c)

10 mg/ml F4TCNQ doped

(d)

Figure S1: SEM images of (a) pristine, (b) Joule-annealed, (c) Joule-annealed followed by 2.5 mg/ml F4TCNQ doped, and  (d) Joule-annealed followed by 10 mg/ml F4TCNQ doped FWCNT yarns.

Table S1: The values of the intensity ratio of IG/ID and I2D/IG.

| Joule Heat (W) | IG/ID | I2D/IG |
| --- | --- | --- |
| 0 (pristine) | 1 | 0.3 |
| 1 | 1.6 | 0.5 |
| 2 | 5 | 0.5 |
| 3 | 11.2 | 0.5 |
| 3.4 | 15.7 | 0.4 |
| 4 | 17.8 | 0.7 |

Figure S2: Fitted curves of the temperature dependent Seebeck coefficient for (a) pristine, (b) Joule-annealed and (c) Joule-annealing followed by F4TCNQ doped FWCNT yarns.

Figure S3: Relationship between the amount of joule-annealing and the intensity of 2D band to G band in Raman spectroscopy, indication of the formation of multi-layered graphene structure on the surface of FWCNT yarn.

Figure S4: Possible mechanism of morphology-change after Joule-annealing and doping.

Figure S5: Raman spectrum of F4TCNQ.

Figure S6: TEM images of (a) pristine, (b) Joule-annealed, and (c) Joule-annealing followed by 2.5 mg/ml F4TCNQ doped FWCNT yarns.

Figure S7: TGA analysis of the FWCNT yarn before and after Joule-annealing.