Investigation on the Electrochemical Performances of Mn2O3 as a Potential Anode for Na-Ion Batteries

Nor Fazila Mahamad Yusoffa, Nurul Hayati Idrisa,* , Mohd Faiz Md Dinb,                           Siti Rohana Majidc, Noor Aniza Harund and Md Mokhlesur Rahmane,*

a Energy Storage Research Group, Faculty of Ocean Engineering Technology and Informatics, Universiti Malaysia Terengganu 21300 Kuala Nerus, Terengganu, Malaysia

b Department of Electrical and Electronic Engineering, Faculty of Engineering, National Defence University of Malaysia , Kem Sungai Besi, 57000 Kuala Lumpur, Malaysia

c Center for Ionics University of Malaya, Department of Physics, Faculty of Science, University of Malaya 50603 Kuala Lumpur, Malaysia

d Advance Nano Materials (ANOMA) Research Group, Faculty of Science and Marine Environment, Universiti Malaysia Terengganu 21300 Kuala Nerus, Terengganu, Malaysia

e Institute for Frontier Materials, Deakin University, Waurn Ponds, Victoria 3216, Australia

*Corresponding authors

Tel.: +60 96683185; fax: +6096683391.

E-mail address: nurulhayati@umt.edu.my (N. H. Idris)

m.rahman@deakin.edu.au (M. M. Rahman)

Supporting information

Table S1. Rietveld refinement results of the MnCO3 and Mn2O3. The standard errors derived from the refinements are also listed in lattice columns.

| Sample | a (Å) | c (Å) | Bragg Rfactor (%) | Rf factor (%) | 2 |
| --- | --- | --- | --- | --- | --- |
| MnCO3 (C) | 4.8045 (3) | 15.6891(8) | 9.45 | 5.65 | 0.846 |
| MnCO3 (S) | 4.8019 (2) | 15.6798(1) | 6.70 | 4.81 | 0.736 |
| Mn2O3(C600) | 9.3996 (0) | - | 3.93 | 3.91 | 2.760 |
| Mn2O3 (S500) | 9.3990 (0) | - | 6.39 | 6.33 | 7.740 |
| Mn2O3 (S600) | 9.4043 (3) | - | 7.34 | 5.88 | 0.892 |
| Mn2O3 (S700) | 9.4057 (3) | - | 7.63 | 7.86 | 0.600 |

Table S2. The specific surface area of Mn2O3 samples.

| Sample | BET surface area (m2/g) |
| --- | --- |
| Mn2O3 (C600) | 13.3268 |
| Mn2O3 (S500) | 27.5512 |
| Mn2O3 (S600) | 20.2528 |
| Mn2O3 (S700) | 10.1416 |

Fig. S1.

Fig. S1. XRD pattern of the MnCO3 (C) sample calcined at 300°C.

Fig. S2.

Fig. S2. SEM images of (a) MnCO3 (C) and (b) MnCO3(S).

Fig. S3.

Fig. S3. TEM image of Mn2O3 (S600).

Fig. S4.

Fig. S4. HRTEM image for sample of Mn2O3 (S600).
Fig. S5.

Fig. S5. N2 adsorption-desorption isotherms and BJH pore-size distribution curves (inset) of (a) Mn2O3 (C600), (b) Mn2O3 (S500), (c) Mn2O3 (S600), and Mn2O3 (S700).

Fig. S6.

Fig. S6. CV curves of (a) Mn2O3 (C600), (b) Mn2O3 (S500), (c) Mn2O3 (S600), and (d) Mn2O3 (S700) at a scan rate of 0.3 mV s-1 (versus Na/Na+).

Fig. S7.

Fig. S7. Ex-situ XRD patterns of Mn2O3 electrode obtained at different charge-discharge state.