Supplementary Information

Sequential delithiation behavior and structural rearrangement of a nanoscale composite-structured Li1.2Ni0.2Mn0.6O2 during charge–discharge cycles

Keiji Shimoda1,*, Koji Yazawa2, Toshiyuki Matsunaga1, Miwa Murakami1, Keisuke Yamanaka3, Toshiaki Ohta3, Eiichiro Matsubara4, Zempachi Ogumi1, Takeshi Abe5

1 Office of Society-Academia Collaboration for Innovation, Kyoto University, Uji, Kyoto 611-0011, Japan

2 JEOL RESONANCE Inc., Akishima, Tokyo 196-8558, Japan

3 SR Center, Ritsumeikan University, Kusatsu, Shiga 525-8577, Japan

4 Department of Materials Science and Engineering, Kyoto University, Kyoto 606-8501, Japan

5 Gradual School of Global Environmental Studies, Kyoto University, Katsura, Nishikyo, Kyoto 615-8510, Japan

- (a) Charge–discharge profiles and (b) dQ/dV curves of the Li//Li1.2Ni0.2Mn0.6O2 cell up to the 20th cycle. The electrochemical measurements were performed at 50 °C between 2.0 and 4.8 V vs. Li/Li+ with a constant current of 20.5 mA g–1.

- (a) HAADF-STEM images of the pristine Li1.2Ni0.2Mn0.6O2 sample. (b) EDS mapping images and its intensity profile (gray value) in the rectangular region. The HAADF-STEM images were acquired at an accelerating voltage of 200 kV in the drift corrected frames integration (DCFI) mode using Talos F200X (FEI).

Fig. S2. (continued).

- SR-XRD profiles of the Li1.2Ni0.2Mn0.6O2 electrode at the 1st cycle. The superlattice peaks (020 and 110 reflections) of the C2/m structure were enlarged. The sample numbers are described in Fig. 1.

- Comparison of 6,7Li MAS NMR spectra of the pristine Li1.2Ni0.2Mn0.6O2 sample.

- Peak deconvolution of the 7Li pj-MATPASS spectra of the Li1.2Ni0.2Mn0.6O2 electrode at the 1st cycle.

- 6Li MAS NMR spectra of Li2MnO3 and Ni-doped Li2MnO3 samples. These spectra were acquired with the spinning rate of 100 kHz. Asterisks indicate spinning sidebands.

- Difference pj-MATPASS difference spectra of the Li1.2Ni0.2Mn0.6O2 electrode at the 1st cycle..

- Evolution of each 7Li signal component in Fig. S5 during the 1st cycle. Component p1: 1514 ppm, p2: 1331 ppm, p3: 791 ppm, p4: 749 ppm, p5: 553 ppm, p6: 352 ppm, and p7: 666 ppm (a new component in #7).

- Evolution of the LiTM/LiLi ratio in the Li1.2Ni0.2Mn0.6O2 electrode during the 1st cycle.

- Evolution of the 1514 ppm peak position during the 1st cycle.

Table S1. The average Ni and Mn valence states estimated from the soft XAS.

|  | Sampling point | Ratio of Ni2+ | Ratio of Ni4+ | Average Ni valence |
| --- | --- | --- | --- | --- |
| 1st cycle | #1 | 0.53 | 0.47 | 2.9 b |
|  | #3 | 0 | 1 a | 4 |
|  | #4 | 0.21 | 0.79 | 3.6 |
|  | #5 | 0.50 | 0.50 | 3.0 |
|  | #7 | 1 a | 0 | 2 |
| 2nd cycle | #9 | 0.52 | 0.48 | 3.0 |
|  | #10 | 1 | 0 | 2 |
| 20th cycle | #11 | 0.72 | 0.28 | 2.6 |
|  | #12 | 1 | 0 | 2 |

|  | Sampling point | Ratio of Mn2+ c | Ratio of Mn3+ c | Ratio of Mn4+ c | Average Mn valence |
| --- | --- | --- | --- | --- | --- |
| 1st cycle | #1 | 0.0 | 0.03 | 0.97 | 4.0 |
|  | #3 | 0.0 | 0.08 | 0.93 | 3.9 |
|  | #4 | 0.0 | 0.12 | 0.88 | 3.9 |
|  | #5 | 0.0 | 0.15 | 0.85 | 3.8 |
|  | #7 | 0.0 | 0.51 | 0.49 | 3.5 |
| 2nd cycle | #9 | 0.0 | 0.14 | 0.86 | 3.9 |
|  | #10 | 0.0 | 0.63 | 0.37 | 3.4 |
| 20th cycle | #11 | 0.0 | 0.29 | 0.71 | 3.7 |
|  | #12 | 0.0 | 0.74 | 0.26 | 3.3 |

a For the linear combination fitting of the Ni LIII-edge spectra, it was assumed that the spectra #3 and #7 are representative of Ni4+ and Ni2+ states, respectively.

b The average Ni valence for the pristine sample seems to be overestimated probably due to larger contributions from the particle surface and/or incomplete assumption described above.

c For the linear combination fitting of the Mn LIII-edge spectra, the reference spectra of MnO (Mn2+), Mn2O3 (Mn3+), and Li2MnO3 (Mn4+) were used.

Determination of chemical composition and ratio of the nanodomains

The chemical compositions of the three phases were determined as follows: The Li2MnO3 domain was clearly identified from 749 and 1514 ppm signals in the 7Li MAS NMR spectrum. The LiTM/LiLi intensity ratio was 0.37 (ideally 0.33). Therefore, the calculated composition is expressed as Li1.37Mn4+0.63O2(–), where oxygen vacancy may be introduced for charge neutrality. Similarly, Li2[Ni1/6Mn5/6]O3-like domain was identified from 553 and 1331 ppm signals. The LiTM/LiLi ratio was 0.26, and the Ni/Mn ratio was fixed at 1/5, and the calculated composition is expressed as Li1.26Ni4+0.11Mn4+0.57O2, assuming that the Ni valence is 4+ in Li2MO3. We know the Li content in each domain from 7Li MAS NMR spectrum; Li1.37Mn0.63O2 : Li1.26Ni0.11Mn0.57O2 : LiMO2 = 0.33 : 0.30 : 0.37. This should be rescaled as Li1.37Mn0.63O2 : Li1.26Ni0.11Mn0.57O2 : LiMO2 = 0.28 : 0.28 : 0.43 (normalized to O). Then, the remaining LiMO2 phase composition can be calculated by subtracting 0.28Li1.37Mn0.63O2 and 0.28Li1.26Ni0.11Mn0.57O2 from the bulk composition Li1.17Ni0.21Mn0.59O2, that is, 0.43LiNi0.41Mn0.57O2.