Nitrogen-rich graphitic-carbon@graphene as a metal-free electrocatalyst for oxygen reduction reaction

Halima Begum, Mohammad Shamsuddin Ahmed, Young-Bae Kim*

Department of Mechanical Engineering, Chonnam National University, Gwangju, Republic of Korea. *E-mail address: ybkim@chonnam.ac.kr

Electrochemical characterization.

An ink of RGO and/or Ng-C@G (2 mg mL−1 in ethanol) was prepared with ultrasonic agitation for 30 min in order to better dispersion. The prepolished glassy carbon electrode (GCE) of rotating ring disk electrode (RRDE) was then drop coated by a 10 μL portion of RGO and/or Ng-C@G ink separately. For the preparation of 20% Pt/C (E-TEK), the suspension of 1 mg mL−1 with 5 μL of Nafion (5%) in ethanol was dropped onto GCE. All electrochemical techniques were recorded using a CHI 700C electrochemical workstation (U.S.A.) three-electrode potentiostat and an EG&G Model 636 RDE system along with the CHI 700C used for RRDE measurements in high purity argon (Ar)- or O2-purged (for at least 30 min) alkaline solution at room temperature (RT). A carbon-rod and Ag/AgCl electrode were used as counter and reference electrode, respectively. The electrode potential was determined with respect to reversible hydrogen electrode (RHE) scale according to the Nernst equation: (ERHE=EAg/AgCl+0.059 pH + E°0.197 V, at 25 °C).

Instrumental Characterization

The transmission electron microscopy (TEM) and energy dispersive X-ray spectroscopy (EDS) were carried out using a Tecnai 20 microscope at 200 kV. The surface morphology was also characterized by a JSM-7500F JEOL for field emission scanning electron microscope (FESEM). Crystal structure was examined by X-ray diffraction (XRD), which was carried out on a Rigaku D/max-2500, using filtered Cu K radiation. Detailed chemical compositions of the samples were analyzed by X-ray photoelectron spectroscopy (XPS) using a VG multilab 2000 spectrometer (Thermo VG Scientific, Southend-on-Sea, Essex, UK) in an ultrahigh vacuum using an unmonochromatized Mg K (1253.6 eV) radiation source and a spherical section analyzer. BET surface area and pore size distribution were obtained through the Barrett-Joyner-Halenda method by nitrogen isotherm adsorption and desorption (BelsorpII mini, BEL Japan Inc.). Raman spectra were collected with a LabRam HR800 UV Raman microscope (Horiba Jobin-Yvon, France), at an excitation wavelength of 514 nm using an argon ion (Ar+) laser.

Koutecky–Levich equation

1j=1jk+1jL					                  (1)

jL = Bω1/2 =0.62nFADO22/3CO2v-1/6ω1/2 	                   (2)

jk = nFkCO2					                    (3)

where j for measured current densities (mA cm−2); A for surface area of working electrode (0.196 cm2); F for Faraday constant (96485.3 C mol−1), DO2 for O2 diffusion coefficient (1.9  10−5 cm2 s−1); CO2 for O2 bulk concentration (1.2 mM L−1); v for kinetic viscosity of 0.1 M KOH (1  10−2 cm2 s−1); ω for revolution speed of electrode (ω = 2π*rpm); k for electron-transfer rate constant and B is a factor which yield from slope of jk–1 vs. ω–1/2 straight line plot.

Figure S1: The SEM images of RGO (a) and Ng-C@G (with 25 µL aniline addition) (b).

Figure S2: TEM images of GOPANI (a) and Ng-C@G at 800 ℃ (b).

Figure S3: The SEM image of pure PANI derived carbon (a) and enlarged SEM image (Figure 2c) of the Ng-C@G at 800 ℃ (b).

Figure S4: The XPS survey spectra (a) and the C 1s XPS spectra (b) of GO, GOPANI, RGO at 800 ℃, Ng-C@G at 800 ℃, and the N 1s XPS spectrum of Ng-C@G at 900 ℃ (c).

Figure S5: The enlarged LSVs of ORR on Ng-C@G and Pt/C catalysts (a) and LSVs of ORR on Ng-C@G which prepared with various addition of aniline (b) in O2-saturated 0.1 M KOH solution at a scan rate of 5 mV s−1 and at 1600 rpm rotation speed.

Figure S6: Cyclic voltammetry of different modified electrodes in a 0.1 M KCl containing with 5.0 mM [Fe(CN)6]3−/4− redox probe solution at a scan rate of 50 mV s−1 (a), and the enlarged LSVs of ORR on Ng-C@G (red) and Pt/C (green) catalysts in O2-saturated 0.1 M HClO4 solution with comparison of Pt/C in 0.1 M KOH solution (black) at a scan rate of 5 mV s−1 and at 1600 rpm rotation speed (b).

Figure S7: The Tafel plots of Ng-C@G, RGO and Pt/C catalysts during ORR in O2-saturated 0.1 M KOH solution.

Figure S8: Current vs. time curves of Ng-C@G and Pt/C at −0.3 V in 0.1 M KOH with the addition of 3 M methanol.

Table S1: The comparison of ORR properties on tested catalysts with other metal-free ORR catalysts.

| Catalysts | Eonset (VRHE) | E1/2 (VRHE) | n value @ 0.6 VRHE | References |
| --- | --- | --- | --- | --- |
| Ng-C@G | 0.96 | 0.806 | 3.96 | This work |
| N-HC@G-900 | 1.0 | 0.85 | 3.9 | [1]2018 |
| BN-CNOs | ~0.78 | ~68 | 3.94 | [2]2018 |
| 30%MIL/PPy-800 | 0.997 | 0.864 | ~3.79 | [3]2018 |
| SN-C@ 800 | 0.962 | 0.865 | 4 | [4]2018 |
| N-pGF | ~0.86 | ~0.76 | 3.9 | [5]2018 |
| N,S1,S2-CM1000-b | 0.98 | ~0.86 | ~3.85 | [6]2018 |
| NCF | 0.93 | ~0.83 | 3.8 | [7]2018 |
| N-GA-150 | ~0.95 | ~0.78 | 3.7 | [8]2018 |
| N′N-GDY | 0.98 | 0.83 | ~3.9 | [9]2017 |
| N,F-Carbon-1000 | 0.97 | 0.84 | 3.92 | [10]2017 |
| BCN | 0.94 | 0.82 | 3.93 | [11]2017 |
| NL-C | 0.95 | 0.86 | ~4 | [12]2016 |
| NGM | 0.89 | 0.77 | 3.8 | [13]2016 |
| N-CNS-120 | 0.9 | 0.77 | 3.9 | [14]2016 |
| NPGC-950 | 0.91 | 0.78 | 3.79 | [15]2016 |
| NCNP−CNF | 0.84 | ~0.77 | 3.5 | [16]2016 |
| N-CNF aerogel | ~0.94 | 0.8 | 3.96 | [17]2015 |
| NGA900 | 0.914 | 0.828 | 3.9 | [18]2015 |
| N-C@CNT-900 | 0.94 | 0.81 | 3.9 | [19]2015 |
| BN-GQD/G-10 | 0.98 | ~0.82 | 3.93 | [20]2014 |

~eye estimated

References

- J. Sun, S. E. Lowe, L. Zhang, Y. Wang, K. Pang, Y. Wang, Y. Zhong, P. Liu, K. Zhao, Z. Tang, H. Zhao, Angew. Chem. Int. Ed. 2018, 57, 16511–16515.

- A. Camisasca, A. Sacco, R. Brescia, S. Giordani, ACS Appl. Nano Mater. 2018, 1, 5763−5773.

- J. Tong, W. Li, L. Bo, J. Ma, T. Li, Y. Li, Q. Zhang, H. Fan, ACS Sustainable Chem. Eng. 2018, 6, 8383−8391.

- J. Tong, W. Li, J. Ma, W. Wang, L. Bo, Z. Lei, A. Mahboob, ACS Appl. Energy Mater. 2018, 1, 5746−5754.

- G. S. Bang, G. W. Shim, G. H. Shin, D. Y. Jung, H. Park, W. G. Hong, J. Choi, J. Lee, S.-Y. Choi, ACS Omega 2018, 3, 5522−5530.

- C. Yang, H. Jin, C. Cui, J. Li, J. Wang, K. Amine, J. Lu, S. Wang, Nano Energy 54 (2018) 192–199.

- H. Zhang, K. Lv, B. Fang, M. C. Forster, R. Dervisoglu, L. B. Andreas, K. Zhang, S. Chen, Electrochim. Acta 292 (2018) 942–950.

- Q. Xue, Y. Ding, Y. Xue, F. Li, P. Chen, Y. Chen, Carbon 139 (2018) 137–144.

- Q. Lv, W. Si, Z. Yang, N. Wang, Z. Tu, Y. Yi, C. Huang, L. Jiang, M. Zhang, J. He, Y. Long, ACS Appl. Mater. Interfaces 2017, 9, 29744−29752.

- Y. Lv, L. Yang, D. Cao, ACS Appl. Mater. Interfaces 2017, 9, 32859−32867.

- J. Wang, J. Hao, D. Liu, S. Qin, D. Portehault, Y. Li, Y. Chen, W. Lei, ACS Energy Lett. 2017, 2, 306−312.

- M. Graglia, J. Pampel, T. Hantke, T.-P. Fellinger, D. Esposito, ACS Nano 2016, 10 (4), 4364

- C. Tang, H.F. Wang, X. Chen, B.Q. Li, T.Z. Hou, B. Zhang, Q. Zhang, M.M. Titirici, F. Wei, Adv. Mater. 2016, 28 (32), 6845–6851.

- H. Yu, L. Shang, T. Bian, R. Shi, G. I. N. Waterhouse, Y. Zhao, C. Zhou, L.-Z. Wu, C.-H. Tung, T. Zhang, Adv. Mater. 2016, 28, 5080–5086.

- B. Men, Y. Sun, M. Li, C. Hu, M. Zhang, L. Wang, Y. Tang, Y. Chen, P. Wan, J. Pan, ACS Appl. Mater. Interfaces 2016, 8, 1415−1423.

- G. Panomsuwan, N. Saito, T, Ishizaki, ACS Appl. Mater. Interfaces 2016, 8, 6962−6971.

- H.-W. Liang, Z.-Y. Wu, L.-F. Chen, C. Li, S.-H. Yu, Nano Energy 2015, 11, 366–376.

- J. Li, Y. Zhang, X. Zhang, J. Han, Y. Wang, L. Gu, Z. Zhang, X. Wang, J. Jian, P. Xu, B. Song, ACS Appl. Mater. Interfaces 2015, 7, 19626−19634.

- C. Guo, W. Liao, Z. Li, L. Sun, C. Chen, Nanoscale, 2015, 7, 15990–15998.

- H. Fei, R. Ye, G. Ye, Y. Gong, Z. Peng, X. Fan, E. L. G. Samuel, P. M. Ajayan, J. M. Tour, ACS Nano, 8, 10837–10843, 2014.