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Supplementary Tables

Supplementary Table S1. Raman bands identified on the 11 wall painting fragments. Blue nod.: blue nodule.
	Colour
	Fragment
	Raman bands (cm-1)
	Compound

	Yellow
	1
	155, 206, 246, 282, 300, 387, 419, 484, 553, 713*, 1086*
	Goethite [1, 2], calcite* [3, 4]

	
	2
	205, 279, 298, 395, 475, 551, 711*, 1089*
	

	
	4
	151, 203, 240, 277, 296, 393, 415, 477, 546, 712*, 1085*
	

	
	6
	209, 278, 298, 397, 478, 558, 713*, 1088* 
	

	
	8
	279, 298, 395, 463, 544 
	

	
	9
	151, 279*, 297, 394, 554, 711*, 1086*
	

	
	10
	150, 204, 241, 278*, 297, 394, 413, 477, 546, 680, 711*, 995, 1086*
	

	
	11
	154, 282, 300, 387, 419, 551, 713*, 911, 1087*
	

	Red
	1
	225, 245, 294, 411, 498, 613, 902
	Hematite [2, 5], calcite* [3, 4]

	
	2
	292, 409, 609
	

	
	3
	221, 241, 290, 406, 494, 608, 1088*
	

	
	4
	224, 243, 292, 409, 497, 610 
	

	
	6
	223, 245, 291, 410, 491, 611, 712*, 1089*
	

	
	8
	222, 242, 289, 406, 496, 607 
	

	
	9
	225, 245, 292, 410, 494, 611, 1086*
	

	
	10
	222, 243, 290, 408, 610
	

	
	11
	225, 244, 293, 410, 495, 611, 747, 910
	

	Brown
	4
	221, 288, 403, 492, 610, 668, 1330*, 1600*
	 Hematite [2, 5],
amorphous carbon* [4, 6, 7]

	
	9
	148, 218, 283, 397, 491, 597, 1322*, 1594*
	

	Pink
	1
	143, 254, 286, 344
	Cinnabar [8, 9]

	
	9
	152, 251, 283, 341
	

	
	10
	252, 285, 342
	

	Blue
	1
	133, 159, 187, 226, 274, 379, 431, 467, 565, 786, 985, 1082 
	Egyptian blue [10, 11]

	
	2
	231, 430, 470, 573, 990, 1086 
	

	
	3
	135, 162, 187, 227, 377, 430, 471, 566, 761, 787, 981, 1007, 1081 
	

	
	5
	134, 161, 187, 227, 334, 377, 402, 430, 469, 566, 761, 786, 980, 1007, 1080, 1134
	

	
	6
	430, 571, 992, 1085 
	

	
	7
	139, 165, 197, 232, 376, 430, 465, 570, 790, 989, 1015, 1086, 1104
	

	Green
	1
	179, 215, 271, 320, 461, 553, 702, 1086 
	Green earth (celadonite) [12, 13, 14, 15]

	
	2
	No Raman data
	-

	
	3
	No Raman data
	-

	
	4
	177, 217, 272, 320, 459, 551, 588, 702, 966 
	Green earth (celadonite) [12, 13, 14, 15]

	
	6
	No Raman data
	-

	
	8
	No Raman data
	-

	
	8 (blue nod.)
	376, 429, 475, 570, 989, 1011, 1085 
	Egyptian blue [10, 11]

	
	9
	270, 317, 702 
	Green earth (glauconite/celadonite) [12, 13, 14, 15]

	
	9 (blue nod.)
	135, 195, 358, 376, 429, 473, 1011, 1084 
	Egyptian blue [10, 11]

	
	10
	No Raman data
	-

	
	10 (blue nod.)
	137, 165, 195, 230, 274, 377, 404, 430, 475, 570, 764, 787, 966, 987, 1014, 1085, 1144
	Egyptian blue [10, 11]

	White
	1
	152, 204, 280, 1085
	Calcite [3, 4]

	
	2
	1085
	

	
	3
	1085
	

	
	4
	154, 206, 282, 1087
	

	
	6
	1085
	

	
	8
	1087
	

	
	9
	152, 205, 283, 705, 1085
	

	
	10
	1085
	

	
	11
	1085
	





Supplementary Table S2. μEDXRF single-spot analyses on fragment 1.
	Fragment 1
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	-Cl
	K2O
	CaO
	TiO2
	V2O5
	Cr2O3
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	As2O3
	Rb2O
	SrO
	Y2O3
	ZrO2
	BaO
	HgO
	PbO2

	Point 1
	0,00
	2,75
	3,62
	24,77
	0,20
	0,00
	0,05
	4,62
	44,34
	0,34
	0,00
	0,01
	0,13
	18,74
	0,06
	0,02
	0,01
	0,02
	0,01
	0,13
	0,00
	0,00
	0,07
	0,00
	0,07

	Point 2
	0,00
	1,38
	2,27
	7,07
	0,80
	0,47
	0,03
	0,37
	37,55
	0,11
	0,00
	0,02
	0,18
	49,18
	0,14
	0,05
	0,01
	0,01
	0,00
	0,21
	0,00
	0,00
	0,02
	0,02
	0,12

	Point 3
	0,00
	2,84
	5,02
	26,06
	0,29
	0,03
	0,04
	3,99
	36,16
	0,14
	0,00
	0,01
	0,05
	24,91
	0,08
	0,07
	0,01
	0,01
	0,00
	0,14
	0,00
	0,00
	0,08
	0,01
	0,06

	Point 4
	1,28
	2,19
	5,75
	36,09
	0,23
	0,09
	0,09
	3,72
	30,65
	0,25
	0,00
	0,01
	0,05
	12,01
	0,05
	7,17
	0,02
	0,02
	0,00
	0,12
	0,00
	0,00
	0,17
	0,00
	0,04

	Point 5
	0,00
	1,26
	2,59
	8,73
	0,55
	0,78
	0,00
	0,72
	61,47
	0,08
	0,00
	0,01
	0,03
	23,02
	0,09
	0,03
	0,01
	0,06
	0,00
	0,25
	0,00
	0,00
	0,02
	0,00
	0,30

	Point 6
	0,00
	1,46
	3,48
	11,57
	0,54
	0,76
	0,00
	0,85
	54,05
	0,11
	0,00
	0,01
	0,04
	25,93
	0,11
	0,03
	0,01
	0,08
	0,00
	0,28
	0,00
	0,00
	0,01
	0,17
	0,50

	Point 7
	0,00
	1,70
	4,75
	15,61
	0,13
	8,69
	0,00
	0,83
	28,01
	0,16
	0,00
	0,02
	0,01
	4,49
	0,03
	0,08
	0,04
	0,11
	0,00
	0,10
	0,03
	0,02
	0,03
	34,42
	0,73

	Point 8
	0,00
	1,86
	6,43
	20,41
	0,00
	13,01
	0,00
	0,96
	25,17
	0,17
	0,04
	0,01
	0,04
	6,09
	0,04
	0,02
	0,06
	0,07
	0,00
	0,15
	0,03
	0,00
	0,09
	24,37
	0,98

	Point 9
	0,00
	1,57
	3,75
	21,58
	1,03
	0,35
	0,00
	1,41
	48,46
	0,15
	0,00
	0,01
	0,02
	2,11
	0,01
	1,47
	0,02
	0,13
	0,00
	0,22
	0,02
	0,01
	0,06
	16,76
	0,88

	Point 10
	0,24
	1,31
	3,77
	23,49
	1,53
	0,14
	0,05
	1,88
	44,05
	0,18
	0,00
	0,01
	0,02
	2,17
	0,01
	1,91
	0,02
	0,15
	0,00
	0,37
	0,02
	0,01
	0,02
	16,86
	1,80

	Point 11
	0,00
	1,62
	4,72
	13,30
	0,20
	8,24
	0,00
	0,45
	37,21
	0,08
	0,01
	0,02
	0,02
	27,41
	0,11
	0,05
	0,04
	0,05
	0,02
	0,12
	0,00
	0,00
	0,02
	5,26
	1,01

	Point 12
	0,00
	1,57
	4,27
	12,28
	0,11
	9,72
	0,00
	0,69
	31,51
	0,16
	0,03
	0,02
	0,03
	6,81
	0,03
	0,04
	0,07
	0,12
	0,01
	0,12
	0,03
	0,00
	0,05
	31,64
	0,71

	Point 13
	0,00
	1,87
	4,09
	11,46
	0,00
	15,94
	0,00
	0,56
	27,62
	0,10
	0,04
	0,03
	0,03
	9,94
	0,07
	0,03
	0,08
	0,02
	0,00
	0,24
	0,03
	0,00
	0,08
	26,72
	1,07

	Point 14
	0,00
	3,23
	4,93
	21,94
	0,35
	0,22
	0,00
	4,82
	41,55
	0,19
	0,01
	0,01
	1,04
	12,93
	0,05
	0,09
	0,02
	0,18
	0,00
	0,14
	0,01
	0,00
	0,11
	7,17
	1,02

	Point 15
	0,00
	1,35
	3,09
	9,54
	0,65
	1,37
	0,00
	1,29
	64,18
	0,09
	0,00
	0,00
	0,03
	5,65
	0,04
	0,01
	0,02
	0,09
	0,00
	0,41
	0,01
	0,01
	0,03
	11,10
	1,02

	Point 16
	0,00
	1,88
	3,50
	10,67
	0,35
	1,93
	0,00
	0,43
	60,41
	0,41
	0,00
	0,01
	0,22
	14,19
	0,07
	0,05
	0,02
	0,07
	0,00
	0,51
	0,00
	0,00
	0,00
	2,73
	2,54

	Point 17
	0,00
	1,56
	3,33
	10,25
	0,27
	3,57
	0,00
	0,48
	58,47
	0,61
	0,00
	0,01
	0,04
	10,24
	0,06
	0,06
	0,04
	0,05
	0,01
	0,53
	0,02
	0,00
	0,01
	8,37
	2,04

	Point 18
	0,00
	1,31
	3,35
	9,77
	0,33
	3,66
	0,00
	0,41
	57,77
	0,19
	0,00
	0,01
	0,03
	16,17
	0,09
	0,02
	0,03
	0,12
	0,04
	0,54
	0,01
	0,00
	0,01
	4,37
	1,78

	Point 19
	0,00
	2,58
	4,42
	25,41
	0,14
	0,00
	0,01
	4,46
	44,75
	0,15
	0,00
	0,01
	0,03
	10,04
	0,04
	0,09
	0,02
	0,05
	0,00
	0,34
	0,01
	0,03
	0,05
	5,53
	1,80

	Point 20
	0,00
	1,49
	3,95
	28,65
	0,21
	0,41
	0,00
	0,96
	49,51
	0,11
	0,00
	0,02
	0,06
	5,84
	0,03
	3,41
	0,01
	0,11
	0,00
	0,41
	0,00
	0,00
	0,01
	2,77
	2,01

	Point 21
	0,00
	1,56
	4,15
	23,97
	1,16
	0,17
	0,01
	1,24
	52,87
	0,12
	0,00
	0,00
	0,03
	3,93
	0,04
	2,98
	0,02
	0,19
	0,00
	0,52
	0,01
	0,00
	0,03
	5,04
	1,98

	Point 22
	0,56
	1,57
	4,35
	26,48
	0,86
	0,23
	0,04
	1,23
	38,75
	0,12
	0,00
	0,03
	0,02
	3,61
	0,02
	6,64
	0,01
	0,14
	0,00
	0,30
	0,02
	0,02
	0,01
	13,60
	1,40

	Point 23
	0,00
	1,52
	3,29
	10,05
	0,47
	2,37
	0,00
	0,40
	70,35
	0,10
	0,00
	0,01
	0,10
	4,74
	0,02
	0,03
	0,02
	0,16
	0,01
	0,63
	0,00
	0,00
	0,03
	2,47
	3,22

	Point 24
	0,00
	1,29
	3,25
	8,56
	0,00
	10,83
	0,00
	0,40
	41,58
	0,07
	0,01
	0,02
	0,04
	19,67
	0,11
	0,07
	0,05
	0,00
	0,00
	0,40
	0,03
	0,00
	0,04
	10,89
	2,68

	Point 25
	0,00
	1,25
	4,35
	13,25
	0,24
	8,95
	0,00
	0,60
	37,68
	0,83
	0,02
	0,03
	0,04
	17,81
	0,05
	0,03
	0,07
	0,21
	0,00
	0,37
	0,02
	0,01
	0,06
	12,32
	1,81

	Point 26
	0,00
	1,44
	2,75
	8,41
	0,48
	2,22
	0,00
	0,33
	63,88
	0,10
	0,00
	0,01
	0,10
	16,29
	0,08
	0,03
	0,02
	0,07
	0,00
	0,26
	0,00
	0,00
	0,00
	2,13
	1,39

	Point 27
	0,00
	1,07
	1,94
	7,97
	0,67
	1,20
	0,00
	0,37
	80,70
	0,09
	0,00
	0,00
	0,04
	3,83
	0,02
	0,02
	0,01
	0,14
	0,00
	0,81
	0,00
	0,00
	0,02
	0,08
	1,02

	Point 28
	0,14
	1,27
	1,41
	4,57
	0,40
	0,57
	0,04
	0,30
	52,28
	0,11
	0,00
	0,02
	0,05
	38,41
	0,09
	0,04
	0,02
	0,01
	0,00
	0,19
	0,00
	0,00
	0,02
	0,01
	0,08

	Point 29
	0,00
	0,98
	2,33
	7,73
	0,81
	1,81
	0,00
	0,45
	72,09
	0,08
	0,00
	0,00
	0,01
	7,29
	0,06
	0,01
	0,02
	0,17
	0,00
	1,08
	0,00
	0,00
	0,02
	3,34
	1,71

	Point 30
	0,00
	1,35
	4,97
	13,64
	0,12
	8,14
	0,00
	0,73
	36,82
	0,16
	0,00
	0,03
	0,02
	18,98
	0,08
	0,06
	0,07
	0,13
	0,00
	0,44
	0,03
	0,00
	0,04
	12,15
	2,04

	Point 31
	0,00
	1,21
	1,56
	4,55
	0,56
	0,89
	0,00
	0,28
	72,67
	0,04
	0,00
	0,00
	0,02
	2,37
	0,02
	0,06
	0,02
	0,16
	0,00
	0,73
	0,02
	0,00
	0,02
	11,45
	3,35

	Point 32
	0,00
	1,91
	1,43
	8,86
	0,62
	0,75
	0,00
	0,38
	53,37
	0,92
	0,00
	0,01
	0,04
	30,22
	0,08
	0,11
	0,01
	0,06
	0,13
	0,18
	0,00
	0,46
	0,03
	0,00
	0,42

	Point 33
	0,00
	1,02
	1,47
	9,73
	0,55
	1,08
	0,00
	0,57
	66,08
	0,07
	0,00
	0,00
	0,11
	17,60
	0,09
	0,02
	0,01
	0,10
	0,00
	0,69
	0,00
	0,00
	0,00
	0,00
	0,82

	Point 34
	0,00
	1,10
	1,59
	5,37
	0,52
	0,85
	0,00
	0,30
	37,73
	0,12
	0,00
	0,02
	0,05
	51,76
	0,15
	0,09
	0,01
	0,03
	0,02
	0,16
	0,00
	0,00
	0,01
	0,00
	0,12

	Point 35
	0,00
	1,12
	3,00
	10,92
	0,90
	0,76
	0,00
	0,51
	60,96
	0,11
	0,00
	0,00
	0,08
	19,47
	0,07
	0,28
	0,01
	0,15
	0,00
	0,36
	0,00
	0,00
	0,02
	0,00
	1,28

	Point 36
	0,07
	1,01
	1,31
	6,63
	0,63
	1,28
	0,00
	0,50
	74,86
	0,14
	0,00
	0,00
	0,09
	12,38
	0,05
	0,02
	0,01
	0,05
	0,00
	0,65
	0,00
	0,00
	0,02
	0,00
	0,29

	Point 37
	0,04
	1,80
	1,23
	4,82
	0,60
	0,65
	0,01
	0,31
	50,25
	0,11
	0,00
	0,02
	0,11
	39,55
	0,10
	0,04
	0,05
	0,02
	0,00
	0,16
	0,00
	0,00
	0,01
	0,01
	0,12



Supplementary Table S3. μEDXRF single-spot analyses on fragment 2.
	Fragment 2
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	-Cl
	K2O
	CaO
	TiO2
	V2O5
	Cr2O3
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	Rb2O
	SrO
	BaO
	PbO2

	Point 1
	0,00
	0,87
	6,10
	15,09
	0,39
	0,13
	0,00
	0,89
	52,50
	0,40
	0,02
	0,01
	0,23
	22,95
	0,05
	0,02
	0,04
	0,00
	0,17
	0,06
	0,08

	Point 2
	0,00
	2,24
	1,79
	6,92
	0,27
	0,12
	0,01
	0,24
	49,27
	0,10
	0,00
	0,02
	0,06
	38,50
	0,08
	0,06
	0,01
	0,00
	0,20
	0,03
	0,07

	Point 3
	0,18
	0,81
	1,48
	6,28
	0,18
	0,23
	0,00
	0,17
	80,73
	0,09
	0,00
	0,00
	0,02
	8,50
	0,08
	0,24
	0,01
	0,01
	0,91
	0,03
	0,07

	Point 4
	1,13
	1,37
	2,78
	54,25
	0,24
	0,00
	0,01
	0,43
	19,63
	0,07
	0,00
	0,00
	0,02
	0,59
	0,00
	18,99
	0,05
	0,00
	0,37
	0,01
	0,04

	Point 5
	0,65
	2,05
	3,20
	57,19
	0,05
	0,11
	0,02
	0,60
	31,79
	0,15
	0,02
	0,00
	0,03
	1,11
	0,00
	2,90
	0,01
	0,00
	0,08
	0,01
	0,02

	Point 6
	0,77
	0,95
	1,12
	4,18
	0,18
	0,28
	0,00
	0,26
	89,40
	0,09
	0,00
	0,01
	0,04
	1,38
	0,01
	0,28
	0,01
	0,00
	0,98
	0,02
	0,05

	Point 7
	0,78
	2,21
	4,32
	21,75
	1,34
	0,15
	0,00
	1,93
	62,88
	0,22
	0,00
	0,01
	0,05
	3,74
	0,00
	0,34
	0,01
	0,12
	0,09
	0,02
	0,05

	Point 8
	0,20
	1,35
	2,44
	15,23
	0,62
	0,97
	0,04
	0,47
	68,40
	0,06
	0,05
	0,00
	0,07
	5,01
	0,04
	4,44
	0,02
	0,00
	0,44
	0,09
	0,05

	Point 9
	0,46
	0,70
	1,64
	24,11
	0,41
	0,71
	0,03
	0,31
	61,07
	0,03
	0,00
	0,00
	0,02
	2,03
	0,02
	7,78
	0,02
	0,00
	0,55
	0,06
	0,03

	Point 10
	1,63
	1,45
	6,31
	22,48
	0,95
	0,78
	0,10
	1,04
	56,33
	0,16
	0,00
	0,01
	0,02
	0,92
	0,01
	6,97
	0,01
	0,05
	0,78
	0,00
	0,02





Supplementary Table S4. μEDXRF single-spot analyses on fragment 3.
	Fragment 3
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	-Cl
	K2O
	CaO
	TiO2
	V2O5
	Cr2O3
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	Rb2O
	SrO
	BaO
	PbO2

	Point 1
	0,19
	1,79
	2,53
	7,45
	0,40
	0,22
	0,02
	0,27
	32,22
	0,10
	0,00
	0,02
	0,03
	54,38
	0,14
	0,04
	0,01
	0,00
	0,10
	0,02
	0,07

	Point 2
	0,00
	2,52
	2,99
	9,73
	0,52
	0,16
	0,02
	0,32
	50,12
	0,13
	0,00
	0,02
	0,04
	33,00
	0,06
	0,04
	0,01
	0,00
	0,20
	0,02
	0,07

	Point 3
	0,00
	2,01
	3,82
	30,42
	1,47
	0,12
	0,02
	3,69
	50,10
	0,27
	0,00
	0,02
	0,04
	7,50
	0,01
	0,29
	0,01
	0,01
	0,15
	0,01
	0,05

	Point 4
	0,00
	2,31
	3,94
	21,36
	0,92
	0,18
	0,00
	2,67
	61,41
	0,23
	0,00
	0,01
	0,06
	6,24
	0,01
	0,39
	0,01
	0,02
	0,13
	0,04
	0,06

	Point 5
	0,00
	4,72
	6,44
	48,85
	0,20
	0,12
	0,00
	9,79
	9,33
	0,28
	0,00
	0,02
	0,07
	19,58
	0,05
	0,09
	0,00
	0,01
	0,13
	0,27
	0,06

	Point 6
	0,00
	1,32
	2,96
	9,23
	0,39
	0,24
	0,00
	0,25
	81,42
	0,10
	0,00
	0,00
	0,05
	2,64
	0,04
	0,03
	0,01
	0,04
	1,19
	0,03
	0,08

	Point 7
	0,00
	1,97
	3,25
	9,63
	0,35
	0,27
	0,00
	0,23
	82,31
	0,09
	0,00
	0,00
	0,11
	1,24
	0,00
	0,17
	0,02
	0,00
	0,18
	0,03
	0,14

	Point 8
	3,28
	0,97
	2,71
	58,04
	0,00
	0,06
	0,16
	0,86
	17,80
	0,08
	0,02
	0,00
	0,03
	0,66
	0,00
	15,04
	0,04
	0,01
	0,15
	0,03
	0,05

	Point 9
	0,31
	2,61
	7,47
	45,18
	0,76
	0,17
	0,07
	1,57
	34,64
	0,29
	0,00
	0,01
	0,06
	1,91
	0,00
	4,68
	0,02
	0,00
	0,18
	0,01
	0,06

	Point 10
	0,18
	1,33
	2,78
	25,28
	0,50
	0,83
	0,00
	0,43
	55,37
	0,08
	0,00
	0,00
	0,06
	4,93
	0,04
	7,64
	0,01
	0,00
	0,49
	0,01
	0,04

	Point 11
	0,00
	2,35
	2,48
	10,88
	0,64
	0,80
	0,05
	0,29
	79,64
	0,08
	0,01
	0,00
	0,19
	0,74
	0,00
	1,73
	0,02
	0,03
	0,02
	0,00
	0,02






Supplementary Table S5. μEDXRF single-spot analyses on fragment 4.
	Fragment 4
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	K2O
	CaO
	TiO2
	V2O5
	Cr2O3
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	As2O3
	Rb2O
	ZrO2
	BaO
	SrO
	PbO2

	Point 1
	0,00
	1,01
	6,02
	17,84
	2,51
	0,17
	1,09
	43,11
	0,35
	0,01
	0,00
	0,27
	27,12
	0,07
	0,02
	0,08
	0,03
	0,00
	0,00
	0,04
	0,20
	0,05

	Point 2
	0,88
	1,05
	2,07
	6,79
	2,84
	0,27
	0,37
	78,36
	0,13
	0,00
	0,00
	0,10
	5,79
	0,04
	0,13
	0,02
	0,00
	0,03
	0,04
	0,03
	0,76
	0,28

	Point 3
	0,19
	0,64
	1,51
	7,84
	3,22
	0,28
	0,45
	54,41
	0,23
	0,01
	0,01
	0,12
	30,51
	0,08
	0,05
	0,04
	0,03
	0,00
	0,00
	0,03
	0,27
	0,10

	Point 4
	0,46
	1,69
	2,13
	10,97
	2,40
	0,26
	0,76
	52,00
	0,11
	0,00
	0,01
	0,07
	28,59
	0,09
	0,07
	0,02
	0,02
	0,00
	0,00
	0,04
	0,23
	0,09

	Point 5
	0,12
	1,35
	3,07
	18,11
	2,51
	0,18
	2,85
	45,74
	0,17
	0,00
	0,01
	0,07
	25,17
	0,11
	0,08
	0,01
	0,02
	0,00
	0,00
	0,04
	0,31
	0,07

	Point 6
	0,23
	2,41
	3,31
	26,22
	2,23
	0,19
	5,66
	33,70
	0,15
	0,01
	0,01
	0,14
	24,86
	0,09
	0,48
	0,02
	0,02
	0,00
	0,00
	0,04
	0,16
	0,07

	Point 7
	0,12
	1,68
	3,62
	21,19
	2,92
	0,18
	3,84
	46,05
	0,22
	0,00
	0,01
	0,08
	19,34
	0,08
	0,03
	0,02
	0,02
	0,00
	0,00
	0,31
	0,21
	0,08

	Point 8
	0,00
	1,88
	1,82
	11,07
	2,12
	0,22
	0,86
	60,96
	0,12
	0,01
	0,00
	0,20
	20,22
	0,05
	0,04
	0,04
	0,02
	0,00
	0,00
	0,05
	0,23
	0,09

	Point 9
	0,33
	1,80
	2,01
	7,26
	2,62
	0,22
	0,45
	49,84
	0,16
	0,00
	0,02
	0,07
	34,69
	0,07
	0,04
	0,04
	0,03
	0,11
	0,00
	0,02
	0,14
	0,08

	Point 10
	0,25
	1,32
	3,93
	13,57
	2,27
	0,20
	0,69
	51,55
	0,27
	0,01
	0,01
	0,34
	25,04
	0,07
	0,03
	0,06
	0,03
	0,00
	0,00
	0,02
	0,27
	0,09

	Point 11
	0,53
	0,54
	1,35
	3,94
	1,60
	0,40
	0,24
	86,97
	0,12
	0,00
	0,01
	0,06
	2,75
	0,03
	0,09
	0,02
	0,01
	0,00
	0,00
	0,01
	1,26
	0,06

	Point 12
	0,05
	1,00
	5,25
	17,21
	1,82
	0,56
	0,89
	42,38
	0,39
	0,02
	0,01
	0,44
	29,40
	0,08
	0,02
	0,05
	0,03
	0,00
	0,00
	0,05
	0,34
	0,04

	Point 13
	0,18
	0,87
	1,68
	7,51
	2,68
	0,38
	0,54
	78,70
	0,09
	0,00
	0,00
	0,09
	6,29
	0,05
	0,02
	0,03
	0,03
	0,00
	0,00
	0,03
	0,77
	0,07

	Point 14
	0,05
	0,67
	4,60
	17,17
	2,01
	0,17
	0,99
	37,45
	0,40
	0,03
	0,01
	0,54
	35,37
	0,11
	0,02
	0,06
	0,03
	0,01
	0,00
	0,05
	0,20
	0,06

	Point 15
	0,50
	2,61
	4,52
	28,19
	2,07
	0,14
	4,38
	41,08
	0,34
	0,02
	0,02
	0,09
	15,63
	0,06
	0,02
	0,02
	0,02
	0,02
	0,00
	0,05
	0,15
	0,05

	Point 16
	0,15
	2,67
	4,13
	37,77
	1,53
	0,16
	6,43
	28,07
	0,13
	0,01
	0,01
	0,06
	18,57
	0,06
	0,01
	0,01
	0,02
	0,03
	0,00
	0,02
	0,12
	0,04

	Point 17
	0,66
	0,96
	2,71
	25,15
	2,04
	0,22
	3,18
	43,59
	0,24
	0,00
	0,01
	0,10
	16,68
	0,08
	4,05
	0,02
	0,01
	0,00
	0,00
	0,04
	0,19
	0,09

	Point 18
	1,28
	1,46
	4,28
	15,60
	4,34
	0,29
	2,04
	51,86
	0,30
	0,00
	0,00
	3,10
	14,68
	0,07
	0,11
	0,03
	0,04
	0,00
	0,00
	0,16
	0,20
	0,15

	Point 19
	0,19
	0,80
	3,88
	56,61
	2,04
	0,18
	1,34
	21,59
	0,27
	0,00
	0,01
	0,03
	12,76
	0,05
	0,04
	0,01
	0,01
	0,00
	0,00
	0,01
	0,17
	0,04

	Point 20
	0,07
	2,19
	1,82
	8,14
	2,31
	0,28
	0,26
	63,08
	0,14
	0,00
	0,01
	0,10
	21,13
	0,03
	0,03
	0,01
	0,02
	0,04
	0,04
	0,05
	0,18
	0,07

	Point 21
	0,00
	1,28
	5,06
	65,65
	1,34
	0,21
	1,95
	19,20
	0,38
	0,00
	0,01
	0,06
	4,66
	0,02
	0,02
	0,02
	0,01
	0,01
	0,00
	0,03
	0,08
	0,03

	Point 22
	0,43
	0,80
	5,69
	21,52
	2,52
	0,58
	3,62
	46,93
	0,42
	0,04
	0,02
	0,10
	16,78
	0,05
	0,03
	0,03
	0,03
	0,05
	0,06
	0,10
	0,12
	0,09

	Point 23
	0,00
	0,81
	1,97
	6,43
	0,42
	0,31
	0,20
	72,68
	0,08
	0,00
	0,00
	0,06
	16,00
	0,07
	0,02
	0,02
	0,07
	0,02
	0,00
	0,03
	0,43
	0,36

	Point 24
	0,10
	1,61
	1,79
	6,45
	0,49
	0,32
	0,40
	45,78
	0,23
	0,00
	0,02
	0,10
	42,01
	0,09
	0,29
	0,03
	0,03
	0,02
	0,00
	0,03
	0,11
	0,11

	Point 25
	0,14
	1,06
	3,42
	14,02
	2,31
	0,40
	0,57
	56,32
	0,25
	0,00
	0,01
	0,10
	19,91
	0,06
	0,06
	0,03
	0,08
	0,00
	0,00
	0,03
	0,85
	0,38

	Point 26
	0,03
	0,61
	2,67
	17,55
	2,12
	0,43
	0,82
	57,43
	0,24
	0,00
	0,00
	0,09
	15,98
	0,05
	0,09
	0,03
	0,09
	0,00
	0,00
	0,03
	1,28
	0,47

	Point 27
	0,40
	0,36
	1,59
	6,28
	2,45
	0,28
	0,32
	80,25
	0,12
	0,00
	0,00
	0,10
	5,24
	0,02
	0,04
	0,02
	0,07
	0,00
	0,00
	0,01
	2,01
	0,42

	Point 28
	0,45
	0,57
	2,18
	6,93
	2,53
	0,27
	0,30
	81,04
	0,20
	0,00
	0,01
	0,08
	3,45
	0,03
	0,04
	0,01
	0,05
	0,00
	0,00
	0,03
	1,49
	0,33

	Point 29
	0,44
	0,96
	2,45
	14,85
	2,38
	0,27
	0,51
	60,84
	0,26
	0,00
	0,00
	0,09
	15,22
	0,05
	0,48
	0,02
	0,07
	0,00
	0,00
	0,02
	0,81
	0,29

	Point 30
	0,36
	0,50
	1,96
	9,31
	2,35
	0,21
	0,58
	33,18
	0,27
	0,02
	0,02
	0,08
	49,46
	0,10
	0,07
	0,09
	0,14
	0,00
	0,00
	0,06
	0,74
	0,51

	Point 31
	0,49
	0,91
	3,63
	13,15
	2,71
	0,25
	1,01
	67,84
	0,22
	0,00
	0,00
	0,08
	8,64
	0,04
	0,03
	0,01
	0,06
	0,00
	0,00
	0,01
	0,54
	0,36

	Point 32
	0,97
	0,66
	1,79
	7,91
	2,59
	0,29
	0,36
	78,90
	0,11
	0,00
	0,00
	0,06
	4,82
	0,04
	0,03
	0,01
	0,05
	0,01
	0,00
	0,03
	0,99
	0,36

	Point 33
	0,06
	0,86
	1,61
	9,53
	2,73
	0,37
	0,39
	69,59
	0,15
	0,00
	0,01
	0,12
	11,76
	0,03
	0,03
	0,02
	0,11
	0,00
	0,00
	0,03
	1,60
	0,99

	Point 34
	0,22
	1,96
	3,40
	12,69
	3,04
	0,28
	0,51
	56,86
	0,19
	0,00
	0,01
	0,40
	18,72
	0,07
	0,07
	0,03
	0,08
	0,00
	0,00
	0,03
	0,99
	0,47

	Point 35
	1,39
	1,31
	1,93
	9,92
	3,90
	0,47
	0,32
	61,32
	0,30
	0,00
	0,00
	0,14
	17,76
	0,05
	0,11
	0,02
	0,07
	0,00
	0,00
	0,03
	0,75
	0,22

	Point 36
	0,00
	1,29
	1,68
	9,33
	2,63
	0,22
	0,36
	54,15
	0,22
	0,00
	0,01
	0,25
	27,83
	0,06
	0,07
	0,03
	0,09
	0,00
	0,00
	0,01
	1,30
	0,48

	Point 37
	0,77
	0,78
	1,57
	5,42
	3,68
	0,35
	0,24
	79,00
	0,08
	0,00
	0,00
	0,05
	4,97
	0,04
	0,04
	0,02
	0,12
	0,00
	0,00
	0,03
	1,55
	1,28

	Point 38
	0,30
	1,10
	2,63
	10,56
	3,75
	0,61
	0,66
	63,77
	0,34
	0,00
	0,00
	0,20
	14,63
	0,04
	0,08
	0,02
	0,05
	0,00
	0,07
	0,02
	0,77
	0,40

	Point 39
	0,40
	1,30
	2,94
	10,89
	2,42
	0,34
	0,32
	72,96
	0,11
	0,00
	0,00
	0,06
	6,65
	0,04
	0,03
	0,01
	0,07
	0,01
	0,00
	0,02
	1,02
	0,39

	Point 40
	0,00
	1,89
	3,09
	12,46
	1,85
	0,29
	0,48
	57,70
	0,19
	0,00
	0,00
	0,12
	19,99
	0,05
	0,10
	0,03
	0,09
	0,00
	0,00
	0,04
	1,26
	0,37

	Point 41
	0,52
	1,09
	3,44
	11,91
	2,94
	0,26
	0,56
	68,93
	0,17
	0,00
	0,00
	0,03
	6,85
	0,03
	0,02
	0,01
	0,10
	0,00
	0,00
	0,02
	1,84
	1,27

	Point 42
	0,34
	1,42
	3,05
	13,94
	3,22
	0,35
	0,65
	52,99
	0,25
	0,00
	0,02
	0,38
	21,53
	0,08
	0,12
	0,03
	0,10
	0,00
	0,00
	0,05
	0,96
	0,50

	Point 43
	0,32
	0,69
	2,17
	24,48
	3,15
	0,29
	0,50
	45,82
	0,27
	0,00
	0,00
	0,11
	20,23
	0,06
	0,34
	0,04
	0,07
	0,00
	0,00
	0,02
	1,07
	0,39

	Point 44
	0,43
	3,04
	4,30
	36,69
	2,62
	0,26
	9,44
	20,69
	0,21
	0,01
	0,02
	0,13
	21,10
	0,06
	0,03
	0,01
	0,01
	0,00
	0,00
	0,08
	0,64
	0,24

	Point 45
	0,74
	0,67
	1,28
	4,61
	2,37
	0,20
	0,12
	83,32
	0,07
	0,00
	0,00
	0,03
	1,47
	0,02
	0,03
	0,01
	0,15
	0,00
	0,00
	0,02
	2,53
	2,36

	Point 46
	0,64
	0,69
	1,47
	20,40
	3,25
	0,86
	0,41
	60,70
	0,06
	0,00
	0,00
	0,05
	3,86
	0,03
	6,78
	0,02
	0,02
	0,00
	0,00
	0,04
	0,62
	0,04

	Point 47
	0,48
	0,64
	1,23
	25,13
	2,90
	0,88
	0,42
	49,85
	0,20
	0,00
	0,00
	0,03
	1,92
	0,03
	15,55
	0,03
	0,03
	0,00
	0,00
	0,00
	0,54
	0,05

	Point 48
	1,07
	1,39
	1,51
	22,44
	3,35
	0,77
	0,39
	56,81
	0,06
	0,00
	0,04
	0,02
	1,77
	0,01
	9,45
	0,02
	0,00
	0,01
	0,00
	0,00
	0,58
	0,28







Supplementary Table S6. μEDXRF single-spot analyses on fragment 5.
	Fragment 5
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	K2O
	CaO
	TiO2
	V2O5
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	As2O3
	Rb2O
	SrO
	ZrO2
	BaO
	PbO2

	Point 1
	0,00
	2,14
	7,90
	36,85
	0,83
	0,56
	1,83
	31,94
	0,21
	0,00
	0,08
	1,84
	0,01
	15,38
	0,04
	0,02
	0,00
	0,08
	0,09
	0,02
	0,19

	Point 2
	0,34
	1,36
	4,55
	52,39
	0,34
	0,35
	1,21
	20,82
	0,14
	0,00
	0,04
	0,96
	0,00
	17,20
	0,04
	0,01
	0,01
	0,07
	0,00
	0,00
	0,18

	Point 3
	1,43
	0,05
	0,72
	60,48
	0,00
	0,05
	0,13
	15,66
	0,03
	0,01
	0,01
	0,29
	0,01
	20,88
	0,04
	0,01
	0,04
	0,06
	0,01
	0,01
	0,10

	Point 4
	0,00
	1,15
	2,94
	42,26
	0,57
	0,41
	1,25
	40,53
	0,16
	0,03
	0,55
	2,15
	0,01
	7,55
	0,03
	0,06
	0,04
	0,07
	0,00
	0,06
	0,15

	Point 5
	0,68
	1,01
	2,72
	46,67
	0,11
	0,23
	0,61
	24,33
	0,04
	0,18
	0,02
	0,90
	0,00
	22,14
	0,04
	0,03
	0,02
	0,10
	0,01
	0,03
	0,13

	Point 6
	0,00
	2,66
	10,35
	38,69
	0,79
	0,64
	2,79
	33,02
	0,38
	0,01
	0,10
	3,44
	0,01
	6,90
	0,03
	0,03
	0,01
	0,06
	0,00
	0,04
	0,08








Supplementary Table S7. μEDXRF single-spot analyses on fragment 6.
	Fragment 6
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	-Cl
	K2O
	CaO
	TiO2
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	As2O3
	SrO
	BaO
	PbO2

	Point 1
	0,12
	1,17
	5,45
	19,91
	0,20
	0,15
	0,04
	1,08
	39,02
	0,31
	0,33
	31,75
	0,10
	0,04
	0,05
	0,04
	0,10
	0,04
	0,08

	Point 2
	0,02
	1,40
	1,42
	5,96
	0,03
	0,24
	0,00
	0,27
	79,75
	0,32
	0,07
	9,54
	0,06
	0,05
	0,02
	0,02
	0,69
	0,05
	0,10

	Point 3
	 0,00
	1,90
	2,79
	13,49
	0,15
	0,27
	0,02
	0,45
	69,25
	0,15
	0,07
	10,76
	0,07
	0,02
	0,02
	0,02
	0,48
	0,03
	0,06

	Point 4
	1,07
	2,03
	3,37
	46,65
	0,00
	0,17
	0,16
	1,16
	24,75
	0,12
	0,03
	8,65
	0,04
	11,51
	0,02
	0,01
	0,18
	0,02
	0,07

	Point 5
	0,00
	3,33
	3,35
	44,00
	0,00
	0,26
	0,07
	3,72
	24,03
	0,16
	0,14
	19,59
	0,07
	1,00
	0,01
	0,03
	0,11
	0,00
	0,12

	Point  6
	0,15
	2,54
	4,12
	35,44
	0,13
	0,17
	0,03
	1,03
	31,82
	0,12
	0,05
	23,16
	0,08
	0,82
	0,01
	0,03
	0,15
	0,00
	0,14

	Point 7
	0,00
	2,57
	2,85
	11,69
	0,31
	0,23
	0,05
	0,42
	53,08
	0,12
	0,14
	28,13
	0,08
	0,04
	0,02
	0,02
	0,11
	0,04
	0,10

	Point  8
	0,04
	0,74
	2,34
	24,27
	0,00
	0,23
	0,07
	0,64
	59,85
	0,29
	0,02
	1,38
	0,01
	8,54
	0,01
	0,02
	1,37
	0,02
	0,13

	Point  9
	0,00
	0,73
	2,01
	8,97
	0,00
	0,25
	0,02
	0,28
	83,97
	0,09
	0,04
	1,69
	0,03
	0,06
	0,01
	0,02
	1,65
	0,03
	0,15

	Point 10
	0,00
	3,01
	3,70
	29,12
	0,00
	0,00
	0,03
	3,75
	41,95
	0,28
	0,08
	17,73
	0,07
	0,02
	0,01
	0,01
	0,08
	0,05
	0,09

	Point 11
	0,68
	1,73
	3,29
	39,42
	0,00
	0,14
	0,13
	2,97
	32,09
	0,18
	0,07
	11,59
	0,05
	7,43
	0,02
	0,02
	0,08
	0,02
	0,08

	Point 12
	0,09
	0,95
	2,31
	14,12
	0,00
	0,23
	0,01
	0,38
	78,25
	0,11
	0,04
	2,29
	0,03
	0,01
	0,01
	0,01
	1,02
	0,02
	0,09

	Point 13
	0,00
	2,72
	4,34
	31,61
	0,02
	0,11
	0,05
	4,85
	36,47
	0,28
	0,21
	18,94
	0,07
	0,04
	0,01
	0,02
	0,12
	0,04
	0,11

	Point 14
	0,00
	1,05
	5,73
	26,32
	0,30
	0,25
	0,11
	2,87
	38,51
	0,59
	0,19
	23,67
	0,08
	0,03
	0,02
	0,02
	0,11
	0,04
	0,10

	Point 15
	0,00
	1,61
	2,91
	10,59
	0,18
	0,20
	0,03
	0,63
	51,86
	0,21
	0,25
	31,06
	0,11
	0,02
	0,05
	0,03
	0,13
	0,03
	0,10

	Point 16
	0,00
	1,62
	6,56
	21,26
	0,19
	0,06
	0,05
	1,08
	48,80
	0,42
	0,48
	19,12
	0,05
	0,03
	0,03
	0,02
	0,11
	0,04
	0,06

	Point 17
	0,00
	1,24
	2,34
	9,67
	0,04
	0,30
	0,00
	0,24
	81,48
	0,09
	0,09
	3,05
	0,02
	0,06
	0,01
	0,01
	1,21
	0,05
	0,08

	Point 18
	0,00
	1,13
	6,11
	23,54
	0,15
	0,12
	0,04
	0,84
	38,55
	0,27
	0,20
	28,65
	0,09
	0,03
	0,05
	0,03
	0,12
	0,01
	0,09





Supplementary Table S8. μEDXRF single-spot analyses on fragment 7.
	Fragment 7
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	-Cl
	K2O
	CaO
	TiO2
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	As2O3
	SrO
	BaO
	PbO2

	Point 1
	0,72
	0,34
	1,65
	52,45
	0,00
	0,48
	0,17
	0,36
	20,32
	0,04
	0,02
	0,37
	0,00
	22,77
	0,05
	0,01
	0,13
	0,02
	0,10

	Point 2
	0,00
	1,45
	5,83
	55,21
	0,18
	0,65
	0,10
	1,11
	19,59
	0,18
	0,07
	1,55
	0,01
	13,75
	0,04
	0,00
	0,06
	0,04
	0,18

	Point 3
	1,04
	0,45
	3,36
	58,82
	0,00
	0,26
	0,14
	1,27
	16,81
	0,11
	0,04
	0,95
	0,00
	16,43
	0,04
	0,03
	0,10
	0,01
	0,13

	Point 4
	0,05
	1,82
	7,20
	46,48
	0,22
	0,86
	0,19
	2,15
	31,89
	0,37
	0,10
	2,74
	0,00
	5,61
	0,03
	0,01
	0,14
	0,01
	0,13





Supplementary Table S9. μEDXRF single-spot analyses on fragment 8.
	Fragment 8
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	-Cl
	K2O
	CaO
	TiO2
	Cr2O3
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	As2O3
	SrO
	BaO
	PbO2

	Point 1
	0,00
	1,60
	2,84
	10,90
	0,07
	0,19
	0,02
	0,31
	55,70
	0,17
	0,01
	0,24
	27,36
	0,07
	0,10
	0,03
	0,08
	0,18
	0,04
	0,09

	Point 2
	0,00
	1,85
	3,40
	10,05
	0,00
	0,10
	0,00
	0,37
	63,76
	0,11
	0,01
	0,10
	19,22
	0,07
	0,05
	0,02
	0,09
	0,53
	0,02
	0,25

	Point 3
	0,00
	0,60
	1,86
	7,51
	0,00
	0,12
	0,19
	0,39
	47,38
	0,14
	0,02
	0,08
	41,25
	0,08
	0,05
	0,02
	0,02
	0,15
	0,02
	0,13

	Point 4
	0,00
	1,10
	2,56
	8,35
	0,02
	0,01
	0,01
	0,32
	54,13
	0,15
	0,01
	0,07
	32,54
	0,09
	0,11
	0,02
	0,07
	0,14
	0,02
	0,31

	Point 5
	0,00
	1,13
	3,12
	10,97
	0,05
	0,17
	0,00
	0,38
	66,32
	0,14
	0,00
	0,04
	16,43
	0,07
	0,28
	0,01
	0,04
	0,58
	0,03
	0,22

	Point 6
	0,00
	0,47
	2,04
	17,61
	0,00
	0,24
	0,03
	0,45
	61,07
	0,11
	0,01
	0,04
	10,94
	0,08
	5,82
	0,02
	0,04
	0,78
	0,01
	0,25

	Point 7
	0,01
	0,62
	1,24
	5,72
	0,00
	0,17
	0,04
	0,16
	80,64
	0,08
	0,01
	0,16
	8,70
	0,06
	0,62
	0,01
	0,07
	1,14
	0,06
	0,49

	Point 8
	0,00
	0,20
	1,78
	6,62
	0,00
	0,12
	0,04
	0,47
	77,37
	0,23
	0,00
	0,15
	10,38
	0,06
	0,70
	0,02
	0,05
	1,49
	0,03
	0,29

	Point 9
	0,14
	0,17
	1,47
	30,90
	0,00
	0,26
	0,06
	0,54
	41,18
	0,09
	0,00
	0,03
	1,66
	0,02
	22,13
	0,05
	0,02
	1,14
	0,00
	0,14

	Point 10
	0,00
	7,58
	1,66
	4,21
	0,05
	0,14
	0,35
	0,10
	31,52
	0,01
	0,01
	0,64
	52,69
	0,18
	0,17
	0,01
	0,00
	0,48
	0,04
	0,17

	Point 11
	0,00
	0,76
	3,59
	11,62
	0,09
	0,30
	0,07
	0,59
	71,65
	0,20
	0,00
	0,08
	9,78
	0,05
	0,25
	0,01
	0,03
	0,71
	0,04
	0,17

	Point 12
	0,00
	0,50
	2,06
	7,97
	0,02
	0,17
	0,04
	0,40
	74,96
	0,18
	0,00
	0,14
	11,81
	0,05
	0,30
	0,03
	0,06
	1,01
	0,03
	0,27

	Point 13
	0,00
	0,82
	3,46
	10,34
	0,00
	0,13
	0,00
	0,41
	80,15
	0,18
	0,00
	0,04
	2,86
	0,04
	0,04
	0,02
	0,04
	1,11
	0,04
	0,33

	Point 14
	0,00
	1,27
	2,06
	6,70
	0,04
	0,07
	0,04
	0,29
	47,74
	0,11
	0,02
	0,14
	40,74
	0,12
	0,08
	0,02
	0,03
	0,17
	0,03
	0,35

	Point 15
	0,00
	1,67
	6,98
	21,56
	0,29
	0,11
	0,02
	1,00
	51,91
	0,24
	0,00
	0,09
	15,42
	0,08
	0,10
	0,02
	0,03
	0,31
	0,02
	0,16

	Point 16
	0,00
	2,21
	3,38
	24,91
	0,00
	0,02
	0,06
	4,07
	39,19
	0,24
	0,01
	0,07
	23,59
	0,11
	1,78
	0,01
	0,03
	0,13
	0,06
	0,14

	Point 17
	0,30
	0,65
	1,64
	44,88
	0,00
	0,00
	0,24
	0,93
	23,85
	0,05
	0,01
	0,04
	14,33
	0,06
	12,81
	0,03
	0,00
	0,06
	0,04
	0,09

	Point 18
	0,00
	1,12
	2,51
	8,27
	0,03
	0,21
	0,00
	0,37
	82,00
	0,11
	0,01
	0,06
	4,19
	0,05
	0,02
	0,02
	0,02
	0,88
	0,06
	0,08

	Point 19
	0,00
	0,80
	5,23
	25,05
	0,32
	0,03
	0,02
	0,97
	40,25
	0,35
	0,03
	0,33
	26,20
	0,07
	0,03
	0,05
	0,02
	0,12
	0,03
	0,11

	Point 20
	0,39
	0,76
	1,78
	41,82
	0,00
	0,02
	0,17
	1,20
	26,53
	0,06
	0,01
	0,04
	15,84
	0,06
	11,11
	0,03
	0,01
	0,06
	0,03
	0,09

	Point 21
	0,00
	1,12
	1,11
	4,45
	0,07
	0,09
	0,14
	0,26
	53,51
	0,12
	0,02
	0,06
	38,46
	0,09
	0,10
	0,02
	0,03
	0,18
	0,03
	0,14










Supplementary Table S10. μEDXRF single-spot analyses on fragment 9.
	Fragment 9
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	K2O
	CaO
	TiO2
	Cr2O3
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	BaO
	Rb2O
	SrO
	As2O3
	HgO
	PbO2

	Point 1
	0,00
	1,50
	3,19
	9,71
	0,39
	0,30
	0,29
	68,44
	0,08
	0,00
	0,05
	14,58
	0,09
	0,03
	0,01
	0,03
	0,00
	0,66
	0,01
	0,07
	0,56

	Point 2
	0,00
	1,88
	4,04
	11,98
	0,30
	0,26
	0,42
	63,68
	0,12
	0,00
	0,08
	16,07
	0,07
	0,02
	0,01
	0,02
	0,01
	0,35
	0,03
	0,61
	0,05

	Point 3
	0,00
	2,14
	5,31
	30,23
	0,90
	1,71
	1,38
	52,42
	0,27
	0,01
	0,05
	4,82
	0,02
	0,04
	0,04
	0,04
	0,00
	0,36
	0,01
	0,07
	0,17

	Point 4
	0,00
	1,52
	3,07
	9,81
	0,25
	0,37
	0,27
	71,48
	0,08
	0,01
	0,04
	10,88
	0,06
	0,03
	0,01
	0,04
	0,00
	0,71
	0,00
	1,03
	0,34

	Point 5(33)
	0,05
	2,32
	3,02
	9,74
	0,61
	0,00
	0,28
	47,77
	0,11
	0,02
	0,01
	35,16
	0,08
	0,03
	0,10
	0,06
	0,07
	0,05
	0,01
	0,38
	0,12

	Point 6
	0,00
	1,77
	2,54
	9,90
	0,26
	0,19
	0,40
	76,75
	0,08
	0,00
	0,09
	6,81
	0,06
	0,03
	0,01
	0,04
	0,00
	0,69
	0,03
	0,19
	0,19

	Point 7
	1,00
	1,05
	3,69
	47,99
	0,20
	0,05
	0,52
	23,57
	0,19
	0,03
	0,02
	1,57
	0,01
	19,36
	0,03
	0,00
	0,00
	0,62
	0,01
	0,00
	0,07

	Point 8
	0,05
	2,52
	3,94
	13,37
	0,49
	0,12
	0,49
	66,85
	0,16
	0,01
	0,27
	10,57
	0,05
	0,15
	0,01
	0,06
	0,00
	0,77
	0,02
	0,00
	0,10

	Point 9
	0,00
	1,67
	3,13
	9,25
	0,49
	0,12
	0,35
	67,37
	0,09
	0,00
	0,43
	16,03
	0,07
	0,11
	0,02
	0,04
	0,00
	0,62
	0,03
	0,01
	0,18

	Point 10
	0,00
	1,23
	1,99
	7,10
	0,34
	0,27
	0,25
	79,97
	0,09
	0,00
	0,08
	6,97
	0,06
	0,34
	0,02
	0,05
	0,01
	1,02
	0,03
	0,06
	0,10

	Point 11
	0,00
	2,15
	5,76
	22,71
	0,54
	0,17
	0,67
	54,83
	0,17
	0,01
	0,13
	12,26
	0,07
	0,03
	0,01
	0,04
	0,00
	0,34
	0,02
	0,04
	0,05

	Point 12
	0,00
	2,20
	3,51
	10,78
	0,39
	0,11
	0,33
	69,04
	0,11
	0,00
	0,25
	10,00
	0,04
	0,09
	0,01
	0,05
	0,00
	0,87
	0,04
	1,96
	0,21

	Point 13
	0,00
	1,47
	2,15
	7,29
	0,36
	0,19
	0,22
	77,93
	0,08
	0,00
	0,08
	3,88
	0,03
	0,02
	0,01
	0,04
	0,00
	1,15
	0,04
	4,89
	0,18

	Point 14
	0,00
	2,64
	3,97
	14,62
	0,61
	0,00
	0,47
	64,28
	0,13
	0,01
	0,04
	12,29
	0,02
	0,60
	0,01
	0,06
	0,04
	0,08
	0,00
	0,00
	0,13

	Point 15
	0,00
	1,56
	2,33
	7,82
	0,36
	0,24
	0,24
	78,01
	0,08
	0,00
	0,08
	5,00
	0,03
	0,03
	0,01
	0,05
	0,00
	1,56
	0,05
	2,41
	0,15

	Point 16
	0,00
	1,51
	2,14
	6,70
	0,24
	0,50
	0,25
	73,24
	0,10
	0,00
	0,05
	5,87
	0,03
	0,13
	0,02
	0,04
	0,00
	0,96
	0,05
	8,04
	0,12

	Point 17
	0,00
	1,88
	3,15
	10,51
	0,29
	0,41
	0,34
	71,39
	0,10
	0,00
	0,04
	8,45
	0,05
	0,07
	0,02
	0,03
	0,01
	0,64
	0,03
	2,47
	0,12

	Point 18
	0,00
	1,95
	2,66
	14,90
	0,37
	0,00
	0,38
	54,70
	0,10
	0,00
	0,28
	23,79
	0,09
	0,31
	0,01
	0,04
	0,01
	0,25
	0,03
	0,01
	0,10

	Point 19
	0,00
	1,53
	2,75
	10,20
	0,42
	0,08
	0,32
	64,39
	0,07
	0,00
	0,18
	19,14
	0,10
	0,17
	0,01
	0,02
	0,00
	0,44
	0,02
	0,00
	0,14

	Point 20
	0,00
	2,44
	8,01
	24,49
	0,42
	0,09
	1,27
	59,24
	0,25
	0,00
	0,10
	2,69
	0,01
	0,15
	0,01
	0,03
	0,00
	0,72
	0,01
	0,00
	0,07

	Point 21
	0,18
	1,91
	5,64
	31,88
	0,40
	0,19
	0,74
	47,38
	0,16
	0,00
	0,05
	2,05
	0,01
	8,49
	0,02
	0,00
	0,00
	0,81
	0,02
	0,00
	0,06

	Point 22
	0,26
	3,04
	4,34
	16,01
	0,37
	0,10
	0,47
	54,81
	0,09
	0,01
	0,26
	19,39
	0,09
	0,10
	0,01
	0,06
	0,00
	0,38
	0,03
	0,00
	0,18

	Point 23
	0,16
	1,74
	3,12
	10,31
	0,33
	0,21
	0,45
	70,02
	0,10
	0,00
	0,10
	12,78
	0,07
	0,02
	0,01
	0,02
	0,05
	0,39
	0,03
	0,02
	0,08

	Point 24
	0,00
	1,42
	2,28
	11,61
	0,28
	0,19
	0,25
	71,04
	0,06
	0,01
	0,09
	11,39
	0,06
	0,03
	0,01
	0,04
	0,00
	0,56
	0,03
	0,47
	0,17

	Point 25
	0,07
	1,24
	2,14
	7,73
	0,36
	0,14
	0,25
	65,20
	0,08
	0,00
	0,15
	21,80
	0,10
	0,07
	0,11
	0,04
	0,00
	0,39
	0,04
	0,00
	0,11

	Point 26
	0,00
	1,85
	2,34
	7,67
	0,29
	0,20
	0,32
	77,52
	0,06
	0,00
	0,09
	5,24
	0,03
	0,07
	0,01
	0,05
	0,00
	1,12
	0,03
	2,90
	0,20

	Point 27
	0,00
	2,19
	2,45
	9,03
	0,43
	0,00
	0,29
	45,19
	0,12
	0,02
	0,10
	39,75
	0,11
	0,06
	0,01
	0,03
	0,01
	0,13
	0,01
	0,02
	0,07

	Point 28
	0,75
	1,69
	6,34
	20,51
	2,02
	0,00
	1,02
	47,54
	0,33
	0,01
	0,21
	19,26
	0,05
	0,03
	0,02
	0,05
	0,02
	0,11
	0,02
	0,01
	0,01

	Point 29
	5,22
	1,64
	5,73
	16,80
	7,35
	0,00
	0,78
	47,35
	0,28
	0,01
	0,15
	14,37
	0,04
	0,04
	0,02
	0,02
	0,00
	0,07
	0,03
	0,00
	0,10

	Point 30
	0,00
	1,52
	7,68
	19,51
	0,52
	0,00
	0,93
	44,93
	0,34
	0,01
	0,09
	24,18
	0,07
	0,01
	0,04
	0,01
	0,00
	0,09
	0,00
	0,00
	0,07

	Point 31
	0,00
	1,62
	7,21
	18,60
	0,46
	0,00
	0,84
	37,81
	0,33
	0,00
	2,38
	29,73
	0,35
	0,02
	0,05
	0,32
	0,01
	0,17
	0,04
	0,00
	0,06

	Point 32
	0,00
	1,74
	7,21
	20,09
	0,51
	0,00
	0,99
	39,87
	0,39
	0,01
	0,24
	28,57
	0,09
	0,02
	0,04
	0,01
	0,00
	0,13
	0,03
	0,00
	0,06

	Point 34
	0,00
	1,56
	2,28
	7,35
	0,13
	0,00
	0,18
	20,42
	0,06
	0,03
	0,07
	67,37
	0,18
	0,06
	0,01
	0,03
	0,01
	0,12
	0,04
	0,02
	0,07

	Point 35
	6,01
	1,39
	1,56
	5,31
	11,07
	0,00
	0,31
	46,05
	0,09
	0,01
	0,04
	27,78
	0,08
	0,03
	0,02
	0,03
	0,03
	0,10
	0,03
	0,00
	0,06

	Point 36
	6,61
	1,63
	1,88
	7,21
	10,35
	0,00
	0,24
	46,36
	0,10
	0,01
	0,04
	25,22
	0,06
	0,11
	0,01
	0,03
	0,00
	0,08
	0,00
	0,00
	0,07

	Point 37
	0,00
	1,81
	2,18
	7,54
	0,31
	0,00
	0,23
	53,61
	0,13
	0,02
	0,05
	33,73
	0,08
	0,03
	0,01
	0,04
	0,00
	0,15
	0,01
	0,00
	0,06

	Point 38
	3,11
	1,03
	0,90
	3,58
	4,01
	0,25
	0,15
	83,38
	0,10
	0,00
	0,04
	2,04
	0,03
	0,02
	0,01
	0,06
	0,00
	1,21
	0,02
	0,00
	0,06

	Point 39
	2,70
	1,48
	4,01
	14,65
	5,12
	0,06
	1,04
	63,55
	0,14
	0,00
	0,03
	6,00
	0,04
	0,31
	0,01
	0,04
	0,00
	0,71
	0,02
	0,01
	0,09

	Point 40
	0,00
	1,81
	2,50
	9,71
	0,35
	0,13
	0,24
	80,13
	0,08
	0,00
	0,04
	3,91
	0,04
	0,01
	0,01
	0,03
	0,00
	0,94
	0,01
	0,00
	0,05

	Point 41
	0,11
	1,56
	3,20
	10,20
	0,28
	0,28
	0,41
	74,49
	0,14
	0,00
	0,05
	8,28
	0,05
	0,01
	0,01
	0,05
	0,02
	0,76
	0,02
	0,00
	0,07

	Point 42
	6,61
	1,90
	6,47
	27,89
	8,66
	0,00
	2,87
	32,26
	0,15
	0,00
	0,08
	12,62
	0,05
	0,19
	0,01
	0,05
	0,00
	0,09
	0,01
	0,03
	0,04

	Point 43
	3,46
	1,88
	3,48
	18,37
	5,12
	0,00
	2,20
	43,46
	0,11
	0,01
	0,06
	20,78
	0,08
	0,27
	0,02
	0,04
	0,00
	0,14
	0,08
	0,01
	0,45

	Point 44
	2,82
	2,32
	3,88
	26,58
	5,28
	0,00
	2,02
	30,78
	0,09
	0,01
	0,08
	20,57
	0,09
	5,23
	0,01
	0,03
	0,00
	0,13
	0,02
	0,01
	0,05

	Point 45
	3,72
	1,35
	3,61
	47,07
	6,99
	0,00
	2,76
	23,93
	0,16
	0,00
	0,04
	9,79
	0,05
	0,28
	0,03
	0,05
	0,00
	0,07
	0,02
	0,00
	0,05

	Point 46
	1,83
	2,03
	7,56
	36,14
	3,75
	0,20
	2,35
	33,58
	0,29
	0,01
	0,08
	11,87
	0,04
	0,06
	0,01
	0,03
	0,00
	0,12
	0,01
	0,00
	0,04

	Point 47
	2,95
	2,55
	4,07
	25,16
	5,01
	0,00
	3,23
	41,50
	0,11
	0,01
	0,09
	14,61
	0,05
	0,36
	0,01
	0,07
	0,00
	0,12
	0,02
	0,00
	0,06

	Point 48
	2,40
	2,21
	3,79
	36,82
	3,84
	0,00
	2,10
	31,05
	0,09
	0,01
	0,03
	8,12
	0,04
	9,29
	0,02
	0,03
	0,00
	0,12
	0,02
	0,00
	0,03

	Point 49
	3,02
	1,68
	2,53
	40,01
	4,14
	0,00
	2,11
	27,56
	0,09
	0,01
	0,03
	6,53
	0,04
	12,00
	0,03
	0,03
	0,00
	0,15
	0,02
	0,00
	0,04

	Point 50
	1,01
	2,60
	3,10
	31,10
	2,90
	0,00
	3,17
	35,16
	0,20
	0,00
	0,04
	18,68
	0,09
	1,65
	0,01
	0,04
	0,00
	0,17
	0,02
	0,00
	0,06

	Point 51
	1,13
	2,23
	2,71
	24,98
	2,98
	0,00
	2,45
	26,80
	0,08
	0,01
	0,02
	31,69
	0,09
	4,43
	0,04
	0,03
	0,00
	0,19
	0,05
	0,01
	0,07

	Point 52
	1,64
	2,08
	2,54
	34,65
	2,47
	0,00
	2,66
	34,23
	0,17
	0,03
	0,04
	13,40
	0,07
	5,70
	0,02
	0,02
	0,00
	0,21
	0,02
	0,00
	0,06



Supplementary Table S11. μEDXRF single-spot analyses on fragment 10.
	Fragment 10
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	-Cl
	K2O
	CaO
	TiO2
	V2O5
	Cr2O3
	MnO
	Fe2O3
	CoO
	CuO
	ZnO
	As2O3
	Rb2O
	Y2O3
	BaO
	HgO
	SrO
	PbO2

	Point 1
	0,32
	1,03
	2,35
	34,69
	0,20
	0,35
	0,04
	2,32
	27,52
	0,09
	0,02
	0,00
	0,04
	19,80
	0,13
	10,78
	0,02
	0,02
	0,00
	0,00
	0,04
	0,00
	0,15
	0,07

	Point 2
	0,00
	2,17
	3,21
	21,28
	0,32
	0,51
	0,01
	3,48
	41,81
	0,12
	0,00
	0,01
	0,03
	26,39
	0,12
	0,09
	0,01
	0,02
	0,01
	0,00
	0,12
	0,00
	0,20
	0,09

	Point 3
	1,36
	1,00
	3,19
	42,59
	0,21
	0,25
	0,05
	2,28
	28,41
	0,13
	0,00
	0,02
	0,03
	9,57
	0,05
	10,50
	0,03
	0,02
	0,01
	0,00
	0,03
	0,01
	0,19
	0,06

	Point 4
	0,00
	2,50
	4,79
	25,92
	0,45
	0,45
	0,03
	3,98
	40,53
	0,15
	0,00
	0,01
	0,06
	18,90
	0,08
	1,82
	0,01
	0,02
	0,00
	0,00
	0,07
	0,00
	0,14
	0,09

	Point 5
	0,00
	1,65
	6,75
	26,63
	0,97
	0,41
	0,04
	2,28
	48,98
	0,34
	0,13
	0,01
	0,06
	10,70
	0,07
	0,54
	0,02
	0,02
	0,00
	0,00
	0,08
	0,01
	0,23
	0,10

	Point 6
	0,50
	0,79
	3,33
	51,34
	0,22
	0,29
	0,06
	0,90
	19,24
	0,09
	0,00
	0,02
	0,02
	1,55
	0,01
	21,32
	0,04
	0,01
	0,12
	0,00
	0,01
	0,01
	0,08
	0,05

	Point 7
	0,00
	1,76
	4,10
	33,74
	0,40
	0,38
	0,03
	3,15
	35,46
	0,09
	0,25
	0,00
	0,07
	18,22
	0,09
	1,79
	0,01
	0,02
	0,05
	0,00
	0,19
	0,01
	0,12
	0,08

	Point 8
	0,07
	0,54
	1,34
	6,41
	0,37
	0,63
	0,02
	0,46
	85,14
	0,08
	0,00
	0,01
	0,06
	3,66
	0,05
	0,01
	0,03
	0,03
	0,00
	0,00
	0,07
	0,00
	0,93
	0,08

	Point 9
	0,00
	0,59
	4,29
	15,24
	0,57
	0,56
	0,03
	1,03
	56,03
	0,54
	0,03
	0,01
	0,22
	20,35
	0,04
	0,03
	0,04
	0,06
	0,03
	0,00
	0,05
	0,00
	0,17
	0,10

	Point 10
	0,00
	0,94
	3,46
	11,92
	0,18
	7,27
	0,00
	0,71
	51,95
	0,20
	0,05
	0,02
	0,04
	5,12
	0,05
	0,05
	0,07
	0,06
	0,00
	0,03
	0,09
	13,49
	0,92
	3,39

	Point 11
	0,00
	1,42
	5,19
	22,80
	0,67
	0,52
	0,03
	1,46
	51,84
	0,30
	0,00
	0,01
	0,09
	14,13
	0,06
	0,40
	0,02
	0,06
	0,00
	0,00
	0,06
	0,32
	0,38
	0,25

	Point 12
	0,00
	0,97
	3,41
	13,54
	0,46
	0,50
	0,01
	1,00
	63,14
	0,13
	0,00
	0,01
	0,07
	15,58
	0,08
	0,32
	0,02
	0,05
	0,00
	0,00
	0,03
	0,02
	0,41
	0,26

	Point 13
	0,15
	1,01
	1,84
	6,84
	0,56
	0,56
	0,05
	0,40
	40,44
	0,13
	0,00
	0,02
	0,10
	47,31
	0,12
	0,06
	0,02
	0,03
	0,00
	0,00
	0,03
	0,02
	0,15
	0,17

	Point 14
	0,00
	0,86
	1,33
	6,07
	0,47
	0,66
	0,05
	0,36
	40,15
	0,12
	0,00
	0,02
	0,05
	49,32
	0,13
	0,12
	0,01
	0,02
	0,00
	0,00
	0,02
	0,00
	0,12
	0,12

	Point 15
	0,00
	0,81
	1,45
	5,97
	0,54
	0,87
	0,06
	0,44
	48,03
	0,14
	0,00
	0,02
	0,09
	41,03
	0,11
	0,08
	0,03
	0,03
	0,03
	0,00
	0,03
	0,02
	0,11
	0,10

	Point 16
	0,00
	0,70
	4,39
	13,40
	0,52
	0,37
	0,02
	0,91
	57,41
	0,31
	0,01
	0,01
	0,22
	21,28
	0,06
	0,02
	0,04
	0,03
	0,00
	0,00
	0,05
	0,00
	0,18
	0,08

	Point 17
	0,00
	0,54
	3,75
	14,76
	0,56
	0,51
	0,04
	1,17
	51,66
	0,44
	0,00
	0,01
	0,16
	25,94
	0,05
	0,01
	0,04
	0,07
	0,02
	0,00
	0,00
	0,02
	0,14
	0,10

	Point 18
	0,00
	0,84
	1,60
	5,08
	0,42
	0,60
	0,01
	0,39
	85,15
	0,11
	0,00
	0,01
	0,05
	4,64
	0,04
	0,02
	0,02
	0,03
	0,01
	0,00
	0,04
	0,00
	0,86
	0,11

	Point 19
	0,00
	0,79
	1,61
	10,83
	0,35
	0,58
	0,02
	0,36
	80,53
	0,11
	0,00
	0,00
	0,06
	3,68
	0,04
	0,04
	0,02
	0,03
	0,00
	0,00
	0,01
	0,00
	0,86
	0,09

	Point 20
	0,00
	1,00
	2,55
	10,54
	0,45
	0,56
	0,04
	0,54
	71,65
	0,13
	0,00
	0,00
	0,08
	11,30
	0,08
	0,18
	0,01
	0,03
	0,00
	0,00
	0,01
	0,00
	0,64
	0,20

	Point 21
	0,00
	0,69
	3,27
	21,91
	0,47
	0,71
	0,04
	0,89
	60,12
	0,36
	0,00
	0,00
	0,10
	10,28
	0,06
	0,38
	0,00
	0,03
	0,00
	0,00
	0,02
	0,04
	0,52
	0,09

	Point 22
	0,00
	0,85
	2,80
	8,37
	0,27
	10,07
	0,00
	0,54
	48,92
	0,14
	0,03
	0,03
	0,34
	3,13
	0,04
	0,06
	0,06
	0,04
	0,00
	0,04
	0,07
	18,53
	1,08
	4,60

	Point 23
	0,00
	1,16
	1,77
	6,03
	0,15
	7,15
	0,00
	0,38
	62,37
	0,08
	0,00
	0,02
	0,05
	4,78
	0,05
	0,04
	0,05
	0,00
	0,00
	0,03
	0,05
	10,88
	1,14
	3,81

	Point 24
	0,00
	1,14
	4,71
	28,86
	0,60
	0,55
	0,03
	1,00
	44,44
	0,19
	0,00
	0,01
	0,13
	16,97
	0,07
	0,34
	0,02
	0,09
	0,00
	0,00
	0,02
	0,04
	0,40
	0,40

	Point 25
	0,00
	1,08
	3,75
	12,65
	0,52
	0,63
	0,01
	0,65
	59,70
	0,11
	0,00
	0,00
	0,03
	18,90
	0,10
	0,41
	0,02
	0,10
	0,00
	0,00
	0,01
	0,14
	0,46
	0,72

	Point 26
	0,00
	0,98
	2,56
	9,04
	0,46
	0,62
	0,02
	0,55
	72,32
	0,11
	0,00
	0,00
	0,04
	11,66
	0,07
	0,14
	0,01
	0,07
	0,00
	0,00
	0,03
	0,05
	0,89
	0,37



Supplementary Table S12. μEDXRF single-spot analyses on fragment 11.
	Fragment 11
	Na2O
	MgO
	Al2O3
	SiO2
	P2O5
	SO3
	Cl-
	K2O
	CaO
	TiO2
	MnO
	Fe2O3
	CuO
	ZnO
	HgO
	CoO
	Rb2O
	V2O5
	PbO2
	As2O3
	SrO

	Point 1
	0,00
	1,77
	3,75
	11,67
	0,54
	0,42
	0,00
	0,50
	66,52
	0,13
	0,12
	13,30
	0,68
	0,01
	0,03
	0,06
	0,00
	0,00
	0,07
	0,01
	0,42

	Point 2
	0,12
	1,10
	2,55
	15,47
	0,40
	0,38
	0,02
	0,50
	46,69
	0,11
	0,06
	27,28
	4,77
	0,01
	0,00
	0,13
	0,00
	0,04
	0,02
	0,02
	0,31

	Point 3
	0,00
	2,42
	3,22
	10,90
	0,46
	0,55
	0,05
	0,36
	43,63
	0,13
	0,07
	37,88
	0,04
	0,01
	0,00
	0,08
	0,00
	0,01
	0,05
	0,01
	0,12

	Point 4
	0,00
	2,24
	3,95
	11,61
	0,53
	0,60
	0,04
	0,41
	40,09
	0,15
	0,04
	39,77
	0,28
	0,01
	0,01
	0,09
	0,00
	0,01
	0,06
	0,02
	0,12

	Point 5
	0,00
	2,06
	6,74
	18,89
	0,49
	0,44
	0,02
	0,75
	37,03
	0,20
	0,08
	32,79
	0,18
	0,01
	0,00
	0,10
	0,00
	0,00
	0,07
	0,02
	0,13

	Point 6
	0,00
	1,86
	4,11
	12,62
	0,53
	0,54
	0,00
	0,46
	61,13
	0,19
	0,11
	17,11
	0,15
	0,01
	0,00
	0,06
	0,00
	0,01
	0,45
	0,09
	0,58

	Point 7
	0,00
	1,86
	4,09
	11,32
	0,48
	0,44
	0,00
	0,42
	55,00
	0,13
	0,18
	24,56
	0,10
	0,02
	0,01
	0,10
	0,01
	0,01
	0,67
	0,11
	0,49

	Point 8
	0,00
	1,87
	2,81
	8,61
	0,48
	0,47
	0,05
	0,36
	34,45
	0,12
	0,04
	50,18
	0,11
	0,01
	0,00
	0,13
	0,00
	0,01
	0,10
	0,02
	0,20

	Point 9
	0,00
	2,00
	5,34
	16,34
	0,62
	0,48
	0,00
	0,83
	49,34
	0,14
	0,11
	24,23
	0,08
	0,01
	0,00
	0,07
	0,08
	0,01
	0,15
	0,04
	0,14

	Point 10
	0,00
	1,50
	2,88
	8,49
	0,50
	0,60
	0,00
	0,34
	64,07
	0,15
	0,10
	20,10
	0,03
	0,01
	0,00
	0,09
	0,00
	0,00
	0,52
	0,08
	0,52

	Point 11
	0,00
	4,01
	5,60
	34,47
	0,25
	0,40
	0,01
	4,80
	33,54
	0,17
	0,06
	15,64
	0,05
	0,01
	0,00
	0,06
	0,02
	0,00
	0,49
	0,08
	0,34

	Point 12
	0,00
	1,59
	3,52
	10,86
	0,55
	0,55
	0,00
	0,40
	67,25
	0,12
	0,05
	13,61
	0,04
	0,01
	0,00
	0,07
	0,00
	0,01
	0,58
	0,08
	0,73

	Point 13
	0,00
	1,80
	3,68
	11,96
	0,48
	0,55
	0,00
	1,01
	65,03
	0,15
	0,11
	13,14
	0,03
	0,02
	0,05
	0,06
	0,00
	0,00
	1,10
	0,13
	0,69

	Point 14
	0,00
	1,96
	3,92
	13,25
	0,54
	0,38
	0,00
	0,54
	62,29
	0,18
	0,07
	15,07
	0,03
	0,01
	0,00
	0,07
	0,00
	0,00
	1,00
	0,09
	0,59

	Point 15
	0,00
	2,38
	6,27
	18,62
	0,56
	0,44
	0,00
	0,79
	56,93
	0,23
	0,05
	12,88
	0,05
	0,01
	0,00
	0,05
	0,01
	0,00
	0,38
	0,06
	0,29

	Point 16
	0,00
	1,71
	3,34
	9,77
	0,50
	0,41
	0,00
	0,32
	65,13
	0,39
	0,08
	16,82
	0,04
	0,02
	0,00
	0,08
	0,00
	0,00
	0,72
	0,10
	0,57

	Point 17
	0,00
	1,91
	9,28
	24,84
	0,61
	0,35
	0,01
	1,57
	34,64
	0,53
	0,61
	25,23
	0,02
	0,04
	0,00
	0,06
	0,01
	0,04
	0,11
	0,03
	0,12

	Point 18
	0,00
	2,08
	3,89
	11,03
	0,64
	0,45
	0,02
	0,76
	50,72
	0,23
	0,18
	29,49
	0,03
	0,04
	0,00
	0,09
	0,00
	0,02
	0,13
	0,05
	0,14

	Point 19
	0,00
	1,72
	3,89
	10,25
	0,51
	0,32
	0,00
	0,33
	53,97
	0,11
	0,01
	27,65
	0,04
	0,03
	0,00
	0,10
	0,00
	0,00
	0,78
	0,13
	0,17

	Point 20
	0,00
	1,85
	4,74
	12,44
	0,49
	0,35
	0,00
	0,36
	50,92
	0,08
	0,03
	27,76
	0,03
	0,03
	0,01
	0,10
	0,00
	0,00
	0,59
	0,12
	0,09

	Point 21
	0,00
	2,21
	5,42
	15,86
	0,58
	0,39
	0,01
	0,61
	60,87
	0,13
	0,04
	13,24
	0,03
	0,01
	0,00
	0,07
	0,00
	0,01
	0,07
	0,02
	0,44

	Point 22
	0,00
	1,62
	5,23
	14,19
	0,45
	0,48
	0,02
	1,31
	62,49
	0,15
	0,04
	13,22
	0,05
	0,01
	0,03
	0,07
	0,00
	0,01
	0,12
	0,03
	0,47

	Point 23
	0,00
	1,77
	4,38
	14,17
	0,68
	0,54
	0,00
	0,53
	56,23
	0,16
	0,10
	20,65
	0,05
	0,01
	0,00
	0,09
	0,00
	0,01
	0,24
	0,05
	0,34

	Point 24
	0,00
	2,48
	3,52
	10,08
	0,67
	0,71
	0,01
	0,44
	59,58
	0,11
	0,46
	21,17
	0,06
	0,01
	0,00
	0,07
	0,03
	0,00
	0,29
	0,06
	0,25

	Point 25
	0,00
	2,24
	4,29
	13,64
	0,57
	0,48
	0,00
	0,50
	59,07
	0,12
	0,15
	17,44
	0,05
	0,01
	0,01
	0,08
	0,00
	0,00
	0,68
	0,11
	0,55

	Point 26
	0,00
	1,77
	5,23
	16,37
	0,51
	0,46
	0,00
	0,67
	50,00
	0,14
	0,12
	23,51
	0,09
	0,01
	0,00
	0,09
	0,00
	0,00
	0,46
	0,06
	0,49

	Point 27
	0,00
	1,73
	3,97
	15,69
	0,52
	0,44
	0,00
	0,89
	61,49
	0,25
	0,08
	13,29
	0,06
	0,01
	0,04
	0,05
	0,00
	0,01
	0,76
	0,11
	0,61

	Point 28
	0,07
	1,89
	4,55
	14,26
	0,56
	0,57
	0,00
	0,78
	65,66
	0,18
	0,05
	10,01
	0,04
	0,01
	0,00
	0,05
	0,01
	0,00
	0,67
	0,09
	0,56

	Point 29
	0,00
	2,21
	3,37
	10,92
	0,57
	0,50
	0,01
	0,39
	57,99
	0,13
	0,06
	23,11
	0,04
	0,01
	0,00
	0,04
	0,00
	0,02
	0,48
	0,05
	0,12

	Point 30
	0,00
	3,23
	4,38
	13,10
	0,64
	0,53
	0,02
	0,50
	57,56
	0,15
	0,16
	17,46
	0,83
	0,01
	0,00
	0,06
	0,00
	0,01
	0,64
	0,10
	0,58

	Point 31
	0,00
	3,40
	4,37
	13,75
	0,53
	0,45
	0,03
	0,50
	44,31
	0,11
	0,43
	29,77
	0,05
	0,02
	0,06
	0,08
	0,00
	0,00
	1,24
	0,11
	0,81

	Point 32
	0,00
	2,06
	5,36
	15,89
	0,52
	0,38
	0,00
	0,56
	50,54
	0,28
	0,16
	23,15
	0,15
	0,01
	0,00
	0,10
	0,00
	0,00
	0,41
	0,07
	0,37

	Point 33
	0,00
	1,98
	4,00
	12,44
	0,69
	0,48
	0,00
	0,41
	62,22
	0,11
	0,29
	14,21
	0,63
	0,01
	0,00
	0,05
	0,00
	0,01
	1,34
	0,16
	0,97

	Point 34
	0,00
	1,93
	3,89
	10,92
	0,50
	0,48
	0,04
	0,39
	25,77
	0,12
	0,03
	55,48
	0,05
	0,01
	0,02
	0,14
	0,01
	0,01
	0,11
	0,01
	0,11

	Point 35
	0,00
	1,72
	4,54
	15,81
	0,51
	0,58
	0,00
	0,52
	58,02
	1,64
	0,03
	15,66
	0,06
	0,01
	0,00
	0,07
	0,01
	0,00
	0,36
	0,06
	0,40

	Point 36
	0,00
	2,33
	4,76
	13,54
	0,52
	0,49
	0,01
	0,48
	44,58
	0,13
	0,18
	32,15
	0,22
	0,01
	0,00
	0,12
	0,00
	0,01
	0,20
	0,05
	0,21

	Point 37
	0,00
	2,59
	5,43
	16,39
	0,49
	0,50
	0,00
	0,55
	56,12
	0,18
	0,32
	16,25
	0,17
	0,01
	0,04
	0,06
	0,00
	0,01
	0,38
	0,06
	0,44

	Point 38
	0,00
	2,56
	3,97
	11,99
	0,48
	0,52
	0,00
	0,43
	55,27
	0,12
	0,13
	23,82
	0,16
	0,01
	0,02
	0,06
	0,00
	0,01
	0,17
	0,03
	0,26

	Point 39
	0,00
	1,92
	3,79
	12,29
	0,48
	0,48
	0,00
	0,43
	50,73
	0,11
	0,05
	28,96
	0,05
	0,01
	0,00
	0,11
	0,00
	0,01
	0,24
	0,05
	0,27

	Point 40
	0,00
	2,38
	8,76
	26,40
	0,77
	0,37
	0,02
	1,65
	48,50
	0,31
	0,03
	10,22
	0,02
	0,01
	0,02
	0,05
	0,00
	0,00
	0,04
	0,04
	0,41

	Point 41
	0,00
	1,97
	5,79
	15,96
	0,42
	0,30
	0,00
	0,59
	50,30
	0,10
	0,02
	23,71
	0,03
	0,02
	0,00
	0,08
	0,00
	0,00
	0,47
	0,10
	0,13

	Point 42
	0,00
	2,20
	4,85
	14,78
	0,47
	0,45
	0,00
	0,53
	63,71
	0,17
	0,03
	11,86
	0,04
	0,02
	0,01
	0,07
	0,01
	0,00
	0,38
	0,06
	0,36

	Point 43
	0,00
	1,72
	3,90
	13,51
	0,46
	0,47
	0,01
	0,44
	64,69
	0,15
	0,03
	12,32
	1,30
	0,02
	0,00
	0,07
	0,00
	0,00
	0,46
	0,08
	0,37

	Point 44
	0,00
	1,75
	4,31
	14,48
	0,44
	0,35
	0,01
	0,46
	60,15
	0,11
	0,04
	16,92
	0,02
	0,02
	0,00
	0,08
	0,00
	0,00
	0,48
	0,08
	0,28

	Point 45
	0,00
	1,55
	4,76
	28,28
	0,42
	0,41
	0,01
	0,49
	42,34
	0,10
	0,03
	13,72
	7,26
	0,02
	0,01
	0,10
	0,00
	0,00
	0,23
	0,05
	0,19

	Point 46
	0,00
	1,43
	4,45
	11,62
	0,49
	0,33
	0,00
	0,37
	46,79
	0,09
	0,03
	33,51
	0,07
	0,03
	0,00
	0,12
	0,00
	0,00
	0,47
	0,10
	0,09

	Point 47
	0,00
	1,26
	3,06
	8,28
	0,40
	0,52
	0,01
	0,35
	69,57
	0,09
	0,02
	15,24
	0,03
	0,02
	0,00
	0,08
	0,00
	0,00
	0,57
	0,09
	0,41

	Point 48
	0,00
	1,47
	3,95
	15,21
	0,44
	0,40
	0,00
	0,49
	62,73
	0,10
	0,04
	12,14
	1,97
	0,02
	0,00
	0,08
	0,00
	0,00
	0,49
	0,09
	0,37

	Point 49
	0,00
	2,24
	5,73
	16,66
	0,48
	0,20
	0,02
	0,66
	62,91
	0,19
	0,06
	10,02
	0,09
	0,02
	0,00
	0,05
	0,00
	0,01
	0,21
	0,04
	0,40

	Point 50
	0,37
	1,28
	3,33
	29,14
	0,26
	0,37
	0,01
	0,48
	49,93
	0,10
	0,03
	6,31
	7,83
	0,03
	0,01
	0,04
	0,00
	0,00
	0,13
	0,05
	0,29

	Point 51
	0,00
	1,71
	3,40
	12,44
	0,41
	0,56
	0,02
	0,41
	65,93
	0,36
	0,03
	13,72
	0,05
	0,03
	0,00
	0,07
	0,00
	0,00
	0,44
	0,08
	0,35

	Point 52
	0,70
	1,48
	3,31
	33,86
	0,26
	0,31
	0,01
	0,39
	40,90
	0,08
	0,01
	8,51
	9,55
	0,03
	0,00
	0,05
	0,00
	0,00
	0,26
	0,06
	0,23

	Point 53
	0,00
	2,21
	3,06
	12,31
	0,41
	0,37
	0,05
	0,40
	44,38
	0,12
	0,11
	35,27
	0,98
	0,01
	0,00
	0,15
	0,00
	0,02
	0,04
	0,02
	0,10

	Point 54
	0,00
	2,55
	5,55
	16,88
	0,55
	0,41
	0,00
	0,65
	58,37
	0,16
	0,13
	13,52
	0,02
	0,01
	0,00
	0,07
	0,00
	0,00
	0,58
	0,10
	0,45

	Point 55
	0,00
	1,92
	4,58
	14,12
	0,59
	0,51
	0,01
	0,58
	71,73
	0,13
	0,05
	3,47
	0,02
	0,01
	0,28
	0,03
	0,00
	0,00
	0,71
	0,10
	1,15









Supplementary Table S13. MRS analysis. Measurement conditions for the spectra of figure 4 (yellow, red, brown and pink) and figure 5 (blue, green and white).
	Colour
	Spectrum
	Device
	Laser
	Laser power
	Nº acc.
	Exposition time

	Yellow
	a1
	Qontor
	785 nm (300 mW)
	0.05 %
	50
	1 s/acc

	
	a2
	Reflex
	785 nm (300 mW)
	50 %
	10
	10 s/acc

	
	a4
	Qontor
	532 nm (50 mW)
	10 %
	30
	1 s/acc

	
	a6
	Reflex
	785 nm (300 mW)
	50 %
	5
	10 s/acc

	
	a9
	Qontor
	785 nm (300 mW)
	5 %
	3
	10 s/acc

	
	a10
	Reflex
	514 nm (25 mW)
	100 %
	5
	10 s/acc

	
	a11
	Qontor
	785 nm (300 mW)
	0.5 %
	30
	1 s/acc

	Red
	b1
	Qontor
	785 nm (300 mW)
	0.05 %
	50
	1 s/acc

	
	b3
	Reflex
	785 nm (300 mW)
	50 %
	3
	10 s/acc

	
	b4
	Qontor
	785 nm (300 mW)
	1 %
	30
	1 s/acc

	
	b6
	Reflex
	785 nm (300 mW)
	50 %
	5
	10 s/acc

	
	b8
	InnoRam
	785 nm (300 mW)
	30 %
	100
	2 s/acc

	
	b9
	Qontor
	785 nm (300 mW)
	0.5 %
	3
	10 s/acc

	
	b10
	InnoRam
	785 nm (300 mW)
	15 %
	30
	5 s/acc

	
	b11
	Qontor
	785 nm (300 mW)
	0.5 %
	30
	1 s/acc

	Brown
	c4.1
	Qontor
	473 nm (25 mW)
	10 %
	30
	1 s/acc

	
	c4.2
	Qontor
	473 nm (25 mW)
	5 %
	30
	1 s/acc

	
	c9
	Qontor
	473 nm (25 mW)
	50 %
	10
	1 s/acc

	Pink
	d1
	Qontor
	785 nm (300 mW)
	0.05 %
	50
	1 s/acc

	
	d9
	Reflex
	785 nm (300 mW)
	10 %
	10
	1 s/acc

	
	d10
	InnoRam
	785 nm (300 mW)
	10 %
	100
	0.1 s/acc

	Blue
	a1
	Qontor
	532 nm (50 mW)
	100 %
	50
	1 s/acc

	
	a2
	Reflex
	514 nm (25 mW)
	100 %
	5
	10 s/acc

	
	a3
	Qontor
	532 nm (50 mW)
	100 %
	50
	1 s/acc

	
	a5
	Qontor
	532 nm (50 mW)
	10 %
	50
	1 s/acc

	
	a6
	Reflex
	514 nm (25 mW)
	100 %
	5
	10 s/acc

	
	a7
	Reflex
	514 nm (25 mW)
	100 %
	5
	10 s/acc

	
	a9
	Qontor
	532 nm (50 mW)
	50 %
	20
	1 s/acc

	
	a10
	Reflex
	514 nm (25 mW)
	100 %
	10
	10 s/acc

	Green
	b1
	Qontor
	532 nm (50 mW)
	10 %
	50
	1 s/acc

	
	b4
	Qontor
	532 nm (50 mW)
	10 %
	30
	10 s/acc

	
	b9
	Qontor
	532 nm (50 mW)
	50 %
	20
	1 s/acc

	White
	c1
	Qontor
	532 nm (50 mW)
	10 %
	50
	1 s/acc

	
	c4
	Qontor
	785 nm (300 mW)
	0.5 %
	30
	1 s/acc

	
	c9
	Qontor
	532 nm (50 mW)
	10 %
	20
	1 s/acc









Supplementary Table S14.  Total spectroscopic analyses by MRS and μEDXRF. Types of colours and decorations.
	Fragment
	Colours
	Decoration
	MRS
	XRF 

	
	Yellow
	Red
	Brown
	Pink
	Blue
	Green
	White
	
	
	Single spot
	Map

	1
	x
	x
	x
	x
	x
	x
	x
	Quiver 
	37
	37
	1

	2
	x
	x
	
	
	x
	x
	x
	No figurative
	14
	10
	-

	3
	
	x
	
	
	x
	x
	x
	No figurative
	6
	11
	1

	4
	x
	x
	x
	
	
	x
	x
	Little owl
	38
	48
	2

	5
	
	
	
	
	x
	
	
	No figurative
	4
	6
	1

	6
	x
	x
	
	
	x
	x
	x
	No figurative
	11
	18
	1

	7
	
	
	
	
	x
	
	
	No figurative
	3
	4
	-

	8
	x
	x
	
	
	
	x
	x
	Human figure
	8
	21
	3

	9
	x
	x
	x
	x
	
	x
	x
	Lar
	58
	51
	5

	10
	x
	x
	
	x
	
	x
	x
	No figurative
	19
	26
	1

	11
	x
	x
	x
	
	
	
	x
	Goat
	12
	55
	4

	Total analyses
	208
	287
	19










Supplementary Table S15. μEDXRF mappings. Experimental conditions for the figures 3, 6 and 7.  
	Fragment
	Mapped motif
	μEDXRF mapping parameters

	
	
	Voltage (kV)
	Current (μA)
	Spot size (μm)
	Step size (μm)
	Dwell time (ms)
	Area
(mm2)
	Mapping time (min)
	Pixel Nº

	1
	Quiver
	50
	600
	25
	50
	5
	132.00 x 85.70
	377.1
	4524960

	4
	Left eye
	50
	600
	25
	50
	2.5
	28.79 x 48.41
	23.2
	557568

	
	Body
	50
	600
	25
	50
	2.5
	51.70 x 69.32
	59.7
	1433124

	6
	Indeterminate
	50
	600
	25
	50
	2
	65.51 x 33.27
	29.1
	871150

	8
	Body
	50
	600
	25
	50
	2
	53.20 x 37.60
	26.6
	800128

	
	Left arm
	50
	600
	25
	50
	2
	35.32 x 61.55
	28.9
	869086

	
	Head
	50
	600
	25
	50
	2
	40.47 x 26.64
	14.4
	431197

	9
	Left arm
	50
	600
	25
	50
	2
	61.60 x 51.10
	42.0
	1259104

	
	Clothing
	50
	600
	25
	50
	2
	42.07 x 65.30
	36.6
	1098346

	
	Right arm
	50
	600
	25
	50
	2
	55.13 x 85.01
	62.5
	1875100

	
	Head
	50
	600
	25
	50
	2
	66.30 x 41.30
	36.5
	1095276

	10
	Indeterminate
	50
	600
	25
	50
	2
	129.55 x 38.94
	67.3
	2017855

	11
	Legs
	50
	600
	25
	50
	2
	28.07 x 43.22
	16.2
	485265

	
	Back
	50
	600
	25
	50
	2
	57.89 x 16.50
	12.7
	382140

	
	Belly
	50
	600
	25
	50
	2
	38.72 x 21.17
	10.9
	327402

	
	Head
	50
	600
	25
	50
	2
	70.43 x 40.95
	38.5
	1153971








Supplementary Figures
Supplementary Figure S1. Location of Cástulo archaeological site at province of Jaén (Spain).
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Supplementary Figure S2. Distribution of μEDXRF single-spot analyses on fragment 1.
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Supplementary Figure S3. Distribution of μEDXRF single-spot analyses on fragment 2.
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Supplementary Figure S4. Distribution of μEDXRF single-spot analyses on fragment 3.
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Supplementary Figure S5. Distribution of μEDXRF single-spot analyses on fragment 4.[image: ]











Supplementary Figure S6. Distribution of μEDXRF single-spot analyses on fragment 5.
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Supplementary Figure S7. Distribution of μEDXRF single-spot analyses on fragment 6.
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Supplementary Figure S8. Distribution of μEDXRF single-spot analyses on fragment 7.
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Supplementary Figure S9. Distribution of μEDXRF single-spot analyses on fragment 8.
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Supplementary Figure S10. Distribution of μEDXRF single-spot analyses on fragment 9.
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Supplementary Figure S11. Distribution of μEDXRF single-spot analyses on fragment 10.
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Supplementary Figure S12. Distribution of μEDXRF single-spot analyses on fragment 11.
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