Supplementary data

Turning date palm waste into carbon nanodots and nano zerovalent iron composites for excellent removal of methylthioninium chloride from water

Munir Ahmada, Mutair A. Akanjia, Adel R.A. Usmana,b, Abdullah S.F. Al-Farraja, Yiu Fai Tsangc, Mohammad I. Al-Wabela,c*

aSoil Sciences Department, College of Food & Agricultural Sciences, King Saud University, P.O.

Box 2460, Riyadh 11451, Kingdom of Saudi Arabia

bDepartment of Soils and Water, Faculty of Agriculture, Assiut University, Assiut 71526, Egypt

cDepartment of Science and Environmental Studies, The Education University of Hong Kong,

Hong Kong

Corresponding author

Email: malwabel@ksu.edu.sa

Phone: +966-1-467-8441

Fax: +966-1-467-8440

Table S1. Comparison of maximum adsorption capacity of various adsorbents as predicted by Langmuir isotherm for methylthioninium chloride sorption (date palm waste-derived biochar (DBC), date palm waste-derived carbon nanodots (nCD-DBC), and date palm waste-derived biochar composited with nano zero-valent iron (nZVI-DBC)).

| Order | Sorbent | Adsorption temperature (°C) | Adsorption pH | Equilibrium time (min) | Langmuir isotherm predicted maximum adsorption capacity (mg g-1) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | nCD-DBC | 23 | 7 | 1440 | 1558.6 | This study |
| 2 | nZVI-DBC | 23 | 7 | 1440 | 1182.9 |  |
| 3 | DBC | 23 | 7 | 1440 | 851.67 |  |
| 4 | Calcium alginate beads | 25 | 5 | 1440 | 1282.20 | Wang et al.1 |
| 5 | Ball milled bamboo biochar+ calcium alginate beads | 25 | 5 | 1440 | 1210.70 |  |
| 6 | Eucalyptus residue-activated carbon+H3PO4 | 25 | 7 | 1440 | 1000 | Han et al.2 |
| 7 | Eucalyptus residue-activated carbon+H3PO4 | 35 | 7 | 1440 | 990.10 |  |
| 8 | Eucalyptus residue-activated carbon+H3PO4 | 45 | 7 | 1440 | 980.39 |  |
| 9 | NaOH-activated carbon | 25 | 6.5 | 150 | 916.26 | Cazetta et al.3 |
| 10 | Thiosemicarbazide functionalized graphene oxide | 30 | -- | 120 | 724.6377 | Bu et al.4 |
| 11 | Core@double-shell structured HNTs/Fe3O4/ poly(DA + KH550) nano-hybrids | 25 | 10 | 180 | 714.29 | Wan et al.5 |
| 12 | Metal-organic framework UiO-66 | 25 | 10 | 300 | 543.48 | Song et al.6 |
| 13 | Bamboo-based activated carbon+KOH | 30 | 7 | 2880 | 454.2 | Hameed et al.7 |
| 14 | Graphene oxide modified persimmon tannin | 30 | 8 | 180 | 444.44 | Wang et al.8 |
| 15 | Graphene oxide modified persimmon tannin | 40 | 8 | 180 | 434.38 |  |
| 16 | Graphene oxide modified persimmon tannin | 50 | 8 | 180 | 404.85 |  |
| 17 | Cotton stalk-activated carbon + ZnCl2 | 25 | 9 | 120 | 315.45 | Deng et al.9 |
| 18 | Nano-zerovalent iron-Bamboo | 32 | 7.6 | 120 | 322.6 | Shaibu et al.10 |
| 19 | Iron/cerium modified activated carbon | 40 | 6-7 | 180 | 264.55 | Cheng et al.11 |
| 20 | Nanoscale manganese-bamboo | 32 | 7.6 | 120 | 263.2 | Shaibu et al.10 |
| 21 | Iron/cerium modified activated carbon | 30 | 6-7 | 180 | 255.76 | Cheng et al.11 |
| 22 | Nano-zerovalent iron | 30 | 9.5 | 1.00 | 208.33 | Arabi and Sohrabi12 |
| 23 | Activated carbon | 40 | 6-7 | 180 | 192.31 | Cheng et al.11 |
| 24 | Ball milled bamboo biochar | 25 | 5 | 1440 | 184.1 | Wang et al.1 |
| 26 | Activated carbon | 30 | 6-7 | 180 | 178.25 | Cheng et al.11 |
| 28 | Carbon nanotubes | 37 | -- | 120 | 119.71 | Shahryari et al.13 |
| 29 | Carbon nanotubes | 27 | -- | 120 | 109.31 |  |
| 30 | Carbon nanotubes | 17 | -- | 120 | 103.62 |  |
| 31 | SnO2 quantum dots decorated silica nanoparticles | 25 | 6.1 | 60.0 | 73.15 | Dutta et al.14 |
| 32 | Carbon nanotubes | 60 | 7 | 90.0 | 64.7 | Yao et al.15 |
| 33 | Carbon nanotubes | 25 | 7 | 90.0 | 46.2 |  |
| 34 | Carbon dots derived poly(4,4′-diaminodiphenylmethane | 25 | -- | 120 | 19.6 | Maruthapandi et al.16 |
| 35 | Sunflower oil cake-activated carbon+H2SO4 | 25 | 6 | 1440 | 16.43 | Karagöz et al.17 |
| 36 | Sunflower oil cake-activated carbon | 25 | 6 | 1440 | 10.21 |  |

Fig. S1. pH at point of zero charge (PZC) of date palm waste derived biochar (DBC), date palm waste derived biochar composite with nano zerovalent iron (nZVI-DBC) and nano carbon dots (nCD-DBC).

Fig. S2. Particle size distribution of a: date palm waste derived biochar (DBC), and b: date palm waste derived biochar composite with nano zerovalent iron (nZVI-DBC), and c: nano carbon dots (nCD-DBC).

Fig. S3. a: TGA (thermogravimetric analyses) thermograms and b: R50 (recalcitrance potential) of date palm waste derived biochar (DBC), date palm waste derived carbon nanodots (nCD-DBC) and date palm waste derived biochar composited with nano zerovalent iron (nZVI-DBC).

Fig. S4. TEM (transmission electron microscope) images of date palm waste derived carbon nanodots (nCD-DBC). The diameter of the nCD-DBC particles was estimated by using Adobe Photoshop CS6 software by randomly selecting the particles in the sample18.

References

- Wang B, Gao B, Wan Y (2019) Comparative study of calcium alginate, ball-milled biochar, and their composites on aqueous methylene blue adsorption. Environ Sci Pollut Res 26(12):11535-11541.

- Han Q, Wang J, Goodman BA, Xie J, Liu Z (2020) High adsorption of methylene blue by activated carbon prepared from phosphoric acid treated eucalyptus residue. Powder Technol. 366:239-248.

- Cazetta AL, Vargas AM, Nogami EM, Kunita MH, Guilherme MR, Martins AC, Silva TL, Moraes JC, Almeida VC (2011) NaOH-activated carbon of high surface area produced from coconut shell: Kinetics and equilibrium studies from the methylene blue adsorption. Chem Engi J 174:117-125.

- Bu J, Yuan L, Zhang N, Liu D, Meng Y, Peng X (2020) High-efficiency adsorption of methylene blue dye from wastewater by a thiosemicarbazide functionalized graphene oxide composite. Diamond Relat Mater 101:107604.

- Wan X, Zhan Y, Long Z, Zeng G, He Y (2017) Core@ double-shell structured magnetic halloysite nanotube nano-hybrid as efficient recyclable adsorbent for methylene blue removal. Chemi Engi J 330:491-504.

- Song X, Yang P, Wu D, Zhao P, Zhao X, Yang L, Zhou Y (2020) Facile synthesis of metal-organic framework UiO-66 for adsorptive removal of methylene blue from water. Chemi Phy 531:110655.

- Hameed BH, Din AM, Ahmad AL (2007) Adsorption of methylene blue onto bamboo-based activated carbon: kinetics and equilibrium studies. J Hazard Mater 141:819-825.

- Wang Z, Gao M, Li X, Ning J, Zhou Z, Li G (2020) Efficient adsorption of methylene blue from aqueous solution by graphene oxide modified persimmon tannins. Mater Sci Engi C 108:110196.

- Deng H, Yang L, Tao G, Dai J (2009) Preparation and characterization of activated carbon from cotton stalk by microwave assisted chemical activation—application in methylene blue adsorption from aqueous solution. J Hazard Mater 166:1514-1521.

- Shaibu SE, Adekola FA, Adegoke HI, Ayanda OS (2014) A comparative study of the adsorption of methylene blue onto synthesized nanoscale zero-valent iron-bamboo and manganese-bamboo composites. Materials 7(6):4493-4507.

- Cheng S, Zhang L, Ma A, Xia H, Peng J, Li C, Shu J (2018) Comparison of activated carbon and iron/cerium modified activated carbon to remove methylene blue from wastewater. J Environ Sci 65:92-102.

- Arabi S, Sohrabi MR (2014) Removal of methylene blue, a basic dye, from aqueous solutions using nano-zerovalent iron. Water Sci Technol 70(1):24-31.

- Shahryari Z, Goharrizi AS, Azadi M (2010) Experimental study of methylene blue adsorption from aqueous solutions onto carbon nano tubes. Int J Water Res Environ Engi 2(2):016-028.

- Dutta D, Thakur D, Bahadur D (2015) SnO2 quantum dots decorated silica nanoparticles for fast removal of cationic dye (methylene blue) from wastewater. Chemi Engi J 281:482-490.

- Yao Y, Xu F, Chen M, Xu Z, Zhu Z (2010) Adsorption behavior of methylene blue on carbon nanotubes. Bioresour Technol 101(9):3040-3046.

- Maruthapandi M, Kumar VB, Gedanken A (2018) Carbon dot initiated synthesis of poly (4, 4′-diaminodiphenylmethane) and its methylene blue adsorption. ACS Omega 3(6):7061-7068.

- Karagöz S, Tay T, Ucar S, Erdem M (2008) Activated carbons from waste biomass by sulfuric acid activation and their use on methylene blue adsorption. Bioresour Technol 99(14):6214-6222.

- Aijaz MO, Karim MR, Alharbi HF, Alharthi NH. (2019) Novel optimised highly aligned electrospun PEI-PAN nanofibre mats with excellent wettability. Polymer 180: 121665.