Supporting Information

Rapid Demulsification of Pickering Emulsions Triggered by Controllable Magnetic Field

Hui Yang,*,#,a Shujuan Wang,#,a Wei Zhang,a Jiazhong Wu,b Siyu Yang,b Danfeng Yu,c Xu Wu,c Yang Sun,d Jinben Wanga

aCAS Key Lab of Colloid, Interface and Chemical Thermodynamics, Institute of Chemistry, Chinese Academy of Sciences, Beijing 100190, P. R. China

bState Key Laboratory of Enhanced Oil Recovery, Research Institute of Petroleum Exploration and Development of PetroChina, Beijing 100083, P. R. China

cDepartment of Chemistry and Chemical Engineering, Guangzhou University, Guangzhou, Guangdong 510006, P. R. China

dCenter for Physicochemical Analysis and Measurement, Institute of Chemistry, Chinese Academy of Sciences, Beijing 100190, P. R. China

Table S1  Conductivity values in the presence of CIPs at different concentrations.

| Particle Concentration wt% | Conductivity μS/cm |
| --- | --- |
| 2 | 0.232 |
| 5 | 0.835 |
| 10 | 0.340 |

Table S2  Distribution of Particles in the Dodecane-in-Water Pickering Emulsions Stabilized by CIPs Initially in Oil.

| Particle concentration/wt% | mpo/g | mpa/g | mpe/g | X/% |
| --- | --- | --- | --- | --- |
| 2 | 0.061 | 0.007 | 0.054 | 88.5 |
| 5 | 0.158 | 0.022 | 0.136 | 86.1 |
| 10 | 0.333 | 0.083 | 0.25 | 75.1 |

Table S3  Composition of the Dodecane-in-Water Pickering Emulsions Stabilized by CIPs Initially in Oil.

| Particle concentration/wt% | Ve/mL | φwe/vol % | φoe/vol % | mpe/g | φp/g (100 mL-1) |
| --- | --- | --- | --- | --- | --- |
| 2 | 5.4 | 26.0 | 74.0 | 0.054 | 1 |
| 5 | 5.7 | 29.8 | 70.2 | 0.136 | 2.4 |
| 10 | 6 | 33.3 | 66.7 | 0.25 | 4.2 |

(a)   (b)

(c)   (d)

Figure S1.  Drop size distributions of emulsions stabilized by CIPs after preparation (a), and placed for 15 day (b), 35 days (c), and 85 days (d) at 5wt%.

24°

Figure S2  Contact angle (CA) of surfaces pressed by CIPs.

Pickering emulsions

After demulsification

2%

2%

5 min

6 min

10%

10%

a

b

Figure S3  Pickering emulsions stabilized by CIPs under an alternating asymmetrical magnetic field at different concentrations of (a) 2 wt% and (b) 10 wt%.

6 min

14 min

22 min

9A 0.2Hz

6A 0.2Hz

4A 0.2Hz

Pickering emulsions

After demulsification

a

b

c

Figure S4  Pickering emulsions stabilized by 5 wt% CIPs under an alternating asymmetrical magnetic field at different currents of (a) 9A, (b) 6A, and (c) 4A.

(a)   (b)

Figure S5.  Drop size distributions of emulsions stabilized by CIPs after preparation (a), and under pulsed asymmetrical magnetic field (b).

Figure S6.  Mean drop size after each cycle of destabilization and reformation.

Oil droplet

CIPs

Fr1

Fr2

Fr3

Fr4

N

S

F'r1

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

F'r2

a. Uniform magnetic field

Fr5

Fr6

Fr7

Fr8

N

S

F'r3

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

N S

F'r4

b. Non-uniform magnetic field

Fr1 = Fr2 = Fr3 = Fr4; F'r1 = F'r2

Fr5 > Fr6 > Fr7 > Fr8; F'r3 > F'r4

Figure S7  Corresponding positioning of particles at a model droplet interface giving a solid-stabilized oil-in-water emulsion and analysis of forces after introducing (a) an uniform magnetic field and (b) a non-uniform magnetic field.

| a | b | c |
| --- | --- | --- |
| Figure S8 Bottom vial area under magnetic field over time. |  |  |

Figure S9  Setup scheme of the electromagnet field generator.