Supplementary Information

Pulmonary surfactant inhibition of nanoparticle uptake by alveolar epithelial cells

M. Radiom1,2*,, M. Sarkis1, O. Brookes3, E.K. Oikonomou1, A. Baeza-Squiban3 and J.-F. Berret1*

1Université de Paris, UMR CNRS 7057, Laboratoire Matière et Systèmes Complexes, Paris, France.

2Present address: Institute for Food, Nutrition and Health, D-HEST, ETH Zürich, Zürich, Switzerland

3Université de Paris Unité BFA, UMR CNRS 8251, Laboratoire de Réponses Moléculaires et Cellulaires aux Xénobiotiques, Paris, France

Correspondence: milad.radiom@hest.ethz.ch, jean-francois.berret@u-paris.fr

Outline

S1 – Production volume and industrial applications for silica nanoparticles (2012)

S2 – Curosurf composition and comparison with native surfactant

S3 – Summary of exposure conditions on glass coverslip

S4 – Summary of exposure conditions on transwell

S5 – Cryo-TEM images of silica nanoparticles

S6 – Dynamic light scattering of silica nanoparticles dispersion in culture media

S7 – Cryo-TEM images of Curosurf vesicles

S8 – Dynamic light scattering of silica nanoparticle-Curosurf dispersions

S9 – Cellular viability assays

S10 – TEM of internalized silica nanoparticles without or with Curosurf

Supplementary Information S1

Production volume and industrial applications for silica nanoparticles (2012)

List of silica nanoparticle applications5:

Silica nanoparticles Production volumes for nanomaterials (2012): 500 000 tons

Aerogels as light-weight materials and thermal insulators

Filler in rubber and polymer compound materials

Nanoelectronics fabrication as mask substrate

Bioceramics (as coatings for implants)

Anti-corrosion and wear resistant coatings

Insulators with high dielectric properties

Supplementary Information S2

Curosurf composition and comparison with native surfactant

Lipid and protein compositions of native surfactant obtained by saline bronchoalveolar lavage compared to that of Curosurf, a pulmonary surfactant substitute indicated for the rescue treatment of Respiratory Distress Syndrome (RDS) in premature infants1. The concentrations are given in percentage by weight of the total lipid content.

| Lipid composition (%, g/g of total lipid) | Native Surfactant | Curosurf |
| --- | --- | --- |
| Phosphatidylcholine (PC) | 70 – 85 | 67 – 74 |
| Lysophosphatidylcholine (LPC) | 0.5 | < 1 |
| Sphingomyelin (SM) | 2 | 8.1 |
| Cholesterol | 5 | 0 |
| Phosphatidylinositol (PI) | 4 – 7 | 3.3 |
| Phosphatidylserine (PS) | 5 |  |
| Phosphatidylethanolamine (PE) | 3 | 4.5 |
| Phosphatidylglycerol (PG) | 7 – 10 | 1.2 |
| Protein concentration (%, g/g of total lipid) | Native Surfactant | Curosurf |
| SP-A | 4 | 0 |
| SP-B | 1 | 0.3 |
| SP-C | 1 | 0.7 |
| SP-D | 4 | 0 |

Supplementary Information S3

Summary of exposure conditions on glass coverslip

Generally, four exposure conditions were used including neat nanoparticles, X = 2, X = 20 and neat Curosurf. The table below summarizes the dispersion preparations for exposure on coverslip. (Top) Concentration, volume and resulting mass of silica nanoparticles and Curosurf during sample preparation. (Middle) Volume and surface concentration of silica nanoparticles in the final dispersion. (Bottom) Volume and surface concentration of Curosurf in the final dispersion. Calculations are for coverslip cell culture support placed inside a 6-well plate, =9.6 cm2 . The difference VTOT-VNP+VCuro is made up by addition of serum free culture medium.

| Initial | Exposure | cNP (g l-1) | VNP (µl) | mNP (µg) | cCuro (g l-1) | VCuro (µl) | mCuro (µg) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Neat nanoparticle | 0.2 | 1000 | 200 |  |  | 0 |
|  | X = 2 | 4 | 50 | 200 | 4 | 100 | 400 |
|  | X = 20 | 21 | 9.5 | 199.5 | 21 | 190.5 | 4000.5 |
|  | Neat Curosurf |  |  | 0 | 4 | 100 | 400 |

| Final – nanoparticle | Exposure | mNP (µg) | VTOT (µl) | cNP (g l-1) | A (cm2) | mNPA (µg cm-2) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Neat nanoparticle | 200 | 2000 | 0.1 | 9.6 | 20.8 |
|  | X = 2 | 200 | 2000 | 0.1 | 9.6 | 20.8 |
|  | X = 20 | 199.5 | 2000 | 0.1 | 9.6 | 20.8 |
|  | Neat Curosurf | 0 | 2000 | 0 | 9.6 | 0 |

| Final – Curosurf | Exposure | mCuro (µg) | VTOT (µl) | cCuro (g l-1) | A (cm2) | mCuroA (µg cm-2) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Neat nanoparticle | 0 | 2000 | 0 | 9.6 | 0 |
|  | X = 2 | 400 | 2000 | 0.2 | 9.6 | 41.6 |
|  | X = 20 | 4000.5 | 2000 | 2 | 9.6 | 416 |
|  | Neat Curosurf | 400 | 2000 | 0.2 | 9.6 | 41.6 |

Supplementary Information S4

Summary of exposure conditions on transwell

Generally, four exposure conditions were used including neat nanoparticles, X = 2, X = 20 and neat Curosurf. The table below summarizes the dispersion preparations for exposure on transwell. (Top) Concentration, volume and resulting mass of silica nanoparticles and Curosurf during sample preparation. (Middle) Volume and surface concentration of silica nanoparticles in the final dispersion. (Bottom) Volume and surface concentration of Curosurf in the final dispersion. Calculations are for transwell insert, =1.12 cm2 . The difference VTOT-VNP+VCuro is made up by addition of serum free culture medium.

| Initial | Exposure | cNP (g l-1) | VNP (µl) | mNP (µg) | cCuro (g l-1) | VCuro (µl) | mCuro (µg) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Neat nanoparticle | 0.2 | 250 | 50 |  |  | 0 |
|  | X = 2 | 4 | 12.5 | 50 | 4 | 25 | 100 |
|  | X = 20 | 21 | 2.4 | 50.4 | 21 | 47.6 | 999.6 |
|  | Neat Curosurf |  |  | 0 | 4 | 25 | 100 |

| Final – nanoparticle | Exposure | mNP (µg) | VTOT (µl) | cNP (g l-1) | A (cm2) | mNPA (µg cm-2) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Neat nanoparticle | 50 | 500 | 0.1 | 1.12 | 44.6 |
|  | X = 2 | 50 | 500 | 0.1 | 1.12 | 44.6 |
|  | X = 20 | 50.4 | 500 | 0.1 | 1.12 | 45.0 |
|  | Neat Curosurf | 0 | 500 | 0 | 1.12 | 0 |
|  |  | mNP (µg) | VTOT (µL) | cNP (g L-1) |  |  |

| Final – Curosurf | Exposure | mCuro (µg) | VTOT (µl) | cCuro (g l-1) | A (cm2) | mCuroA (µg cm-2) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Neat nanoparticle | 0 | 500 | 0 | 1.12 | 0 |
|  | X = 2 | 100 | 500 | 0.2 | 1.12 | 89.3 |
|  | X = 20 | 999.6 | 500 | 2 | 1.12 | 892.5 |
|  | Neat Curosurf | 100 | 500 | 0.2 | 1.12 | 89.3 |

Supplementary Information S5

Cryo-TEM images of silica nanoparticles

Cryo-TEM images (a) and size distribution (b) of silica nanoparticles. The distribution is well accounted for by a log-normal function of median 41.2 nm and dispersity 0.11.

Supplementary Information S6

Dynamic light scattering of silica nanoparticles dispersion in culture media

Silica nanoparticles in DMEM and RPMI after 5-minute incubation (25°C). The DLS experiments were performed at two concentrations, 0.1 and 1 g l-1, both with and without fetal bovine serum (FBS).

| Conc. (g l-1) | Solvent | FBS | DH (nm) | ± Delta (DH) (nm) | Derived count rate (kcps) |
| --- | --- | --- | --- | --- | --- |
| 0.1 | DMEM | no | 1309 | 385 | 6089 |
| 0.1 | DMEM | yes | 380 | 124 | 25244 |
| 1 | DMEM | no | 6813 | 1580 | 31849 |
| 1 | DMEM | yes | 4181 | 1190 | 43258 |
| 0.1 | RPMI | no | 1196 | 328 | 6394 |
| 0.1 | RPMI | yes | 441 | 159 | 23194 |
| 1 | RPMI | no | 3863 | 1018 | 31487 |
| 1 | RPMI | yes | 3616 | 1140 | 42071 |

Silica nanoparticles in DMEM and RPMI after 120-minute incubation (25°C). The DLS experiments were performed at two concentrations, 0.1 and 1 g l-1, both with and without fetal bovine serum (FBS).

| Conc. (g l-1) | Solvent | FBS | DH (nm) | ± Delta (DH) (nm) | Derived count rate (kcps) |
| --- | --- | --- | --- | --- | --- |
| 0.1 | DMEM | no | 1235 | 274 | 5976 |
| 0.1 | DMEM | yes | 396 | 117 | 29120 |
| 1 | DMEM | no | 3099 | 869 | 37185 |
| 1 | DMEM | yes | 2704 | 788 | 47335 |
| 0.1 | RPMI | no | 1563 | 428 | 6121 |
| 0.1 | RPMI | yes | 467 | 151 | 28148 |
| 1 | RPMI | no | 2970 | 673 | 34970 |
| 1 | RPMI | yes | 2401 | 759 | 49447 |

Supplementary Information S7

Cryo-TEM images of Curosurf vesicles

Cryo-TEM images of Curosurf vesicles at a concentration of 5 g l-1 2-4.

Supplementary Information S8

Dynamic light scattering of silica nanoparticles-Curosurf dispersions

Scattered intensity (a and c) and hydrodynamic diameter (b and d) of silica particles mixed with Curosurf at T = 25ºC (a and b) and at T = 37ºC (c and d). X is the ratio between the surfactant and nanoparticle mass concentrations. Continuous lines in green in a and c represent the scattered intensities calculated assuming that particles and vesicles do not interact. The error bars represent the mean of the standard deviations for measurements made in triplicate.

Supplementary Information S9

Cellular viability assays

WST-1 toxicity assay. Cells were seeded in a 96-well plate at 20k cells per well in white DMEM with serum. After 24 h, the cells were rinsed with PBS and incubated for another 24 h at 37°C with 200 μl of silica in white DMEM. The cells were rinsed with PBS and incubated for 30 min with 100 μl of WST-1 per well (dilution 1:20 in white DMEM). The assay is based upon the reduction by cellular dehydrogenase of the achromatic tetrazolium salt WST-1 to the dark yellow colored soluble formazan. The generation of formazan was measured at 450 nm in a microplate reader (ELx808, Biotek Instruments, Winooski, United States) against a blank containing culture media and WST-1 and the data were corrected from the absorbance at 630 nm. Positive controls were performed with hydrogen peroxide and the non-interference between nanoparticles, cells and WST-1 was assessed treating half of the cultures with Triton (2% in white DMEM, 15 min of incubation at 37°C). Data are represented as means ± standards deviations (n = 3) and were analyzed with the GraphPad Prims 7 software using variance analysis (one-way ANOVA) followed by Dunnett’s test with p = 0.0332, 0.0021, 0.002 and 0.0001 (one to four stars respectively). In figure below, a and b) cell viability of A549 treated with increasing concentration of silica in DMEM without and with serum, respectively. c) Cell viability of A549 treated with an increasing concentration of Curosurf in serum-free medium. d) Cell viability of A549 treated with an increasing concentration of silica-Curosurf dispersion at X = 20 in serum-free medium.

Supplementary Information S10

TEM of internalized silica nanoparticles without or with Curosurf

The figure below shows TEM images of positively charged silica internalized by A549 cells where vacuoles are also formed in the process. The nanoparticles enter the cells by disrupting the plasma membrane.

The figure below shows TEM images of supported lipid bilayer (SLB) coated positively charged silica internalized by A549 cells. Vacuoles are absent in this process. The nanoparticles are internalized via membrane bound vesicles.

References

1.	Braun, A.; Stenger, P. C.; Warriner, H. E., et al., A Freeze-Fracture Transmission Electron Microscopy and Small Angle X-Ray Diffraction Study of the Effects of Albumin, Serum, and Polymers on Clinical Lung Surfactant Microstructure. Biophysical Journal 2007, 93 (1), 123-139.

2.	Mousseau, F.; Berret, J. F., The role of surface charge in the interaction of nanoparticles with model pulmonary surfactants. Soft Matter 2018, 14 (28), 5764-5774.

3.	Mousseau, F.; Le Borgne, R.; Seyrek, E., et al., Biophysicochemical Interaction of a Clinical Pulmonary Surfactant with Nanoalumina. Langmuir 2015, 31 (26), 7346-7354.

4.	Mousseau, F.; Puisney, C.; Mornet, S., et al., Supported Pulmonary Surfactant Bilayers on Silica Nanoparticles: Formulation, Stability and Impact on Lung Epithelial Cells. Nanoscale 2017, 9 (39), 14967-14978.

5.	The Global Market for Aluminium Oxide Nanoparticles, in TECHNOLOGY REPORT No. 76. 2013, Future Markets, Inc.