Facile Synthesis and Defect Optimization of 2D-layered MoS2 on TiO2 Heterostructure for Industrial Effluent, Wastewater Treatments

Ramalingam Gopal1*, Maria Magdalane Chinnapan2, Arjun Kumar Bojarajan1,  Naresh Kumar Rotte 2, Joice Sophia Ponraj3,4, Ravi Ganesan5, Ivanov Atanas 6, Manivannan Nadarajah 7, Rajesh Kumar Manavalan8,  Joao Gaspar4

1Quantum Materials Research Lab (QMRL), Department of Nanoscience and Technology, Alagappa University, Karaikudi - 630003, Tamil Nadu, India.

2Department of Chemistry, St. Xavier College (Autonomus), Tirunelveli 627002, Tamil Nadu, India.

3Centre for Advanced Materials, Integrated-Inter-Department of LiWET Communications, Aaivalayam - Dynamic Integrated Research Academy and Corporations (A-DIRAC), Coimbatore 641046, India

4Department of Micro and Nanofabrication, INL–International Iberian Nanotechnology Laboratory, 4715-330 Braga, Portugal

5Department of Physics, Alagappa University, Karaikudi 630003, Tamil Nadu, India.

6Department of Mechanical, Aerospace and Civil Engineering (MACE), Brunel University, Uxbridge, UK

7Department of Design, Brunel University, Uxbridge, UK

8Institute of Natural Science and Mathematics, Ural Federal University, 620002 Yekaterinburg, Russia

*Corresponding authors: Dr.G.Ramalingam, Alagappa University, Karaikudi-India.

Email:ramanloyola@gmail.com

C.Maria Magdalane, Department of Chemistry, St.Xavier College (Autonomus), Tirunelveli 627002, Tamilnadu, India. Email:cmagdalane@yahoo.com

Supplementary Information

Characterizations:

X-ray diffraction patterns were recorded using Bruker advance diffractometer with a scanning rate of 5° per min with Cukα radiation source (λ=1.54060 Å) operating at 40 kV. The optical properties were analyzed using Shimadzu UV-2550 spectrophotometer in the range of 200 to 800 nm. Emission spectra with excitation wavelength of 320 nm were performed by the ultraviolet-visible-near infrared spectrophotometer (Varian Cary Eclipse Photo Luminescence, Oxford Low temperature LN2 77K set up). PHI - VERSAPROBE III – X-ray Photoelectron Spectroscopy was used with Monochromatic X-ray Beam (15 µm). Transmission electron microscopy measurements (TEM) were conducted through JEOL 2100 instrument with an operating voltage of 25KeV. Elemental analysis was performed on energy-dispersive X-ray spectrometer included in the high resolution-TEM. Electrochemical impedance spectroscopy was carried out using BioLogic SP-300 electrochemical workstation operated at  102 to 106 Hz frequency range with 0.5 M KCl solution containing 5.0 mM K3[Fe(CN)6]/K4 [Fe(CN)6] under open circuit potential conditions.

Figure S1. Elemental spectrum (EDAX) and mapping images of Ti, O, Mo, S and figure namely identified (a), (b), (c) and (e) respectively.

Table. ST1.Obtained data from equivalent circuit [Rs(Qdl(RCT(Q dl (REW))))]for PT, MT, L-MT

| Code | Rs /Ω cm2 | Qdl/ F cm-2 | n | RCT /Ω cm2 | Qdl/ F cm-2 | n | RE /Ω cm2 | W/cm s-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| L-MT | 34.06 | 1.05x10-8 | 0.9039 | 336.7 | 2.4x10-5 | 0.8732 | 0.3509 | 1x10-20 |
| MT | 46.57 | 3.96x10-9 | 0.9582 | 426.8 | 4.211x10-5 | 0.8217 | 1.25x1011 | 1x10-20 |
| PT | 373 | 1.353x10-5 | 0.8635 | 488.2 | 0.001714 | 0.56 | 5320 | 0.02407 |

Table ST2. Evaluation of photocatalysis and comparison with reported ones in dye degradation.

| Nanocomposite | Dye | Deg.Time Deg.( %) | Light source | (mg)Cat / (mg/L)Dye, mlDye | Ref |
| --- | --- | --- | --- | --- | --- |
| 3DMoS2@TiO2 @poly (methyl methacrylate) | Methyl Orange (MO) | 50 min 95.7% | UV Light | 100mg/10(mg/L), 100 ml | 25 |
| MoS2 titania nanoheterojunctions | Methylene Blue(MB) | 100 min 90% | 20 W tungsten halogen lamp | 10mg/10(mg/L), 100ml | 30 |
| TiO2/MoS2 composite | MO | 10 min 97% | 500 W xenon long-arc lamp | 400mg/(20mg/L), 100ml | 57 |
| 3D MoS2 nanosheet/TiO2 nanofiber heterostructures | Rhodamine B(Rh B), MO | 120 min 98.2%, 97.0% | 50 W high-pressure mercury lamp | 10mg/10(mg/L), 100ml | 58 |
| CdS–TiO2–Au | MO | 300 min 98% | 400 W metal halogen lamp | 150 mg/10(mg/L), 100 ml | 59 |
| 1D CdS NWs@TiO2 NPs | Mixture of MO Rh B MB | 120 sec 120 sec 180 sec 98.2% 99.2% ~100% | Sunlight | 15 mg/10(mg/L), 10 ml 15 mg/10(mg/L) , 10 ml 15 mg/10(mg/L) , 10 ml | 60 |
| CdS/TiO2 heteronanofibers | MB | 170 min 86% | 800 W xenon lamp | 100 mg/20(mg/L), 200 ml | 61 |
| Co/Ti LDH | CR | 75 min 99.7% | 300 W tungsten lamp | 15 mg/5(mg/L), 200 ml | 62 |
| ZrO2/TiO2 | RhB | 50min 100% | UV light (18 W, l = 254 nm) | 30 mg/10(mg/L), 30 ml | 63 |
| SnO2/TiO2 | Malachite green (MG) | 75 min, 94%. | 400 W metal halogen lamp | 60 mg/30(mg/L), 100 ml | 54 |
| L-cysteine capped MoS2@TiO2 (L-MT) | CR | 120 min, 97%. | 400 W metal halogen lamp | 60 mg/15(mg/L), 100 ml | Present work |