Supplementary Information

Environmentally Friendly Pd(II) Recovery from Spent Automotive Catalysts Using Resins Impregnated with a Pincer-Type Extractant

Manabu Yamada1, Shun Kimura2, Muniyappan Rajiv Gandhi3 & Atsushi Shibayama4

1 Research Center of Advanced Materials for Breakthrough Technology, Graduate School of Engineering Science, Akita University, 1-1 Tegatagakuen-machi, Akita 010-8502, Japan; 2Applied Chemistry Course, Department of Materials Science, Graduate School of Engineering Science, Akita University, 1-1 Tegatagakuen-machi, Akita 010-8502, Japan; 3 Quality Control Department, Panipat Refinery & Petrochemical Complex, Indian Oil Corporation Limited, Haryana, 132140, India; 4 Graduate School of International Resources Science, Akita University, 1-1 Tegatagakuen-machi, Akita 010-8502, Japan

*Corresponding author. Tel +81 18 889 3068; fax: +81 18 889 3068.

E-mail address: myamada@gipc.akita-u.ac.jp

Table of content

Table S1. Physical and chemical properties of XAD resin.

Figure S1. (a) The chemical structure of XAD-7 and (b) cluster model of XAD-7 surface.

Figure S2. The relationship between impregnated amounts of 1 into XAD-7 and Pd(II) quantity adsorbed by 1-EIR. Sorption condition: [HCl] = 0.1~8.0 M, [Pd(II)] = 100 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 24 h.

Figure S3. Effect of shaking time for Pd(II) adsorption capability of 1-EIR. Sorption condition: [HCl] = 0.1 M, [Pd(II)] = 100 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 0 ~ 240 min.

Figure S4. Photographs a) before and b) after Pd(II) adsorption by 1-EIR.

Figure S5. Nitrogen isotherms of XAD-7 (red circle) and 1-EIR (blue circle).

Figure S6. Brunauer-Emmett-Teller (BET) plots and the sorption parameters of a) XAD-7 and b) 1-EIR.

Figure S7.  Pore size distribution of XAD-7 (red circle) and 1-EIR (blue circle) by Dollimore-Heal (DH) method.

Figure S8. The sizes of a PdCl42- species and a CH4N2S molecule.

Figure S9. Photographs a) before and b) after Soxhlet extraction of residual Pd(II) in 1-EIR.

Figure S10. Full scan X-ray photoelectron spectroscopy (XPS) after Soxhlet extraction from the undesorbed Pd(II) in 1-EIR.

Figure S11. 1H NMR spectra of the Pd(II)–extractant 1 complex flaked from Pd(II)-loaded 1-EIR.

Figure S12. a) Freundlich and b) Langmuir isotherms for Pd(II) sorption by 1-EIR. Sorption conditions: 1-EIR = 0.1 g, [HCl] = 0.1 M; [Pd(II)] = 500–700 ppm (= mg L−1); temperature = 293–313 K; shaking time = 24 h; shaking speed = 80 rpm.

Figure S13. Van’t Hoff plot relating ln K0 against 1/T for Pd(II) sorption by 1-EIR. Sorption conditions: 1-EIR = 0.1 g, [HCl] = 0.1 M; [Pd(II)] = 500–700 ppm (= mg L−1); temperature = 293–313 K; shaking time = 24 h; shaking speed = 80 rpm.

Figure S14. Pseudo-first-order for Pd(II) sorption by 1-EIR. Sorption condition: [HCl] = 0.1 M, [Pd(II)] = 600 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 0.5~12 h.

Figure S15. Pseudo-second-order for Pd(II) sorption by 1-EIR. Sorption condition: [HCl] = 0.1 M, [Pd(II)] = 600 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 0.5~12 h.

Figure S16. Particle diffusion for Pd(II) sorption by 1-EIR. Sorption condition: [HCl] = 0.1 M, [Pd(II)] = 600 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 0.5~12 h.

Figure S17. Intraparticle diffusion for Pd(II) sorption by 1-EIR. Sorption condition: [HCl] = 0.1 M, [Pd(II)] = 600 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 0.5~12 h..

Table S2. Application of kinetic models to the sorption of Pd(II) ions onto 1-EIR at r.t.

Figure S18. Selective Pd(II) sorption of 1-EIR from a simulated 13 metals containing HCl solution. Sorption condition: [HCl] = 0.1 M, [Metals] = each 100 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 3 h.

Table S3. Metal species and metal concentration in the leachate of automotive catalyst.

Table S1. Physical and chemical properties of XAD resin.

| Constituents |  |
| --- | --- |
| Matrix structure | Acrylic |
| Classification | Nonionic Spherical |
| Specific surface area (m²/g) | 500 |
| Pore ​​volume (cm³/g) | 0.6 |
| Pore diameter (Å) | 100 |
| Apparent density (g/L) | ~655 |
| Moisture holding capacity (%) | 61-69 |
| Harmonic mean diameter (mm) | 0.43 - 0.69 |
| Uniformity coefficient | ≦ 2.0 |
| Effective pH range | 0-14 |
| Polarity | Intermediate polarity |

Figure S1. (a) The chemical structure of XAD and (b) cluster model of XAD surface.

Figure S2. The relationship between impregnated amounts of 1 into XAD-7 and Pd(II) quantity adsorbed by 1-EIR. Adsorption condition: [HCl] = 0.1~8.0 M, [Pd(II)] = 100 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 24 h.

Figure S3. Effect of shaking time for Pd(II) adsorption capability of 1-EIR. Sorption condition: [HCl] = 0.1 M, [Pd(II)] = 100 ppm (= mg L−1) , 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 0 ~ 240 min.

Figure S4. Photographs a) before and b) after Pd(II) adsorption by 1-EIR.

Figure S5. Nitrogen isotherms of XAD-7 (red circle) and 1-EIR (blue circle).

Figure S6. Brunauer-Emmett-Teller (BET) plots and the sorption parameters of a) XAD-7 and b) 1-EIR.

Figure S7.  Pore size distribution of XAD-7 (red circle) and 1-EIR (blue circle) by Dollimore-Heal (DH) method.

Figure S8. The sizes of a PdCl42- species and a CH4N2S molecule.

Figure S9. Photographs a) before and b) after Soxhlet extraction of residual Pd(II) in 1-EIR.

Figure S10. Full scan X-ray photoelectron spectroscopy (XPS) after Soxhlet extraction from the undesorbed Pd(II) in 1-EIR.

Figure S11. 1H NMR spectra of the Pd(II)–extractant 1 complex flaked from Pd(II)-loaded 1-EIR.

Figure S12. a) Freundlich and b) Langmuir isotherms for Pd(II) sorption by 1-EIR. Sorption conditions: 1-EIR = 0.1 g, [HCl] = 0.1 M; [Pd(II)] = 500–700 ppm (= mg L−1); temperature = 293–313 K; shaking time = 24 h; shaking speed = 80 rpm.

Figure S13. Van’t Hoff plot relating ln K0 against 1/T for Pd(II) sorption by 1-EIR. Sorption conditions: 1-EIR = 0.1 g, [HCl] = 0.1 M; [Pd(II)] = 500–700 ppm (= mg L−1); temperature = 293–313 K; shaking time = 24 h; shaking speed = 80 rpm.

Figure S14. Pseudo-first-order for Pd(II) sorption by 1-EIR. Sorption condition: [HCl] = 0.1 M, [Pd(II)] = 600 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 0.5~12 h.

Figure S15.  Pseudo-second-order for Pd(II) sorption by 1-EIR. Sorption condition: [HCl] = 0.1 M, [Pd(II)] = 600 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 0.5~12 h.

Figure S16. Particle diffusion for Pd(II) sorption by 1-EIR. Sorption condition: [HCl] = 0.1 M, [Pd(II)] = 600 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 0.5~12 h.

.

Figure S17. Intraparticle diffusion for Pd(II) sorption by 1-EIR. Sorption condition: [HCl] = 0.1 M, [Pd(II)] = 600 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 0.5~12 h.

Table S2. Application of kinetic models to the sorption of Pd(II) ions onto 1-EIR at r.t.

| Kinetic models | Parameters | Pd(II) = 600 ppm 1-EIR |
| --- | --- | --- |
| Pseudo-first-order | kad (min-1) | 5.0E -4 |
|  | r | 0.8650 |
| Pseudo-second-order | qe (mg/g) | 25.00 |
|  | k (g/mg min) | 3.163E -4 |
|  | h (mg/g min) | 0.2164 |
|  | r | 0.9985 |
| Particle diffusion | kp (mg/g min) | 5.9E -3 |
|  | r | 0.9999 |
| Intraparticle diffusion | ki (mg/g min0.5) | 0.8773 |
|  | r | 0.9938 |

Figure S18. Selective Pd(II) sorption of 1-EIR from a simulated 13 metals containing HCl solution. Sorption condition: [HCl] = 0.1 M, [Metals] = each 100 ppm (= mg L−1), 1-EIR = 0.1 g, shaking speed = 280 rpm, shaking time = 3 h.

Table S3. Metal species and metal concentration in the leachate of automotive catalyst

| Metal ions | [M]aq,init (mg/L) |
| --- | --- |
| Pd(II) Pt(IV) Rh(III) La(III) Ce(III) Y(III) Zr(IV) Ba(II) Al(III) Fe(III) | 111.4 53.6 41.4 84.4 569.1 4.0 19.8 307.7 291.5 7.7 |