# Supplementary Materials

Figure S1: A detailed view of the in vivo microelectrode array showing dimensions and spacing of the electrodes

150µm

Table S1. Comparison of the three-dimensional in vivo microelectrodes developed in this work to other works

|  | Clinical ECoG* [1] | Xiang et al. [2] | This Work |
| --- | --- | --- | --- |
| Substrate | Silicone (Silastic™) | Polyimide | Polyimide |
| Metallization | Pt, stainless steel | Cr/Au | ENIG, ENEPIG |
| Electrode Pad | 3-5mm (diameter) | 500µm x300µm (rectangular) | 150µm (diameter) |
| Electrode Tip Diameter | N/A | 80-200µm | 17 or 25µm |
| Electrode Height | N/A (planar) | 500-2250µm | 300µm |
| Electrode Spacing | 5mm | 0.8mm | 0.35mm (in vivo) |

*Ad-Tech 4-channel strip (Catalog# IS04R-SP10X-000)

[1] V. Palys, “Intracranial Electrodes (icEEG),” Viktor's notes for the neurosurgery resident, 13-Jan-2021.

[2] Z. Xiang et al., “A flexible three-dimensional electrode mesh: An enabling technology for wireless brain–computer interface prostheses,” Microsystems & Nanoengineering, vol. 2, no. 1, May 2016.

Supplementary Video: A video of a brain slice recording using the gold three-dimensional electrodes can be seen at the following link: link to be provided for journal readers.