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[bookmark: _Toc36340320]Supplementary Fig. 1| Dimensions of moulds. a, Dimensions of type A mould and b, Dimensions of type B mould in mm
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Supplementary Fig. 2|Inoculated sawdust bags. a, before growth and b, after growth
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Supplementary Fig. 3|Dried Mycelium blocks
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Supplementary Fig. 4|Production of DMC under heat and pressure.
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Supplementary Fig. 5|Sample under 4-point bending test


Supplementary Note 2
Supplementary Tables. 
Supplementary Table 1|Rb raw data and ANOVA results
	[bookmark: _Hlk72479660]Rb raw data
	 
	 
	 
	 

	
	Day 0
	Day 7
	Day 21
	Day 35

	Uncoated group
	2.07
	2.27
	1.26
	1.11

	
	2.76
	2.76
	1.80
	1.01

	
	3.21
	2.27
	2.12
	1.19

	Coated group
	1.45
	1.74
	1.50
	1.22

	
	2.75
	2.71
	2.04
	1.85

	
	3.39
	2.53
	2.23
	1.79

	ANOVA
	
	
	
	

	Source of Variation
	df
	F
	P-value
	

	
	
	
	
	

	Between groups
	1
	0.30
	0.59
	

	
	
	
	
	



Supplementary Table 2|Rc raw data and ANOVA results
	Rc raw data
	 
	 
	 
	 

	
	Day 0
	Day 7
	Day 21
	Day 35

	Uncoated group
	2.68
	1.28
	2.55
	0.62

	
	7.61
	2.15
	1.65
	0.50

	
	3.04
	3.33
	1.66
	1.01

	Coated group
	2.96
	1.31
	1.52
	1.49

	
	4.89
	2.94
	2.26
	3.59

	
	2.24
	2.06
	2.38
	1.55

	ANOVA
	
	
	
	

	Source of Variation
	df
	F
	P-value
	

	Between groups
	1
	0.03
	0.86
	








Supplementary Table 3|Rt raw data and ANOVA results
	Rt raw data
	 
	 
	 
	 

	
	Day 0
	Day 7
	Day 21
	Day 35

	Uncoated group
	1.90
	0.39
	0.70
	0.47

	
	1.03
	0.80
	0.58
	0.28

	
	1.72
	0.63
	0.33
	0.22

	Coated group
	1.35
	0.81
	1.00
	0.78

	
	1.91
	1.06
	0.92
	0.82

	
	1.33
	0.46
	0.68
	0.82

	ANOVA
	
	
	
	

	Source of Variation
	df
	F
	P-value
	

	Between groups
	1
	5.22
	0.04
	



	Et raw data
	 
	 
	 
	 

	
	Day 0
	Day 7
	Day 21
	Day 35

	Uncoated group
	872.95
	49.86
	127.70
	163.46

	
	536.67
	213.64
	84.51
	100.47

	
	530.79
	136.31
	20.47
	84.42

	Coated group
	485.11
	293.20
	190.96
	281.15

	
	696.95
	521.76
	386.14
	388.43

	
	624.64
	40.15
	168.42
	188.60

	ANOVA
	
	
	
	

	Source of Variation
	df
	F
	P-value
	

	Between groups
	1
	4.19
	0.06
	


 Supplementary Table 4|Et raw data and ANOVA results
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