Spent coffee ground characterization, pelletization test and emissions assessment in the combustion process

Colantoni, A.1*,Paris, E.2,Bianchini, L.1*,Ferri, S.1, Marcantonio, V.1, Carnevale, M.1, Palma, A.2, Civitarese, V.2,Gallucci, F.2

1	Tuscia University – Department of Agriculture and Forestry Science (UNITUS-DAFNE); *l.bianchini@unitus.it

2	Consiglio per la ricerca in agricoltura e l’analisi dell’economia agraria (CREA) – Centro di ricerca Ingegneria e Trasformazioni agroalimentari (CREA-IT);

Highlights

- A study was conducted on the re-use of coffee grounds as an energy source.

- Spent coffee grounds can be employed as pellet to obtain high-value products.

- The biomass combustion products have been evaluated experimentally.

- Simulative combustion model was developed with Aspen Plus.

*Corresponding author: colantoni@unitus.it, Tuscia University, +39 0761357356

Abstract

Industrial development and increased energy requirements have led to high consumption of fossil fuels. Thus, environmental pollution has become a profound problem. Every year, a large amount of agro-industrial, municipal and forest residues are treated as waste, but they can be recovered and used to produce thermal and electrical energy through biological or thermochemical conversion processes. Among the main types of agro-industrial waste, soluble coffee residues represent a significant quantity all over the world. Silver coffee peel and spent coffee grounds are the main residues of the coffee industry. The many organic compounds contained in coffee residues motivate their enhancement. Thanks to its composition it can be used in the production of biodiesel, as a source of sugar, as a precursor for the creation of active carbon or it can be used as a sorbent for the removal of metals. After a careful evaluation of the possible use of coffee grounds, the aim of this work was to show a broad characterization of coffee waste for energy purposes, through physical and chemical analyses that highlighted the most significant quality indexes, the interactions between them and the quantification of their importance. This study provides results that are important tools for the qualification and quantification of the effects of coffee waste properties on energy production processes. It shows that SCGs are an excellent raw material as biomass, showing excellent values in terms of calorific value and low ash content that have allowed the obtainment of 98% coffee pellets excellent for use in thermal conversion systems.Combustion tests were also carried out in an 80kWth boiler and the emissions produced, without any type of abatement filter, were characterized.

List of abbreviations

SCG		Spent coffee grounds

HHV		Higher Heating Value

LHV		Lower Heating Value

ACF		Activated Carbon Fibers

FID		Flame Ionization Detector

BTEX 		Benzene Toluene Ethylbenzene Xylenes

TOC		Total Organic Carbon

VOCs		Volatile OrganicCompounds

PM		Particulate Matter

ANOVA 	Analysis Of Variance

%		Percentage

°C		Degrees Celsius

kg		Kilogram

ml		Millilitre

ppm		Part per million

ppb		Parts per billion

MJ/kg		Megajoules per kilogram

mg/Nm3	Milligrams per normal cubic metre

mg/kg		Milligrams per kilogram

LoQ		Limit Of Quantification

Ag		Silver

Al		Aluminium

As		Arsenic

B		Boron

Ba		Barium

Be		Beryllium

C		Carbon

Ca		Calcium

Cd		Cadmium

Cl		Chlorine

Co		Cobalt

Cr		Chromium

Cs		Caesium

Cu		Copper

Fe		Iron

Ga		Gallium

Ge		Germanium

H		Hydrogen

In		Indium

K		Potassium

Li		Lithium

Mg		Magnesium

Mn		Manganese

N		Nitrogen

Na		Sodium

Ni		Nickel

O		Oxygen

Pb		Lead

S		Sulphur

Sb		Antimony

Sc		Scandium

Se		Selenium

Sn		Tin

Sr		Strontium

Ti		Titanium

Tl		Thallium

Zn		Zinc

CO		Carbon monoxide

NOx		Nitrogen oxides

CO2		Carbon dioxide

SO2		Sulfur dioxide

HNO3		Nitric acid

H2O2		Hydrogen peroxide

CH4		Methane

H2O		Water

NH3		Ammonia

O2r		Percentage of reference oxygen content

O2m		Percentage of oxygen measured

Cm		Concentation of anlite measured