Supplementary material

Catalytic hydrotreating of bio-oil and evaluation of main noxious emissions of gaseous phase

Rami Doukeh1, Dorin Bombos1, Mihaela Bombos2, Elena-Emilia Oprescu1,2, Gheorghe Dumitrascu3¸ Vasilievici Gabriel2, Catalina Calin1*

1Chemistry Department, Petroleum-Gas University of Ploiesti, 39 Bucuresti Blvd., 100680, Ploiesti, Romania

2National Institute for Research and Development for Chemistry and Petrochemistry ICECHIM Bucuresti, 202 Splaiul Independentei, 060021, Bucharest, Romania

3Department of Engineering Thermodynamics, ‘‘Gh. Asachi’’ Technical University of Iasi, Bd. D. Mangeron, 59-61,6600 Iasi, Romania

Correspondence to: catalina.calin20@yahoo.com; catalina.calin@upg-ploiesti.ro; oprescuemilia@gmail.com

Number of pages: 2

Number of figures: 1

Number of tables : 1

Table S1. Chemical composition of pyrolysis bio-oil

| Peak Number | Retention time | Area Sum % |
| --- | --- | --- |
| Ethyl levulinate | 5.903 | 3.24 |
| Phenol, 4-methyl | 6.103 | 0.85 |
| Phenol, 2-methoxy | 6.286 | 0.88 |
| Tetradecane | 10.531 | 0.96 |
| Naphtalene, 1,3-dimethyl | 11.002 | 1.5 |
| Benzil alcohol, α-isobutyl, 3,4,6-trimethyl | 11.816 | 5.89 |
| Naphtalene, 2,3,6-trimethyl | 12.789 | 6.8 |
| Hexadecane | 13.044 | 7.97 |
| Naphtalene, 1,6,7-trimethyl | 13.116 | 3.29 |
| Tetradecane, 2,6,10-trimethyl | 13.571 | 4.22 |
| Heptadecan | 14.217 | 19.22 |
| Octadecane | 15.31 | 11.92 |
| Octadecane, 3-ethyl-5-(2-ethylbutyl) | 15.366 | 3.97 |
| Nonadecane | 16.356 | 11.13 |
| Heneicosane | 17.337 | 3.52 |
| Heptacosane | 18.295 | 3.71 |
| 1-hexadecanol, 2 -mehtyl | 19.204 | 0.73 |
| Other small compounds | - | 10.20 |

Figure S1. TPD-pyridine profile of the CoMo/γ-Al2O3-HMS catalyst