Supplementary Information

Article Title: 3D printing fluorescent material with tunable optical properties

Authors: Alberto J. Ruiz1,2, Sadhya Garg1, Samuel Streeter1, Mia K. Giallorenzi1, Ethan P.M. LaRochelle2, Kimberley S. Samkoe1, Brian W. Pogue1,2

1Thayer School of Engineering at Dartmouth, Hanover NH 03755

2QUEL Imaging LLC, White River Junction VT 05001

Supplementary Fig. 1 Manufacturing steps and respective considerations for the presented 3D printing methodology. Pre-dispersed solutions of the fluorophores, absorbers, and scatterers are integrated into the resin to generate 3D printed fluorescent structures with tuned optical absorption and reduced scattering properties.

Supplementary Fig. 2 3DP cuvettes used for optical characterization a Visualization of “yellowing” associated with increased post-curing time on 3DP solid cuvettes (eSun clear resin). b Polished and unpolished 3DP cuvettes. Polishing enables spectral measurements of the printed material.

Supplementary Fig. 3 Spectral shifts of IR-125 laser dye in three commercially available resins. a normalized absorbance spectra b normalized fluorescence emission spectra. Optical measurements were performed on 3DP cuvettes with an IR-125 dye concentration of 1000nM.

Supplementary Fig. 4 Spectral comparison of IR-125 doped uncured resin and 3D printed material using three commercially available resins. a,b eSun Standard Clear resin. c,d 3DM Tough resin.  e,f , NextGen 3Dresyn TD90. Optical measurements were performed on 3DP cuvettes with an IR-125 dye concentration of 1000nM.

Supplementary Fig. 5 Photostability measurements performed over two months on IR-125 and quantum dot doped 3DP material. a First 16 days of measurements  b 64 days of photostability measurements. The measured standard deviation for the each timepoint is 1-2%; error bars are omitted for visual clarity.