Supplementary Information

Oxidative coupling of methane—Comparisons of MnTiO3-Na2WO4 and MnOx-TiO2-Na2WO4 catalysts on different silica supports

Worapinit Tiyatha1,2, Thanaphat Chukeaw1,2, Sarannuch Sringam1,2, Thongthai Witoon1,2,3, Metta Chareonpanich1,2,3, Günther Rupprechter4, Anusorn Seubsai1,2,3*

1 Department of Chemical Engineering, Faculty of Engineering, Kasetsart University, Bangkok 10900, Thailand

2 Center of Excellence on Petrochemical and Materials Technology, Kasetsart University, Bangkok 10900, Thailand

3 Research Network of NANOTEC–KU on NanoCatalysts and NanoMaterials for Sustainable Energy and Environment, Kasetsart University, Bangkok 10900, Thailand

4 Institute of Materials Chemistry, TU Wien, 1060 Vienna, Austria

*Corresponding author: fengasn@ku.ac.th

Supplementary Figure S1 Activity in OCM reaction: a) MnTiO3-NW/CS, b) MnTiO3-NW/SG, and c) Mn-Ti-NW/SG catalysts. Testing conditions: 50 mg catalyst, gas feed of CH4:O2:N2 = 3:1:4, reactor temperature = 700 °C, atmospheric pressure, total gas flow rate = 50 mL min-1 (GHSV = 30,588 h-1).

Supplementary Table S1 Characteristic XRD values (2θ) crystalline phases found in different catalysts.

| Catalyst | Crystalline phase | 2θ (degree) | ICDD No. |
| --- | --- | --- | --- |
| NW/CS | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |
| 5MnTiO3-NW/CS | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | Manganese oxide (Mn2O3) | 21.101, 32.930, 38.171, 55.110 | 01-071-0635 |
|  | Manganese oxide (Mn3O4) | 31.138, 32.533, 36.191, 38.101, 44.600 | 00-001-1127 |
|  | Rutile (TiO2) | 27.436, 36.080, 41.240, 54.321, 56.759 | 01-075-1753 |
|  | Manganese titanium oxide (MnTiO3) | 41.385, 48.104, 52.262, 55.368 | 00-002-0846 |
|  | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |
| 20MnTiO3-NW/CS | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | Manganese oxide (Mn2O3) | 21.101, 32.930, 38.171, 55.110 | 01-071-0635 |
|  | Manganese oxide (Mn3O4) | 31.138, 32.533, 36.191, 38.101, 44.600 | 00-001-1127 |
|  | Rutile (TiO2) | 27.436, 36.080, 41.240, 54.321, 56.759 | 01-075-1753 |
|  | Manganese titanium oxide (MnTiO3) | 41.385, 48.104, 52.262, 55.368 | 00-002-0846 |
|  | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |
| NW/SG | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |
| 10MnTiO3-NW/SG | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | Manganese oxide (Mn2O3) | 21.101, 32.930, 38.171, 55.110 | 01-071-0635 |
|  | Manganese oxide (Mn3O4) | 31.138, 32.533, 36.191, 38.101, 44.600 | 00-001-1127 |
|  | Rutile (TiO2) | 27.436, 36.080, 41.240, 54.321, 56.759 | 01-075-1753 |
|  | Manganese titanium oxide (MnTiO3) | 41.385, 48.104, 52.262, 55.368 | 00-002-0846 |
|  | Quartz (SiO2) | 20.861, 26.642, 50.145 | 01-075-0443 |

Supplementary Table S1 Characteristic XRD values (2θ) crystalline phases found in different catalysts. (Continued)

| Catalyst | Crystalline phase | 2θ (degree) | ICDD No. |
| --- | --- | --- | --- |
| 10MnTiO3-NW/SG | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |
| 20MnTiO3-NW/SG | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | Manganese oxide (Mn2O3) | 21.101, 32.930, 38.171, 55.110 | 01-071-0635 |
|  | Manganese oxide (Mn3O4) | 31.138, 32.533, 36.191, 38.101, 44.600 | 00-001-1127 |
|  | Rutile (TiO2) | 27.436, 36.080, 41.240, 54.321, 56.759 | 01-075-1753 |
|  | Manganese titanium oxide (MnTiO3) | 41.385, 48.104, 52.262, 55.368 | 00-002-0846 |
|  | Quartz (SiO2) | 20.861, 26.642, 50.145 | 01-075-0443 |
|  | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |
| 5Mn-Ti-NW/SG | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | Manganese oxide (Mn2O3) | 21.101, 32.930, 38.171, 55.110 | 01-071-0635 |
|  | Manganese oxide (Mn3O4) | 31.138, 32.533, 36.191, 38.101, 44.600 | 00-001-1127 |
|  | Rutile (TiO2) | 27.436, 36.080, 41.240, 54.321, 56.759 | 01-075-1753 |
|  | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |
| 20Mn-Ti-NW/SG | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | Manganese oxide (Mn2O3) | 21.101, 32.930, 38.171, 55.110 | 01-071-0635 |
|  | Manganese oxide (Mn3O4) | 31.138, 32.533, 36.191, 38.101, 44.600 | 00-001-1127 |
|  | Rutile (TiO2) | 27.436, 36.080, 41.240, 54.321, 56.759 | 01-075-1753 |
|  | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |
| Used MnTiO3-NW/CS | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | Manganese oxide (Mn2O3) | 21.101, 32.930, 38.171, 55.110 | 01-071-0635 |
|  | Manganese oxide (Mn3O4) | 31.138, 32.533, 36.191, 38.101, 44.600 | 00-001-1127 |
|  | Rutile (TiO2) | 27.436, 36.080, 41.240, 54.321, 56.759 | 01-075-1753 |
|  | Manganese titanium oxide (MnTiO3) | 41.385, 48.104, 52.262, 55.368 | 00-002-0846 |
|  | Quartz (SiO2) | 20.861, 26.642, 50.145 | 01-075-0443 |
|  | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |

Supplementary Table S1 Characteristic XRD values (2θ) crystalline phases found in different catalysts. (Continued)

| Catalyst | Crystalline phase | 2θ (degree) | ICDD No. |
| --- | --- | --- | --- |
| Used MnTiO3-NW/SG | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | Manganese oxide (Mn2O3) | 21.101, 32.930, 38.171, 55.110 | 01-071-0635 |
|  | Manganese oxide (Mn3O4) | 31.138, 32.533, 36.191, 38.101, 44.600 | 00-001-1127 |
|  | Rutile (TiO2) | 27.436, 36.080, 41.240, 54.321, 56.759 | 01-075-1753 |
|  | Manganese titanium oxide (MnTiO3) | 41.385, 48.104, 52.262, 55.368 | 00-002-0846 |
|  | Quartz (SiO2) | 20.861, 26.642, 50.145 | 01-075-0443 |
|  | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |
| Used Mn-Ti-NW/SG | Sodium tungsten oxide (Na2WO4) | 16.806, 27.612, 32.499, 48.828, 52.004, 57.015 | 01-074-2369 |
|  | α-cristobalite (SiO2) | 21.947, 28.401, 31.375, 36.056 | 01-071-0785 |
|  | Manganese oxide (Mn2O3) | 21.101, 32.930, 38.171, 55.110 | 01-071-0635 |
|  | Manganese oxide (Mn3O4) | 31.138, 32.533, 36.191, 38.101, 44.600 | 00-001-1127 |
|  | Rutile (TiO2) | 27.436, 36.080, 41.240, 54.321, 56.759 | 01-075-1753 |
|  | α-tridymite (SiO2) | 23.440, 24.443, 29.625, 30.064, 35.853 | 01-086-0681 |

Supplementary Figure S2 XRD patterns of catalysts.

Supplementary Figure S3 The average particle size of CS.

Supplementary Table S2 The average particle size of CS.

| No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.032 | 11 | 0.027 | 21 | 0.030 | 31 | 0.031 | 41 | 0.028 |
| 2 | 0.060 | 12 | 0.033 | 22 | 0.040 | 32 | 0.037 | 42 | 0.037 |
| 3 | 0.039 | 13 | 0.035 | 23 | 0.040 | 33 | 0.023 | 43 | 0.027 |
| 4 | 0.041 | 14 | 0.033 | 24 | 0.033 | 34 | 0.028 | 44 | 0.029 |
| 5 | 0.044 | 15 | 0.030 | 25 | 0.029 | 35 | 0.032 | 45 | 0.032 |
| 6 | 0.036 | 16 | 0.031 | 26 | 0.043 | 36 | 0.038 | 46 | 0.034 |
| 7 | 0.033 | 17 | 0.048 | 27 | 0.027 | 37 | 0.033 | 47 | 0.033 |
| 8 | 0.028 | 18 | 0.038 | 28 | 0.038 | 38 | 0.032 | 48 | 0.030 |
| 9 | 0.038 | 19 | 0.031 | 29 | 0.033 | 39 | 0.015 | 49 | 0.030 |
| 10 | 0.035 | 20 | 0.036 | 30 | 0.039 | 40 | 0.025 | 50 | 0.030 |
|  |  |  |  |  |  |  |  | Avg. | 0.034 |

Supplementary Figure S4 The average particle size of NW/CS.

Supplementary Table S3 The average particle size of NW/CS.

| No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.240 | 11 | 0.380 | 21 | 0.244 | 31 | 0.370 | 41 | 0.227 |
| 2 | 0.368 | 12 | 0.290 | 22 | 0.334 | 32 | 0.379 | 42 | 0.230 |
| 3 | 0.156 | 13 | 0.173 | 23 | 0.360 | 33 | 0.341 | 43 | 0.420 |
| 4 | 0.198 | 14 | 0.269 | 24 | 0.279 | 34 | 0.413 | 44 | 0.424 |
| 5 | 0.176 | 15 | 0.230 | 25 | 0.337 | 35 | 0.244 | 45 | 0.234 |
| 6 | 0.348 | 16 | 0.394 | 26 | 0.335 | 36 | 0.325 | Avg. | 0.312 |
| 7 | 0.373 | 17 | 0.283 | 27 | 0.308 | 37 | 0.433 |
| 8 | 0.201 | 18 | 0.317 | 28 | 0.325 | 38 | 0.309 |
| 9 | 0.301 | 19 | 0.367 | 29 | 0.332 | 39 | 0.357 |
| 10 | 0.289 | 20 | 0.362 | 30 | 0.393 | 40 | 0.397 |

Supplementary Figure S5 The average particle size of 5MnTiO3-NW/CS.

Supplementary Table S4 The average particle size of 5MnTiO3-NW/CS.

| No. | Length (μm) | No. | Length (μm) | No. | Length (μm) |
| --- | --- | --- | --- | --- | --- |
| 1 | 0.336 | 11 | 0.538 | 21 | 0.449 |
| 2 | 0.440 | 12 | 0.725 | 22 | 0.303 |
| 3 | 0.550 | 13 | 0.682 | 23 | 0.405 |
| 4 | 0.713 | 14 | 0.383 | 24 | 0.372 |
| 5 | 0.640 | 15 | 0.425 | 25 | 0.345 |
| 6 | 0.372 | 16 | 0.787 | 26 | 0.490 |
| 7 | 0.424 | 17 | 0.806 | 27 | 0.566 |
| 8 | 0.442 | 18 | 0.301 | 28 | 0.254 |
| 9 | 0.516 | 19 | 0.721 | 29 | 0.429 |
| 10 | 0.518 | 20 | 0.604 | 30 | 0.383 |
|  |  |  |  | Avg. | 0.497 |

Supplementary Figure S6 The average particle size of 20MnTiO3-NW/CS.

Supplementary Table S5 The average particle size of 20MnTiO3-NW/CS.

| No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.281 | 11 | 0.430 | 21 | 0.666 | 31 | 0.294 |
| 2 | 0.324 | 12 | 0.475 | 22 | 0.362 | 32 | 0.267 |
| 3 | 0.212 | 13 | 0.308 | 23 | 0.186 | 33 | 0.242 |
| 4 | 0.270 | 14 | 0.184 | 24 | 0.325 | 34 | 0.305 |
| 5 | 0.394 | 15 | 0.266 | 25 | 0.466 | 35 | 0.318 |
| 6 | 0.441 | 16 | 0.526 | 26 | 0.310 | Avg. | 0.324 |
| 7 | 0.299 | 17 | 0.278 | 27 | 0.236 |
| 8 | 0.226 | 18 | 0.186 | 28 | 0.336 |
| 9 | 0.408 | 19 | 0.138 | 29 | 0.266 |
| 10 | 0.391 | 20 | 0.433 | 30 | 0.288 |

Supplementary Figure S7 The average particle size of SG.

Supplementary Table S6 The average particle size of SG.

| No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.426 | 6 | 0.579 | 11 | 0.296 | 16 | 0.311 | 21 | 0.591 |
| 2 | 0.430 | 7 | 0.245 | 12 | 0.288 | 17 | 0.383 | 22 | 0.477 |
| 3 | 0.434 | 8 | 0.262 | 13 | 0.310 | 18 | 0.385 | 23 | 0.493 |
| 4 | 0.416 | 9 | 0.401 | 14 | 0.323 | 19 | 0.395 | 24 | 0.470 |
| 5 | 0.379 | 10 | 0.317 | 15 | 0.284 | 20 | 0.551 | 25 | 0.553 |
|  |  |  |  |  |  |  |  | Avg. | 0.400 |

Supplementary Figure S8 The average particle size of NW/SG.

Supplementary Table S7 The average particle size of NW/SG.

| No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.260 | 11 | 0.416 | 21 | 0.211 | 31 | 0.228 |
| 2 | 0.276 | 12 | 0.599 | 22 | 0.521 | 32 | 0.258 |
| 3 | 0.315 | 13 | 0.605 | 23 | 0.356 | 33 | 0.305 |
| 4 | 0.255 | 14 | 0.564 | 24 | 0.282 | 34 | 0.641 |
| 5 | 0.267 | 15 | 0.234 | 25 | 0.480 | 35 | 0.140 |
| 6 | 0.239 | 16 | 0.308 | 26 | 0.680 | Avg. | 0.392 |
| 7 | 0.220 | 17 | 0.545 | 27 | 0.668 |
| 8 | 0.228 | 18 | 0.310 | 28 | 0.449 |
| 9 | 0.216 | 19 | 0.623 | 29 | 0.667 |
| 10 | 0.331 | 20 | 0.542 | 30 | 0.469 |

Supplementary Figure S9 The average particle size of 10MnTiO3-NW/SG.

Supplementary Table S8 The average particle size of 10MnTiO3-NW/SG.

| No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.323 | 11 | 0.336 | 21 | 0.489 | 31 | 1.234 |
| 2 | 0.328 | 12 | 0.261 | 22 | 0.674 | Avg. | 0.469 |
| 3 | 0.314 | 13 | 0.226 | 23 | 0.633 |
| 4 | 0.351 | 14 | 0.267 | 24 | 0.785 |
| 5 | 0.341 | 15 | 0.300 | 25 | 0.436 |
| 6 | 0.344 | 16 | 0.440 | 26 | 0.693 |
| 7 | 0.432 | 17 | 0.221 | 27 | 0.505 |
| 8 | 0.319 | 18 | 0.375 | 28 | 0.449 |
| 9 | 0.412 | 19 | 0.342 | 29 | 0.728 |
| 10 | 0.316 | 20 | 0.553 | 30 | 1.107 |

Supplementary Figure S10 The average particle size of 20MnTiO3-NW/SG.

Supplementary Table S9 The average particle size of 20MnTiO3-NW/SG.

| No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.439 | 11 | 0.484 | 21 | 0.682 | 31 | 0.685 |
| 2 | 0.512 | 12 | 0.530 | 22 | 0.438 | 32 | 0.511 |
| 3 | 0.366 | 13 | 0.502 | 23 | 0.493 | 33 | 0.677 |
| 4 | 0.489 | 14 | 0.440 | 24 | 0.448 | 34 | 0.412 |
| 5 | 0.289 | 15 | 0.529 | 25 | 0.472 | 35 | 0.765 |
| 6 | 0.354 | 16 | 0.595 | 26 | 0.511 | 36 | 0.795 |
| 7 | 0.570 | 17 | 0.635 | 27 | 0.439 | 37 | 0.786 |
| 8 | 0.513 | 18 | 0.634 | 28 | 0.327 | Avg. | 0.506 |
| 9 | 0.403 | 19 | 0.490 | 29 | 0.350 |
| 10 | 0.337 | 20 | 0.531 | 30 | 0.306 |

Supplementary Figure S11 The average particle size of 5Mn-Ti-NW/SG.

Supplementary Table S10 The average particle size of 5Mn-Ti-NW/SG.

| No. | Length (μm) | No. | Length (μm) | No. | Length (μm) | No. | Length (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.418 | 11 | 0.714 | 21 | 0.444 | 31 | 0.657 |
| 2 | 0.503 | 12 | 0.467 | 22 | 0.452 | 32 | 0.403 |
| 3 | 0.589 | 13 | 0.524 | 23 | 0.758 | 33 | 0.368 |
| 4 | 0.440 | 14 | 0.756 | 24 | 0.735 | Avg. | 0.500 |
| 5 | 0.557 | 15 | 0.340 | 25 | 0.400 |
| 6 | 0.371 | 16 | 0.384 | 26 | 0.451 |
| 7 | 0.288 | 17 | 0.407 | 27 | 0.468 |
| 8 | 0.461 | 18 | 0.391 | 28 | 0.442 |
| 9 | 0.387 | 19 | 0.527 | 29 | 0.753 |
| 10 | 0.500 | 20 | 0.464 | 30 | 0.682 |

Supplementary Figure S12 The average particle size of 20Mn-Ti-NW/SG.

Supplementary Table S11 The average particle size of 20Mn-Ti-NW/SG.

| No. | Length (μm) | No. | Length (μm) | No. | Length (μm) |
| --- | --- | --- | --- | --- | --- |
| 1 | 0.433 | 9 | 0.720 | 17 | 0.810 |
| 2 | 0.479 | 10 | 0.694 | 18 | 0.882 |
| 3 | 0.492 | 11 | 0.349 | 19 | 1.193 |
| 4 | 0.387 | 12 | 0.720 | 20 | 0.401 |
| 5 | 0.291 | 13 | 0.605 | 21 | 0.239 |
| 6 | 0.439 | 14 | 0.685 | 22 | 0.937 |
| 7 | 0.305 | 15 | 0.767 | Avg. | 0.585 |
| 8 | 0.374 | 16 | 0.679 |

Supplementary Figure S13 Plots of N2-physisorption at standard temperature and pressure (STP): a) CS and SG, b) MnTiO3-NW/CS, c) MnTiO3-NW/SG, and d) Mn-Ti-NW/SG catalysts. Each inset shows the corresponding pore size distribution plot.

Supplementary Table S12 FE-SEM and EDX images of catalysts.

| Catalyst | SEM | EDX and weight percent elemental |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Mn | Ti | Na | W | Si |
| NW/CS |  |  |  | 0.30% | 2.80% | 39.34% |
| 5MnTiO3-NW/CS |  | 0.01% | 0.01% | 0.10% | 2.15% | 45.46% |
| 20MnTiO3-NW/CS |  | 0.34% | 0.28% | 0.14% | 3.11% | 27.81% |
| NW/SG |  |  |  | 0.01% | 2.17% | 27.81% |

Supplementary Table S12 FE-SEM and EDX images of catalysts. (Continued)

| Catalyst | SEM | EDX and weight percent elemental |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Mn | Ti | Na | W | Si |
| 10MnTiO3-NW/SG |  | 1.59% | 0.52% | 0.02% | 1.89% | 39.72% |
| 20MnTiO3-NW/SG |  | 1.56% | 0.93% | 0.15% | 0.01% | 25.84% |
| 5Mn-Ti-NW/SG |  | 1.23% | 0.01% | 0.01% | 1.22% | 19.79% |
| 20Mn-Ti-NW/SG |  | 2.81% | 0.01% | 0.53% | 2.81% | 28.15% |

Supplementary Table S12 FE-SEM and EDX images of catalysts. (Continued)

| Catalyst | SEM | EDX and weight percent elemental |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Mn | Ti | Na | W | Si |
| Used MnTiO3-NW/CS |  | 0.15% | 0.16% | 0.23% | 1.66% | 35.15% |
| Used MnTiO3-NW/SG |  | 0.01% | 0.01% | 0.30% | 1.44% | 24.64% |
| Used Mn-Ti-NW/SG |  | 4.26% | 0.01% | 0.30% | 1.96% | 24.44% |

Supplementary Figure S14  FTIR spectra of CS, Na/CS, NW/CS, and MnTiO3-NW/CS.

Supplementary Table S13 Observed XPS binding energies of Na 1s, W 4f, Si 2p, Ti 2p, and Mn 2p.

| Catalyst | Binding energy (eV) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Na 1s | W 4f |  | Si 2p | Mn 2p |  | Ti 2p |  |
|  |  | 4f5/2 | 4f7/2 |  | 2p1/2 | 2p3/2 | 2p1/2 | 2p3/2 |
| NW/CS | 1071.3 | 37.6 | 35.4 | 103.5 | - | - | - | - |
| MnTiO3-NW/CS | 1071.3 | 37.6 | 35.4 | 103.4 | 655.4, 654.1, 652.8 | 643.9, 642.4, 641.3 | 464.74 | 459.1 |
| NW/SG | 1071.6 | 37.8 | 35.7 | 103.7 | - | - | - | - |
| MnTiO3-NW/SG | 1071.6 | 37.8 | 35.7 | 103.1 | 655.7, 654.1, 652.8 | 644.9, 642.1, 641.4 | 464.8 | 459.2 |
| Mn-Ti-NW/SG | 1071.3 | 37.6 | 35.5 | 103.4 | 655.1, 654.0, 652.8 | 643.3, 642.4, 641.4 | 464.0 | 458.5 |

Supplementary Figure S15 XPS Na 1s spectra of catalysts.

Supplementary Figure S16 XPS W 4f spectra of catalysts.

Supplementary Figure S17 XPS Si 2p spectra of catalysts.

Supplementary Figure S18 XPS Mn 2p spectra of catalysts.

Supplementary Figure S19 XPS Ti 2p spectra of the catalysts.

Supplementary Figure S20 Catalytic performance of Mn-Ti-NW/CS.

Supplementary Figure S21 The average particle size of Used MnTiO3-NW/CS.

Supplementary Table S14 The average particle size of Used MnTiO3-NW/CS.

| No. | Length (μm) |
| --- | --- |
| 1 | 0.831 |
| 2 | 0.977 |
| 3 | 0.862 |
| 4 | 1.476 |
| 5 | 1.600 |
| 6 | 1.349 |
| 7 | 1.223 |
| 8 | 1.540 |
| 9 | 1.493 |
| 10 | 1.401 |
| Avg. | 1.275 |

Supplementary Figure S22 The average particle size of Used MnTiO3-NW/SG.

Supplementary Table S15 The average particle size of Used MnTiO3-NW/SG.

| No. | Length (μm) |
| --- | --- |
| 1 | 0.861 |
| 2 | 1.088 |
| 3 | 0.871 |
| 4 | 1.490 |
| 5 | 1.522 |
| 6 | 1.508 |
| 7 | 1.429 |
| 8 | 1.160 |
| 9 | 0.962 |
| 10 | 1.430 |
| Avg. | 1.232 |

Supplementary Figure S23 The average particle size of Used Mn-Ti-NW/SG.

Supplementary Table S16 The average particle size of Used Mn-Ti-NW/SG.

| No. | Length (μm) |
| --- | --- |
| 1 | 1.541 |
| 2 | 1.509 |
| 3 | 1.994 |
| 4 | 1.369 |
| 5 | 1.432 |
| 6 | 1.509 |
| 7 | 1.519 |
| 8 | 1.626 |
| 9 | 1.458 |
| 10 | 1.798 |
| Avg. | 1.575 |

The mechanisms of OCM reaction, methane oxidation, and dehydrogenation are shown in equations (S1)–(S14).

.

2CH4 + 0.5O2  → C2H6 + H2O		(S1)

C2H6 + 0.5O2  → C2H4 + H2O		(S2)

CH4 + O2         → CO2 + 2H2O		(S3)

CH4 + O2         → CO2 + 2H2O + H2		(S4)

CO + 0.5O2     → CO2			(S5)

C2H4 + 2O2     → 2CO + 2H2O		(S6)

C2H6               → C2H4 + H2			(S7)

C2H4 + 2H2O  → 2CO + 4H2		(S8)

CO + H2O     → CO2+ H2			(S9)

CO2 + H2      → CO+ H2O			(S10)

C3H6 + 4.5O2 → 3CO2 + 3H2O		(S11)

C3H6 + H2 → C3H8				(S12)

C3H8 + 0.5O2 → C3H6 + H2O		(S13)

C3H8 + 5O2 → 3CO2 + 4H2O			(S14)

[Reference: B. Beck et al. / Catalysis Today 228 (2014) 212–218]

Supplementary Table S17 A survey of catalysts reported in literature.

| No. | Catalyst | Reaction temperature (˚C) | C2+ yield (%) |  | C2+ selectivity (%) |  | CH4 conversion (%) |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Na2WO4/SiO2 | 800 | 9.1 |  | 74.3 |  | 12.3 |  | 1 |
| 2 | Mn-Na2WO4/SiO2 | 800 | 23.9 |  | 64.9 |  | 36.8 |  | 1 |
| 3 | Mn/Na2WO4/SiO2 | 850 | 26.4 |  | 80.0 |  | 33.0 |  | 2 |
| 4 | Na2WO4/SiO2 | 850 | 22.9 |  | 52.0 |  | 44.0 |  | 2 |
| 5 | Na2WO4/SiO2 | 775 | 7.0 |  | 63.0 |  | 11.0 |  | 3 |
| 6 | V/Na2WO4/SiO2 | 775 | 1.2 |  | 12.0 |  | 10.0 |  | 3 |
| 7 | Cr/Na2WO4/SiO2 | 775 | 2.4 |  | 24.0 |  | 10.0 |  | 3 |
| 8 | Mn/Na2WO4/SiO2 | 775 | 16.0 |  | 80.0 |  | 20.0 |  | 3 |
| 9 | Fe/Na2WO4/SiO2 | 775 | 9.0 |  | 60.0 |  | 15.0 |  | 3 |
| 10 | CO/Na2WO4/SiO2 | 775 | 11.0 |  | 68.0 |  | 16.0 |  | 3 |
| 11 | Zn/Na2WO4/SiO2 | 775 | 6.0 |  | 63.0 |  | 9.0 |  | 3 |
| 12 | Mn-Na2WO4/SiO2 | 850 | 17.0 |  | 75.0 |  | 22.0 |  | 4 |
| 13 | Na2WO4/Mn/SiO2 | 850 | 17.2 |  | 54.0 |  | 32.0 |  | 5 |
| 14 | W-Mn/SiO2 | 820 | 20.7 |  | 68.4 |  | 30.3 |  | 6 |
| 15 | W-Li/SiO2 | 800 | 6.0 |  | 52.0 |  | 10.0 |  | 7 |
| 16 | Mn-Li/SiO2 | 800 | 6.0 |  | 40.0 |  | 15.0 |  | 7 |
| 17 | Mn-W/SiO2 | 800 | 6.0 |  | 40.0 |  | 15.0 |  | 7 |
| 18 | Mn-0.1Li-W/SiO2 | 800 | 11.0 |  | 58.0 |  | 18.0 |  | 7 |
| 19 | Mn-0.25Li-W/SiO2 | 800 | 15.0 |  | 78.0 |  | 18.0 |  | 7 |
| 20 | W-Li-W/SiO2 | 800 | 15.0 |  | 79.0 |  | 19.0 |  | 7 |
| 21 | Na2WO4/Mn/SiO2 | 800 | 11.2 |  | 27.4 |  | 41.0 |  | 8 |
| 22 | La/Na2WO4/Mn/SiO2 | 800 | 10.6 |  | 25.4 |  | 41.7 |  | 8 |
| 23 | Na-W-Mn/SiO2 | 850 | 29.0 |  | 69.0 |  | 42.0 |  | 9 |
| 24 | Na2WO4/SiO2 | 800 | 15.0 |  | 74.0 |  | 20.0 |  | 10 |
| 25 | W/SiO2 | 800 | 6.0 |  | 54.0 |  | 11.0 |  | 10 |
| 26 | Mn/SiO2 | 800 | 9.0 |  | 43.0 |  | 19.0 |  | 10 |
| 27 | W-Na-Mn/SiO2 | 775 | 18.3 |  | 39.6 |  | 46.1 |  | 11 |
| 28 | Mo-Na-Mn/SiO2 | 775 | 12.5 |  | 37.2 |  | 33.6 |  | 11 |
| 29 | Nb-Na-Mn/SiO2 | 775 | 13.0 |  | 33.2 |  | 39.3 |  | 11 |
| 30 | V-Na-Mn/SiO2 | 775 | 2.7 |  | 8.0 |  | 33.5 |  | 11 |
| 31 | Cr-Na-Mn/SiO2 | 775 | 4.6 |  | 11.5 |  | 40.1 |  | 11 |
| 32 | Ce-Mn/Na2WO4/SiO2 | 840 | 21.1 |  | 62.4 |  | 33.9 |  | 12 |
| 33 | Na-W-Mn/SiO2 | 800 | 19.1 |  | 63.2 |  | 30.2 |  | 13 |
| 34 | Mn-Na2WO4/SiO2 | 825 | 19.1 |  | 72.2 |  | 26.5 |  | 14 |
| 35 | Mn/SiO2 | 800 | 0.6 |  | 14.4 |  | 5.7 |  | 15 |
| 36 | Na2WO4/SiO2 | 800 | 2.9 |  | 69.0 |  | 4.8 |  | 15 |
| 37 | Mn-Na2WO4/SiO2 | 800 | 18.5 |  | 73.3 |  | 28.5 |  | 15 |
| 38 | NaCl-Mn-Na2WO4/SiO2 | 750 | 34.6 |  | 62.9 |  | 55.0 |  | 16 |
| 39 | (NaCl+KCl)-Mn-Na2WO4/SiO2 | 750 | 31.6 |  | 70.0 |  | 45.1 |  | 16 |

Supplementary Table S17 A survey of catalysts reported in literature. (Continued)

| No. | Catalyst | Reaction temperature (˚C) | C2+ yield (%) |  | C2+ selectivity (%) |  | CH4 conversion (%) |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 40 | KCl-Mn-Na2WO4/SiO2 | 750 | 27.0 |  | 75.3 |  | 35.9 |  | 16 |
| 41 | CsCl-Mn-Na2WO4/SiO2 | 750 | 22.6 |  | 74.9 |  | 30.1 |  | 16 |
| 42 | LiCl-Mn-Na2WO4/SiO2 | 750 | 11.3 |  | 80.2 |  | 14.1 |  | 16 |
| 43 | Mn-Na2WO4/SiO2 | 750 | 5.2 |  | 63.4 |  | 8.2 |  | 16 |
| 44 | MnxOy-Na2WO4/D11-10 | 750 | 3.6 |  | 52.9 |  | 6.7 |  | 17 |
| 45 | MnxOy-Na2WO4/SiO2 (grade 923) | 750 | 1.3 |  | 63.6 |  | 2.0 |  | 17 |
| 46 | MnxOy-Na2WO4/SiO2 (fumed) | 750 | 4.5 |  | 61.3 |  | 7.4 |  | 17 |
| 47 | MnxOy-Na2WO4/Aerosil TT 600 | 750 | 4.5 |  | 60.7 |  | 7.3 |  | 17 |
| 48 | MnxOy-Na2WO4/Aeroperl R 806/30 | 750 | 4.9 |  | 68.9 |  | 7.1 |  | 17 |
| 49 | MnxOy-Na2WO4/Aerosil OX 50 | 750 | 3.5 |  | 55.4 |  | 6.4 |  | 17 |
| 50 | MnxOy-Na2WO4/Aerosil 380 | 750 | 4.2 |  | 62.6 |  | 6.6 |  | 17 |
| 51 | MnxOy-Na2WO4/Aerosil 300 | 750 | 3.3 |  | 57.4 |  | 5.9 |  | 17 |
| 52 | MnxOy-Na2WO4/Sipernat D10 | 750 | 3.5 |  | 80.3 |  | 4.4 |  | 17 |
| 53 | MnxOy-Na2WO4/Sipernat 310 | 750 | 5.4 |  | 75.8 |  | 7.0 |  | 17 |
| 54 | MnxOy-Na2WO4/SBA-15 | 750 | 10.4 |  | 73.4 |  | 14.1 |  | 17 |
| 55 | Na2WO4/Mn/SiO2 | 800 | 2.5 |  | 67.6 |  | 3.2 |  | 18 |
| 56 | Na2WO4-Mn/SiO2 | 800 | 19.6 |  | 66.4 |  | 29.5 |  | 18 |
| 57 | TiO2-Mn2O3-Na2WO4/SiO2 | 700 | 14.0 |  | 70.0 |  | 20.0 |  | 19 |
| 58 | TiO2-Mn2O3-Na2WO4/SiO2 | 720 | 19.7 |  | 76.0 |  | 26.0 |  | 20 |
| 59 | Mn2O3-TiO2-Na2WO4/SiO2 | 650 | 13.6 |  | 62.0 |  | 22.0 |  | 20 |
| 60 | Na2WO4/Mn/SiO2 (silica gel) | 775 | 16.9 |  | 50.8 |  | 33.4 |  | 21 |
| 61 | Na2WO4/Mn/SiO2 (silica gel) | 800 | 17.1 |  | 51.0 |  | 33.5 |  | 21 |
| 62 | Na2WO4/Mn/SiO2 (fumed silica) | 800 | 16.5 |  | 52.7 |  | 33.3 |  | 21 |
| 63 | Mn/Na2WO4/SiO2 | 725 | 16.0 |  | 79.8 |  | 20.2 |  | 22 |
| 64 | Mn-Na-W/SiO2 | 750 | 16.0 |  | 64.0 |  | 25.0 |  | 23 |
| 65 | Al-Na2WO4/SiO2 | 800 | 3.2 |  | 37.0 |  | 7.69 |  | 24 |
| 66 | Li-Na2WO4/SiO2 | 800 | 4.6 |  | 47.8 |  | 9.56 |  | 24 |
| 67 | La-Na2WO4/SiO2 | 800 | 6.1 |  | 49.5 |  | 11.9 |  | 24 |
| 68 | Cu-Na2WO4/SiO2 | 800 | 7.5 |  | 22.3 |  | 33.8 |  | 24 |
| 69 | Cr-Na2WO4/SiO2 | 800 | 9.8 |  | 29.9 |  | 27.7 |  | 24 |
| 70 | Na2-WO4/SiO2 | 800 | 10.9 |  | 24.0 |  | 33.5 |  | 24 |
| 71 | Mg-Na2WO4/SiO2 | 800 | 12.5 |  | 53.2 |  | 21.6 |  | 24 |
| 72 | Ni-Na2WO4/SiO2 | 800 | 13.7 |  | 36.1 |  | 35.4 |  | 24 |
| 73 | Ce-Na2WO4/SiO2 | 800 | 15.4 |  | 32.9 |  | 42.1 |  | 24 |
| 74 | Zn-Na2WO4/SiO2 | 800 | 17.8 |  | 65.9 |  | 25.5 |  | 24 |
| 75 | Co-Na2WO4/SiO2 | 800 | 18.4 |  | 10.2 |  | 41.8 |  | 24 |
| 76 | Mn-Na2WO4/SiO2 | 800 | 19.5 |  | 41.1 |  | 45.4 |  | 24 |

Supplementary Table S17 A survey of catalysts reported in literature. (Continued)

| No. | Catalyst | Reaction temperature (˚C) | C2+ yield (%) |  | C2+ selectivity (%) |  | CH4 conversion (%) |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 77 | Mn-W/SiO2 | 800 | 11.0 |  | 48.0 |  | 24.0 |  | 24 |
| 78 | Ce-W/SiO2 | 800 | 7.0 |  | 35.0 |  | 20.0 |  | 24 |
| 79 | Mn-Na/SiO2 | 800 | 14.0 |  | 44.0 |  | 31.0 |  | 24 |
| 80 | Na2WO4-Mn/SiO2 | 800 | 20.0 |  | 67.0 |  | 30.0 |  | 24 |
| 81 | Na2WO4-Ce/SiO2 | 800 | 20.0 |  | 74.0 |  | 27.0 |  | 24 |
| 82 | TiO2-Mn2O3‐Na2WO4/SiO2 | 700 | 16.7 |  | 73.0 |  | 23.0 |  | 25 |
| 83 | Na2WO4-TiO2/SiO2 | 700 | 4.9 |  | 71.7 |  | 6.8 |  | 26 |
| 84 | MnOx-Na2WO4/SiO2 | 770 | 12.4 |  | 70.4 |  | 17.6 |  | 27 |
| 85 | Nb-MnOx-Na2WO4/SiO2 | 770 | 15.2 |  | 68.2 |  | 22.3 |  | 27 |
| 86 | Ti-MnOx-Na2WO4/SiO2 | 770 | 11.2 |  | 70.4 |  | 15.9 |  | 27 |
| 87 | Sn-MnOx-Na2WO4/SiO2 | 770 | 7.5 |  | 69.5 |  | 10.8 |  | 27 |
| 88 | Ce-MnOx-Na2WO4/SiO2 | 770 | 12.7 |  | 66.7 |  | 19.0 |  | 27 |
| 89 | Fe-MnOx-Na2WO4/SiO2 | 770 | 15.8 |  | 65.5 |  | 24.1 |  | 27 |
| 90 | Ge-MnOx-Na2WO4/SiO2 | 770 | 16.4 |  | 70.7 |  | 23.2 |  | 27 |
| 91 | Mn2O3-Na2WO4/SiC | 800 | 20.5 |  | 54.5 |  | 37.5 |  | 28 |
| 92 | Mn2O3-Na2WO4/SiO2 | 700 | 23.5 |  | 60.5 |  | 39.7 |  | 29 |
| 93 | Na2WO4-Ti-Mn/SiO2 | 700 | 22.1 |  | 62.3 |  | 35.4 |  | 30 |
| 94 | Na2WO4-TiO2-MnOx-Sr0.25/SiO2 | 750 | 22.9 |  | 62.5 |  | 36.6 |  | 31 |

Supplementary Table S18 Comparisons of OCM performance of catalysts having different initial specific surface area. Testing conditions: 50 mg catalyst, gas feed of CH4:O2:N2 = 3:1:4, reactor temperature = 700 °C, atmospheric pressure, total feed gas flow rate = 50 mL min-1 (GHSV = 30,588 h-1).

| Catalyst | Specific surface area of fumed SiO2 (m² g-1) | BET surface area of catalyst (m² g-1) | C2+ selectivity (%) | CH4 conversion (%) | C2+ yield (%) |
| --- | --- | --- | --- | --- | --- |
| 5MnTiO3-NW/CS | 85–115 | 3.20 | 58.1 | 35.5 | 20.6 |
| 5MnTiO3-NW/CS* | 350–420 | 2.86 | 57.0 | 34.3 | 19.6 |

Supplementary Table S19 Catalytic performance of 20Mn-Ti-NW/SG catalysts over 24 h. Testing conditions: 50 mg catalyst, gas feed of CH4:O2:N2 = 3:1:4, reactor temperature = 700 °C, atmospheric pressure, total feed gas flow rate = 50 mL min-1 (GHSV = 30,588 h-1).

| Time (h) | C2+ selectivity (%) | CH4 conversion (%) | C2+ yield (%) | rC2+ * | CH4 balance (%)** |
| --- | --- | --- | --- | --- | --- |
| 1 | 62.2 | 33.7 | 21.0 | 0.24 | 5.9 |
| 2 | 61.7 | 35.6 | 22.0 | 0.25 | 1.7 |
| 3 | 58.9 | 38.1 | 22.4 | 0.26 | 6.7 |
| 4 | 60.8 | 36.6 | 22.3 | 0.25 | 4.0 |
| 5 | 63.1 | 34.8 | 22.0 | 0.25 | 0.2 |
| 6 | 62.2 | 35.2 | 21.9 | 0.25 | 1.2 |
| 7 | 62.8 | 34.8 | 21.9 | 0.25 | 1.7 |
| 8 | 62.5 | 35.1 | 22.0 | 0.25 | 1.2 |
| 9 | 62.5 | 34.8 | 21.8 | 0.25 | 1.5 |
| 10 | 62.5 | 34.9 | 21.8 | 0.25 | 1.2 |
| 11 | 63.0 | 34.7 | 21.9 | 0.25 | 1.1 |
| 12 | 62.6 | 35.1 | 22.0 | 0.25 | 0.4 |
| 13 | 62.0 | 35.2 | 21.8 | 0.25 | 0.4 |
| 14 | 62.0 | 34.8 | 21.6 | 0.25 | 0.6 |
| 15 | 62.0 | 34.7 | 21.5 | 0.25 | 0.5 |
| 16 | 62.1 | 34.4 | 21.4 | 0.24 | 0.4 |
| 17 | 62.0 | 33.9 | 21.0 | 0.24 | 0.1 |
| 18 | 62.0 | 33.6 | 20.9 | 0.24 | 0.0 |
| 19 | 61.9 | 33.7 | 20.8 | 0.24 | 0.6 |
| 20 | 61.8 | 32.7 | 20.2 | 0.23 | 0.8 |
| 21 | 61.7 | 33.1 | 20.4 | 0.23 | 0.9 |
| 22 | 61.4 | 32.6 | 20.0 | 0.23 | 0.0 |
| 23 | 61.5 | 32.6 | 20.0 | 0.23 | 0.6 |
| 24 | 61.3 | 32.7 | 20.1 | 0.23 | 1.4 |

* unit of rC2+ = moles of C2+/[(total moles of MnTiO3 or (Mn+Ti) and Na2WO4)×h]

** CH4 balance (%) = {nCH4 in –[2nC2H4+ nC2H6+3nC3H6+ nC3H8+4nC4H10+ nCO+ nCO2+nCH4out]}×100/nCH4 in

References

- Jiang, Z. C., Yu, C. J., Fang, X. P., Li, S. B. & Wang, H. L. Oxide/support interaction and surface reconstruction in the sodium tungstate (Na2WO4)/silica system. J. Phys. Chem. A 97, 12870-12875 (1993).

- Palermo, A., Vazquez, J. P. H., Tikhov, M. S. & Lambert, R. M. Critical influence of the amorphous silica-to-cristobalite phase transition on the performance of Mn/Na2WO4/SiO2 catalysts for the oxidative coupling of methane. J. Catal. 177, 259-266 (1998).

- Malekzadeh, A. et al. Correlation of electrical properties and performance of OCM MOx/Na2WO4/SiO2 catalysts. Catal. Commun. 2, 241-247 (2001).

- Ji, S. F. et al. The relationship between the structure and the performance of Na-W-Mn/SiO2 catalysts for the oxidative coupling of methane. Appl. Catal. A Gen. 225, 271-284 (2002).

- Ji, S. et al. Surface WO4 tetrahedron: The essence of the oxidative coupling of methane over M-W-Mn/SiO2 catalysts. J. Catal. 220, 47-56 (2003).

- Wang, J. et al. Comparative study on oxidation of methane to ethane and ethylene over Na2WO4-Mn/SiO2 catalysts prepared by different methods. J. Mol. Catal. A Chem. 245, 272-277 (2006).

- Malekzadeh, A., Khodadadi, A., Dalai, A. K. & Abedini, M. Oxidative coupling of methane over lithium doped (Mn+W)/SiO2 catalysts. J. Nat. Gas Chem. 16, 121-129 (2007).

- Wu, J., Zhang, H., Qin, S. & Hu, C. La-promoted Na2WO4/Mn/SiO2 catalysts for the oxidative conversion of methane simultaneously to ethylene and carbon monoxide. Appl. Catal. A Gen. 323, 126-134 (2007).

- Chua, Y. T., Mohamed, A. R. & Bhatia, S. Oxidative coupling of methane for the production of ethylene over sodium-tungsten-manganese-supported-silica catalyst (Na-W-Mn/SiO2). Appl. Catal. A Gen. 343, 142-148 (2008).

- Gholipour, Z., Malekzadeh, A., Hatami, R., Mortazavi, Y. & Khodadadi, A. Oxidative coupling of methane over (Na2WO4+Mn or Ce)/SiO2 catalysts: In situ measurement of electrical conductivity. J. Nat. Gas Chem. 19, 35-42 (2010).

- Mahmoodi, S., Ehsani, M. R. & Ghoreishi, S. M. Effect of promoter in the oxidative coupling of methane over synthesized Mn/SiO2 nanocatalysts via incipient wetness impregnation. J. Ind. Eng. Chem. 16, 923-928 (2010).

- Shahri, S. M. K. & Pour, A. N. Ce-promoted Mn/Na2WO4/SiO2 catalyst for oxidative coupling of methane at atmospheric pressure. J. Nat. Gas Chem. 19, 47-53 (2010).

- Lee, J. Y. et al. Scaled-up production of C2 hydrocarbons by the oxidative coupling of methane over pelletized Na2WO4/Mn/SiO2 catalysts: Observing hot spots for the selective process. Fuel 106, 851-857 (2013).

- Godini, H. R. et al. Sol–gel method for synthesis of Mn–Na2WO4/SiO2 catalyst for methane oxidative coupling. Catal. Today 236, 12-22 (2014).

- Elkins, T. W. & Hagelin-Weaver, H. E. Characterization of Mn-Na2WO4/SiO2 and Mn-Na2WO4/MgO catalysts for the oxidative coupling of methane. Appl. Catal. A Gen. 497, 96-106 (2015).

- Hiyoshi, N. & Ikeda, T. Oxidative coupling of methane over alkali chloride-Mn-Na2WO4/SiO2 catalysts: Promoting effect of molten alkali chloride. Fuel Process. Technol. 133, 29-34 (2015).

- Yildiz, M. et al. Silica material variation for the MnxOy-Na2WO4/SiO2. Appl. Catal. A Gen. 525, 168-179 (2016).

- Fleischer, V., Steuer, R., Parishan, S. & Schomäcker, R. Investigation of the surface reaction network of the oxidative coupling of methane over Na2WO4/Mn/SiO2 catalyst by temperature programmed and dynamic experiments. J. Catal. 341, 91-103 (2016).

- Wang, P., Zhao, G., Liu, Y. & Lu, Y. TiO2-doped Mn2O3-Na2WO4/SiO2 catalyst for oxidative coupling of methane: Solution combustion synthesis and MnTiO3-dependent low-temperature activity improvement. Appl. Catal. A Gen. 544, 77-83 (2017).

- Wang, P., Zhao, G., Wang, Y. & Lu, Y. MnTiO3-driven low-temperature oxidative coupling of methane over TiO2-doped Mn2O3-Na2WO4/SiO2 catalyst. Sci. Adv. 3, e1603180; doi:10.1126/sciadv.1603180 (2017).

- Yunarti, R. T. et al. Oxidative coupling of methane using Mg/Ti-doped SiO2-supported Na2WO4/Mn catalysts. ACS Sustain. Chem. Eng. 5, 3667-3674 (2017).

- Uzunoglu, C., Leba, A. & Yildirim, R. Oxidative coupling of methane over Mn-Na2WO4 catalyst supported by monolithic SiO2. Appl. Catal. A Gen. 547, 22-29 (2017).

- Hayek, N. S., Lucas, N. S., Damouny, C. W. & Gazit, O. M. Critical surface parameters for the oxidative coupling of methane over the Mn-Na-W/SiO2 catalyst. ACS Appl. Mater. Interfaces 9, 40404-40411 (2017).

- Gu, S. et al. Effects of metal or metal oxide additives on oxidative coupling of methane using Na2WO4/SiO2 catalysts: Reducibility of metal additives to manipulate the catalytic activity. Appl. Catal. A Gen. 562, 114-119 (2018).

- Wang, P., Zhang, X., Zhao, G., Liu, Y. & Lu, Y. Oxidative coupling of methane: MOx-modified (M=Ti, Mg, Ga, Zr) Mn2O3-Na2WO4/SiO2 catalysts and effect of MOx modification. Chinese J. Catal. 39, 1395-1402 (2018).

- Seubsai, A., Tiencharoenwong, P., Kidamorn, P. & Niamnuy, C. Synthesis of light hydrocarbons via oxidative coupling of methane over silica-supported Na2WO4-TiO2 catalyst. Eng. J. 23, 169-182 (2019).

- Hayek, N. S., Khlief, G. J., Horani, F. & Gazit, O. M. Effect of reaction conditions on the oxidative coupling of methane over doped MnOx-Na2WO4/SiO2 catalyst. J. Catal. 376, 25-31 (2019).

- Kim, J., Park, L.-H., Ha, J.-M. & Park, E. D. Oxidative coupling of methane over Mn2O3-Na2WO4/SiC catalysts. Catalysts 9; doi:10.3390/catal9040363 (2019).

- Chukeaw, T., Sringam, S., Chareonpanich, M. & Seubsai, A. Screening of single and binary catalysts for oxidative coupling of methane to value-added chemicals. Mol. Catal. 470, 40-47 (2019).

- Sringam, S., Kidamorn, P., Chukeaw, T., Chareonpanich, M. & Seubsai, A. Investigation of metal oxide additives onto Na2WO4-Ti/SiO2 catalysts for oxidative coupling of methane to value-added chemicals. Catal. Today 358, 263-269 (2020).

- Kidamorn, P. et al. Synthesis of value-added chemicals via oxidative coupling of methanes over Na2WO4-TiO2-MnOx/SiO2 catalysts with alkali or alkali earth oxide additives. ACS Omega 5, 13612-13620 (2020).