# Characterisation of dust emissions from machined engineered stones to understand the hazard for accelerated silicosis

Chandnee Ramkissoon1, Sharyn Gaskin1*, Leigh Thredgold1, Tony Hall2, Shelley Rowett3 and Richard Gun1

1Adelaide Exposure Science and Health, School of Public Health, The University of Adelaide, South Australia

2School of Physical Sciences, The University of Adelaide, South Australia

3SafeWork SA, Government of South Australia, 33 Richmond Road, Keswick, South Australia

Corresponding author: sharyn.gaskin@adelaide.edu.au ORCID ID 0000-0002-1507-6425

Fig. S1: Thermogravimetric (TGA) (solid line) and derivative TGA (DTG) curves of an engineered stone sample (heating rate, 10⁰C min−1 to 1000⁰C under N2 atmosphere).

Table S1: Specific surface area of the ‘settled’ dust fraction (including respirable fraction) generated from machining engineered (ES1-ES12) and natural stone.

| Stone | Specific surface area |
| --- | --- |
|  | m2/g |
| ES1 | 2.72 |
| ES2 | 2.43 |
| ES3 | 2.73 |
| ES4 | 1.93 |
| ES5 | 1.62 |
| ES6 | 1.43 |
| ES7 | 1.78 |
| ES8 | 1.54 |
| ES9 | 1.87 |
| ES10 | 1.89 |
| ES11 | 2.34 |
| ES12 | 2.38 |
| Black granite | 0.768 |
| White granite | 0.878 |
| White marble | 0.439 |

Table S2: Pearson’s coefficients for the correlations between elements in engineered stone (n=12).

|  | Fe | Al | Ca | Mg | K | Na | Ti | Cu | P | S | Ni | Co | Cr | Sn | Zr |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Al | 0.40 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Ca | 0.01 | 0.25 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Mg | 0.38 | 0.88** | 0.64** |  |  |  |  |  |  |  |  |  |  |  |  |
| K | 0.41 | 0.09 | 0.58 | 0.28 |  |  |  |  |  |  |  |  |  |  |  |
| Na | 0.16 | 0.62** | 0.91** | 0.90** | 0.46 |  |  |  |  |  |  |  |  |  |  |
| Ti | 0.23 | 0.64** | 0.17 | 0.64** | 0.01 | 0.61* |  |  |  |  |  |  |  |  |  |
| Cu | 0.02 | 0.30 | 0.26 | 0.26 | 0.07 | 0.30 | 0.18 |  |  |  |  |  |  |  |  |
| P | 0.22 | 0.43 | 0.13 | 0.10 | 0.21 | 0.10 | 0.07 | 0.29 |  |  |  |  |  |  |  |
| S | 0.12 | 0.74** | 0.13 | 0.61* | 0.22 | 0.42 | 0.72** | 0.00 | 0.17 |  |  |  |  |  |  |
| Ni | 0.12 | 0.74** | 0.13 | 0.61* | 0.22 | 0.42 | 0.72** | 0.00 | 0.17 | 0.08 |  |  |  |  |  |
| Co | 0.11 | 0.27 | 0.19 | 0.24 | 0.22 | 0.26 | 0.13 | 0.96** | 0.31 | 0.17 | 0.84** |  |  |  |  |
| Cr | 0.12 | 0.74** | 0.13 | 0.61* | 0.22 | 0.42 | 0.72** | 0.00 | 0.17 | 0.08 | 0.21 | 0.01 |  |  |  |
| Sn | 0.00 | 0.10 | 0.13 | 0.18 | 0.38 | 0.16 | 0.17 | 0.39 | 0.30 | 0.01 | 0.40 | 0.38 | 0.30 |  |  |
| Zr | 0.48 | 0.15 | 0.20 | 0.24 | 0.66** | 0.20 | 0.22 | 0.23 | 0.26 | 0.32 | 0.48 | 0.19 | 0.50 | 0.66** |  |
| Cl | 0.12 | 0.74** | 0.13 | 0.61* | 0.22 | 0.42 | 0.72** | 0.00 | 0.17 | 0.08 | 0.21 | 0.01 | 0.56 | 0.16 | 0.27 |

*: Statistical significance at 95% confidence level (p<0.05)

**: Statistical significance at 99% confidence level (p<0.01)