## Supplementary Information

# A virtual laboratory based on full-field crystal plasticity simulation to characterize the multiscale mechanical properties of AHSS

Hongyue Ma1,2, Yangqi Li1,2, Haiming Zhang1,2*, Qian Li3, Fei Chen1,2, Zhenshan Cui1,2

1. School of Materials Science and Engineering, Shanghai Jiao Tong University, 800 Dongchuan Road, Shanghai 200240, China

2. Institute of Forming Technology & Equipment, Shanghai Jiao Tong University, 1954
Huashan Road, Shanghai, 200030, PR China

3. Institute of Shanghai Aircraft Design & Research of Commercial Aircraft Corporation of China, Jinke Road, Shanghai, 201210, PR China

Table S1 Chemical composition of the cold-rolled and annealing DP980 steel (wt.%)

| C | Mn | Si | P | S | Al | Fe |
| --- | --- | --- | --- | --- | --- | --- |
| 0.15 | 2.73 | 1.56 | 0.029 | 0.025 | 0.033 | Balance |

Figure S1. (a) The geometric shapes and dimensions of the specimens designed for biaxial tensile, pure shear, and uniaxial tensile tests; σ11 and σ22 denote the normal stress in the rolling direction (RD) and transverse direction (TD). The equipments used in the experiments are (b) the universal testing machine of INSTRON 8080 and (c) the planar biaxial test system MTS BIA5105.

Figure S2. r-value versus θ of different RVEs at deformation stage with the specific plastic work of 8 MPa.

Figure S3. The ND and RD IPF maps of the as-received DP980 sheet steel characterized on the RD-TD plane (a) at the surface and (b) at the thickness center. The maps was generated by the MATLAB® (version R2018b) open-source toolbox MTEX [38].

Table S2. Comparation of the average r-value and the planar anisotropy between the experiments results and simulation ones.

|  | Experiments | Dual-phase | Single-phase of ferrite | Single-phase of martensite | Dual-phase with q=1.0 |
| --- | --- | --- | --- | --- | --- |
| r | 0.941 | 1.047 | 1.057 | 1.071 | 1.063 |
| ∆r | 0.380 | 0.443 | 0.702 | 0.685 | 0.560 |

### Yield functions and the analytical expressions of r-value

The r-value rθ (where θ is the inclined angle of the uniaxial tensile specimen with respect to the RD) is defined as the ratio of the plastic strain rates associated to width (inclined at the angle θ+90° with respect to the RD), εθ+90, and thickness, ε33

rθ=εθ+90ε33                                                        (1)

If the associated flow rule is used, the above equation can be rewritten in terms of the stress components as

rθ=-∂σ∂σ11sin2θ+∂σ∂σ22cos2θ-∂σ∂σ12sinθcosθ∂σ∂σ11+∂σ∂σ22                                    (2)

Where σ is the effective stress defined by a specific yield function, and σ11, σ22, and σ12 are the in-plane stress components. More details about the derivation can be referred to the work of Banabic 3.

### The quadratic Hill48 yield function

The Hill48 yield criterion 5 is a typical quadratic yield function; its effective stress is written as:

σ=Fσ22-σ332+Gσ33-σ112+Hσ11-σ222+2Lσ232+2Mσ312+2Nσ122   (3)

where F,G,H,L,M, and N are the anisotropic parameters. The expression of ∂σ∂σij for this function is straightforward, and rθ is written as

rθ=-Gcos2θsin2θ+Fcos2θsin2θ-Hcos22θ-12Nsin22θGcos2θ+Fsin2θ   		   			 		   (4)

### The Yld91 yield function

The effective stress of then Yld91 yield criterion 9 is:

σ=3I221m∅1m+∅2m+∅3m1m               			           (5)

with ∅1=2cos2α+π6，∅2=2cos2α+3π6, ∅3=2cos2α+5π6 and α=arccosI3I232. I2 and I3 are the second and the third invariants of stress tensor, respectively. For the anisotropic case, I2 and I3 become:

I2=fF2+gG2+hH23+aA-cC2+cC-bB2+bB-aA254                         (6)

I3=cC-bBaA-cCbB-aA54+fghFGH-cC-bBfF2+aA-cCgG2+bB-aAhH26   (7)

where A=σ22-σ33, B=σ33-σ11, C=σ11-σ22, F=σ23, G=σ31, and H=σ12. a,b,c,f,g,h, and m are material parameters.

By means of chain rule of derivative, ∂σ∂σij is explained as follows,

∂σ∂σij=∂σ∂I2∂I2∂σij+∂σ∂α∂α∂σij and ∂σ∂α=∂σ∂∅i∂∅i∂α                                  (8)

The last term follows the Einstein summation convention. By means of the direct mathematical operations, the components in Eq. 5 are obtained as

∂σ∂I2=σ2I2      															    (9)

∂σ∂∅i=3I221m∅1m+∅2m+∅3m1m-1∅im-2∅i			             (10)

∂α∂σij=∂α∂I2∂I2∂σij+∂α∂I3∂I3∂σij, with ∂α∂I2=-3I32I2521-I32I23 and ∂α∂I3=-2I23I3∂α∂I2           (11)

While ∂I2∂σij, ∂I3∂σij, and ∂∅i∂α are easily accessible. In the end, a complete expression of ∂σ∂σij reads,

∂σ∂σij=∂σ∂I2+∂σ∂α∂α∂I2∂I2∂σij+∂σ∂α∂α∂I3∂I3∂σij,                                   (12)

Substitute the aforementioned components into Eq. 8, one can obtain the specific expressions of ∂σ∂σ11, ∂σ∂σ22, and ∂σ∂σ12. rθ then can be derived based on Eq. 2.

### The Yld2004-18p yield function

The Yld2004-18p anisotropic yield function proposed by Barlat et al. 12 is one of the most widely used advanced yield functions; its effective stress is defined as follows,

σ=14∅1m                                                       (13)

where m is the homogeneous exponent related to the crystal structure of materials. ∅ is expressed as follows:

∅=s'1-s''1m+s'1-s''2m+s'1-s''3m+s'2-s''1m+s'2-s''2m

+s'2-s''3m+s'3-s''1m+s'3-s''2m+s'3-s''3m           (14)

where s'i and s''i i=1, 2, 3 are the principal values of tensors S' and S'', which are defined by liner transformations of deviatoric part of Cauchy stress tensor σ':

S'=C:σ', S’’=D:σ'                                                (15)

The fourth-order tensors C and D characterize the anisotropy of the material, and each contains nine material parameters as follows (in Voigt notation).

C=0-c12-c13000-c210-c23000-c31-c320000000c44000000c55000000c66                              (16)

D=0-d12-d13000-d210-d23000-d31-d320000000d44000000d55000000d66                            (17)

The identified coefficients include the elements in the tensors C and D and the exponent m. This yield function contains 18 anisotropic parameters, among which c55, c66, d55 and d66 are used to characterize the out-of-plane anisotropies, and the other 14 parameters describe the in-plane properties of the sheet. Note that the Yld2004-18p reduces to the Yld91 yield function when C=D.

By means of chain rule of derivative, ∂σ∂σij=∂σ∂∅∂∅∂σij, and

∂σ∂∅=14m⋅14∅1m-1                                                  (18)

∂∅∂σij=∂∅∂sk'∂sk'∂σij+∂∅∂sk''∂sk''∂σij                                              (19)

As illustrated in Eq. 15, the principal stresses sk' (k=1, 2, 3) and sk'' have the same form. In the following, we focus the derivation associated with sk'. First, the expression of sk' reads,

sk'=I13+23I12-3I2cosα+2π3k, k=1, 2, 3                           (20)

with

α= arccos2I13-9I1I2+27I32I12-3I232-2π3                                      (21)

where I1, I2, and I3 are the stress invariants of the stress tensor S'. Thus, sk' is a function of I1, I2, and I3. Therefore

∂sk'∂σij=∂sk'∂Im∂Im∂σij                                                      (22)

where

∂sk'∂I1=13+23I12-3I2-12I1cosα+2kπ3-23I12-3I2sin⁡α+2kπ3∂α∂I1     (23)

∂sk'∂I2=-I12-3I2-12cosα+2kπ3-23I12-3I2sin⁡α+2kπ3∂α∂I2          (24)

∂sk'∂I3=-23I12-3I2sin⁡α+2kπ3∂α∂I3                                   (25)

Since ∂Im∂σij and ∂α∂Im (m=1,2,3) can routinely derived. ∂∅∂σij can be obtained through the assembly of the above equations.