Supplementary Table 1. Comparison of the calculated results with the relevant literature.

| Material | Young’s modulus (GPa) | Ultimate stress (GPa) | Failure strain (%) | Thermal conductivity (W/m-K) | Temperature | Method | References |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MoS2 | 159.05 (armchair) 161.95 (zigzag) | 15.03 14.95 | 12.3 12.9 | - | 300 K |  | Changli et al. [79] |
| MoS2 | 158.1 (armchair) 159.7 (zigzag) | 16.5 16.2 | 19.6 22.7 | - | 1 K |  | Subad et al. [29] |
| MoS2 | 165.7 (armchair) 167.0 (zigzag) | 16.8 16.2 | 19.5 20 | - | 1 K |  | Jiang et al. [46] |
| MoS2 | 148.9÷248.3 |  | 23 | - | 0 K |  | Cooper et al. [80] |
| MoS2 |  |  |  | 47.5 | 300 K | DFT | Xiang et al. [35] |
| MoS2 |  |  |  | 23.2 | 300 K | DFT | Cai et al. [38] |
| MoS2 |  |  |  | 130.3 | 300 K | DFT | Ouyang et al. [81] |
| MoS2 |  | - | - | 51.4 | 300 K | MD | Krishnamoorthy et al. [51] |
| MoS2 |  |  |  | 42.18 | 300 K | MD | Chen et al. [55] |
| MoS2 |  |  |  | 80-105 | 300 K | Experiment | Yang et al. [30] |
| MoS2 |  |  |  | 40.8 | 300 K | Experiment | Li et al. [31] |
| MoS2 |  |  |  | 34.5±4 | 300 K | Experiment | Yan et al. [32] |
| MoS2 |  |  |  | 84±17 | 300 K | Experiment | Zhang et al. [34] |
| MoS2 |  | - | - | 52 | 300 K | Experiment | Shahoo et al. [52] |
| MoS2 |  |  |  | 48-52 | 300 K | Experiment | Jo et al. [54] |
| MoS2 | 158.73 (armchair) 158.01 (zigzag) | 16.96 16.25 | 19.78 22.79 |  | 1 K | MD | This research |
|  | 149.08 (armchair) | 13.54 | 12.4 | κMD = 52.91 κcorr = 43.41 | 300 K | MD | This research |
|  | 145.04 (zigzag) | 12.90 | 13.23 | κMD =52.35 κcorr = 42.92 | 300 K |  |  |

Supplementary References:

[79] Yi, C., Hu, C., Bai, M., Lv, J., & Tang, D. (2020). Molecular dynamics study on the mechanical properties of multilayer MoS2 under different potentials. Nanotechnology, 31(21), 215703.

[80] Cooper, R. C., Lee, C., Marianetti, C. A., Wei, X., Hone, J., & Kysar, J. W. (2013). Nonlinear elastic behavior of two-dimensional molybdenum disulfide. Physical Review B, 87(3), 035423.

[81] Ouyang, B., Chen, S., Jing, Y., Wei, T., Xiong, S., & Donadio, D. (2018). Enhanced thermoelectric performance of two dimensional MS2 (M= Mo, W) through phase engineering. Journal of Materiomics, 4(4), 329-337.