Supporting Information

Multifunctional green synthesized Cu-Al layered double hydroxide (LDH) nanoparticles: Anti-cancer and antibacterial activities

Mahsa Kiani1, Mojtaba Bagherzadeh1,*, Amir Mohammad Ghadiri1, Pooyan Makvandi2, Navid Rabiee1,3

- Department of Chemistry, Sharif University of Technology, Tehran, Iran

- Istituto Italiano di Tecnologia, Center for Materials Interfaces, viale Rinaldo Piaggio 34, 56025 Pontedera, Pisa, Italy

- School of Engineering, Macquarie University, Sydney, New South Wales, 2109, Australia

*Corresponding author: Mojtaba Bagherzadeh (bagherzadeh@sharif.edu)

## Green synthesis of molecules

Multi-step synthesis of molecules was performed by mechanochemical and standard reactions (Scheme 1); the objective is to enhance the biocompatibility of the final products, along with significantly reducing the generation of pollutants.

Scheme 1. Synthesis procedure of the deployed molecules.

4-aminobenzohydrazide (2)

Benzocaine (1) (5 mmol) and hydrazine hydrate (20 mmol) were melted together (115 °C, 60 min) in a closed container. Recrystallization was conducted by using EtOH yielded needle crystalline product. Yield 85%, m.p: 321-324 °C, IR (KBr) ν (cm-1) 3300-3200 (NH, NH2), 1670, 1650 (C=O), LC-MS (ESI) m/z 256 (M+H).

4-(2-(4-(3-carboxypropanamido)benzoyl)hydrazineyl)-4-oxobutanoic acid (3a)

p-Amino benzohydrazide (2) (0.151g, 1 mmol) with succinic anhydride (2.02 mmol) was refluxed in ethyl acetate (20 mL) for 12 hours. The organic solvent was removed under vacuum and the mixture was poured into 30 mL of distilled water and stirred for 30 minutes. The reaction was made acidic by adding concentrated HCl. The crude product was dried and then recrystallized from EtOAc and finally purified by a short column of silica gel and mobile phase of hexane: chloroform (20:80). Yield 45%, m.p: 185-187 °C. IR (KBr) ν (cm-1) 3200-2800 (NH, COOH), 2750-2600 (-CH2-CH2), 1700 (C=O), 1200-1400 (Ar). 1H NMR(400 MHz, DMSO) δppm 11.66 (s, 2H, 2 COOH), 10.32-10.23 (d, 3H, 3NH), 7.80 (d, J = 8.5 Hz, 2H, Ar), 7.67 (d, J = 8.5 Hz, 2H, Ar), 2.60 (d, J = 6.3 Hz, 2H, -CH2), 2.55 (d, J = 6.1 Hz, 2H, -CH2), 1.99-1.94 (d, 4H, -CH2). 13C NMR (101 MHz, DMSO) δppm 174.30, 171.00, 163.11, 160.17, 142.45, 129.03, 128.56, 118.45, 31.56, 29.12, 25.56, 18.45.  LC-MS (ESI) m/z 350 (M-H). Anal. Calcd. for C15H17N3O7: C, 51.28; H, 4.88; N, 11.96. Found: C, 51.20; H, 4.91; N, 12.04.

General procedure for the green synthesis of the compounds 3b-3e

p-Amino-benzohydrazide (2) (0.151g, 1 mmol) with the either acyl chloride or benzenesulfonyl chloride (2.02 mmol) was stirred in pyridine (5 ml) for 24 hours. The reaction mixture was poured into 30 mL of distilled water and stirred for 15 minutes. The pH of the mixture was decreased by adding concentrated HCl. The precipitate was then recrystallized from EtOH to afford white amorphous solid.

4-fluoro-N-(4-(2-(4-fluorobenzoyl)hydrazine-1-carbonyl)phenyl)benzamide (3b)

Yield: 60%, m.p: 322-325 °C, IR (KBr) ν (cm-1) 3700-3100 (NH), 1700-1650 (C=O), 1200-1400 (Ar). 1H NMR(400 MHz, DMSO) δppm 10.55 (s, 2H, 2NH), 10.51 – 10.46 (m, 1H, NH), 8.05 (dd, J = 8.4, 5.4 Hz, 4H, Ar), 7.98 – 7.89 (m, 4H, Ar), 7.39 (d, J = 8.7 Hz, 4H, Ar). 13C NMR (101 MHz, DMSO) δppm 165.93, 165.81, 165.32, 165.26, 163.45, 142.80, 131.55, 131.09, 131.00, 130.69, 130.60, 128.75, 127.81, 120.06, 116.13, 116.01, 115.92, 115.79.  LC-MS (ESI) m/z 394 (M-H). Anal. Calcd. for C21H15F2N3O3: C, 63.80; H, 3.82; N, 10.63. Found: C, 63.74; H, 3.86; N, 10.61.

4-methoxy-N-(4-(2-(4-methoxybenzoyl)hydrazine-1-carbonyl)phenyl)benzamide (3c)

Yield: 67%, m.p: 264-266 °C, IR (KBr) ν (cm-1) 3300-3100 (NH), 1700-1650 (C=O), 1200-1400 (Ar). 1H NMR(400 MHz, DMSO) δppm 10.36 (s, 3H, 3NH), 7.99 (d, J = 8.8 Hz, 2H, Ar), 7.92 (d, J = 5.5 Hz, 6H, Ar), 7.07 (m, 4H, Ar), 3.85 (s, 3H, OMe), 3.84 (s, 3H, OMe). 13C NMR (101 MHz, DMSO) δppm 165.89, 165.69, 162.58, 162.47, 143.04, 130.24, 128.68, 127.62, 127.10, 125.22, 119.93, 114.19, 114.15, 55.94, 55.87.  LC-MS (ESI) m/z 418 (M-H). Anal. Calcd. for C23H21N3O5: C, 65.86; H, 5.05; N, 10.02. Found: C, 65.94; H, 5.02; N, 10.00.

4-nitro-N-(4-(2-(4-nitrobenzoyl)hydrazine-1-carbonyl)phenyl)benzamide (3d)

Yield: 74%, m.p: 287-289 °C, IR (KBr) ν (cm-1) 3300-3100 (NH), 1700-1650 (C=O), 1350, 1550 (NO), 1200-1400 (Ar). 1H NMR (400 MHz, DMSO) δppm 10.86 (s, 1H, NH), 10.72 (s, 2H, 2NH), 8.40 (m, 4H, Ar), 8.26 – 8.15 (m, 4H, Ar), 8.02 – 7.85 (m, 4H, Ar). 13C NMR (101 MHz, DMSO) δppm 165.53, 164.76, 149.83, 149.75, 142.45, 140.77, 138.85, 129.83, 129.44, 128.84, 128.17, 124.25, 124.08, 120.25.  LC-MS (ESI) m/z 448 (M-H). Anal. Calcd. for C21H15N5O7: C, 56.13; H, 3.36; N, 15.58. Found: C, 56.09; H, 3.39; N, 15.55.

N-(4-(2-(phenylsulfonyl)hydrazine-1-carbonyl)phenyl)benzenesulfonamide (3e)

Yield: 38%, m.p: 239-241 °C, IR (KBr) ν (cm-1) 3700-3300 (NH), 1700-1650 (C=O), 1200-1400 (Ar), 1100-1200 (SO2). 1H NMR (400 MHz, DMSO) δppm 11.40 (s, 1H, NH), 10.88 (s, 2H, 2NH), 7.97– 7.50 (m, 14H, Ar). 13C NMR (101 MHz, DMSO) δppm 166.03, 142.33, 139.68, 138.63, 135.10, 133.76, 129.94, 129.67, 129.24, 128.97, 128.05, 127.14, 126.29, 118.65.  LC-MS (ESI) m/z 430 (M-H). Anal. Calcd. for C19H17N3O5S2: C, 52.89; H, 3.97; N, 9.74. Found: C, 52.80; H, 3.94; N, 9.78.