Supplementary information

Nanomechanical Variability in the Early Evolution of Vertebrate Dentition

Mohammad Shohel1, Kamal K. Ray1, Alexei V. Tivanski1, Neo E.B. McAdams2, Alyssa M. Bancroft3, Bradley D. Cramer*4, Tori Z. Forbes*1

1Department of Chemistry, University of Iowa, Iowa City, IA-52242

2Department of Geosciences, Texas Tech University, Lubbock, TX-79409

3Iowa Geological Survey, University of Iowa, Iowa City, IA-52242

4Department of Earth and Environmental Sciences, University of Iowa, Iowa City, IA-52242

*Corresponding authors: tori-forbes@uiowa.edu; bradley-cramer@uiowa.edu

Table of Contents

- Calculation of Young’s Modulus

- AFM Images of Surface

- Calculation of Young’s Modulus

The equations used to calculate the radius of contact area (aJKR), the force arising from interactions between two spheres (FJKR), the indentation depth (hJKR), the work of adhesion (W) and YM in the JKR models are:

aJKR=3RFJKR4E*                                             	(1)

hJKR=aJKR2R-2πWaJKRE*                                           	(2)

FJKR=F+3πWR+ 6πWR+ 9π2W2R2   	                       	(3)

W= -23Fpull-offπR                                    	 (4)

here R is tip radius of curvature, E* the effective Young’s modulus of the tip and sample determined from the following equation:

1E*=1-νtip2Etip+1-νcrystal2Ecrystal 			        (5)

where Ecrystal and Etip are the Young’s modulus of the sample and tip, respectively. Here, νtip and νcrystal are the Poisson’s ratio of the tip and crystal, respectively. The estimated Poisson’s ratio of the tip and crystal are 0.2 and 0.33, respectively.2-4 The radius of curvature of the AFM tip and Young’s modulus of tip were 8 nm and 865 GPa, respectively. A representative force versus tip sample separation plot with JKR model fit is shown in Figure S1.

Figure S1. A representative force versus tip−sample separation plot is shown at a maximum applied force of 500 nN. The blue and green dots are the approach and retract data, respectively. The solid red line is shown for the JKR fitting of the approach data.

Table S1. Young’s modulus values measured using AFM nanoindentation of conodont elements of Dapsilodus obliquicostatus at different zones with one standard deviation (average ± SD). All units are in GPa, J and O refers to juvenile and older, respectively.

| Zone | Sa (J) | Sa (O) | Sb-c (J) | Sb-c (O) | M (J) | M (O) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 5.3±0.6 | 8.4±0.6 | 6.0 ± 2.7 | 6.7 ± 1.8 | 6.8 ± 1.1 | 17.7 ± 5.8 |
| 2 | 36.7±3.3 | 43.9±3.8 | 30.0 ± 10.2 | 41.5±10.4 | 26.8 ± 3.2 | 52.5 ± 9.6 |
| 3 | 52.6±5.4 | 66.6±4.8 | 40.5 ± 12.9 | 65± 13.6 | 53.8 ± 4.4 | 65.7 ± 4.1 |
| 4 | 19.3±2.7 | 35.6±5.4 | 15.4 ± 6.6 | 20.4 ± 8.6 | 25.3 ± 3.1 | 32.1 ± 9.9 |
| 5 | 9.9±1.8 | 16.6±2.6 | 4.7 ± 2.0 | 12.5 ± 2.3 | 5.6 ± 0.6 | 6.9 ± 3.1 |

*J= Juvenile, O= Older

- AFM Images of Surface

5

4

3

2

1

O

J

Figure S2. Representative AFM amplitude images of Sa conodonts, where top (a-e: Zones 1-5) and bottom (f-j: Zones 1-5) rows are for the juvenile and older samples, respectively. The images sequentially show the tip to base segments from left to right.

1

2

3

4

5

O

J

Figure S3. Representative AFM amplitude images of Sb-c conodonts, where top (a-e= Zones 1-5) and bottom (f-j= Zones 1-5) rows are for the juvenile and older conodonts, respectively. Left to right rows sequentially show the tip to base segments.

O

J

5

4

3

2

1

Figure S4. Representative AFM amplitude images of M conodonts, where top (a-e: Zones 1-5) and bottom (f-j: Zones 1-5) rows are for the juvenile and older conodonts, respectively. Left to right rows sequentially show the tip to base segments.

References:

1.	Johnson, K. L.;  Kendall, K.; Roberts, A. D., Surface energy and the contact of elastic solids. Proceedings of the royal society of London. A. mathematical and physical sciences 1971, 324 (1558), 301-313.

2.	Lee, H. D.;  Ray, K. K.; Tivanski, A. V., Solid, Semisolid, and Liquid Phase States of Individual Submicrometer Particles Directly Probed Using Atomic Force Microscopy. Analytical Chemistry 2017, 89 (23), 12720-12726.

3.	Hutchins, K. M.;  Rupasinghe, T. P.;  Oburn, S. M.;  Ray, K. K.;  Tivanski, A. V.; MacGillivray, L. R., Remarkable decrease in stiffness of aspirin crystals upon reducing crystal size to nanoscale dimensions via sonochemistry. CrystEngComm 2019, 21 (13), 2049-2052.

4.	Mohapatra, H.;  Kruger, T. M.;  Lansakara, T. I.;  Tivanski, A. V.; Stevens, L. L., Core and surface microgel mechanics are differentially sensitive to alternative crosslinking concentrations. Soft matter 2017, 13 (34), 5684-5695.