Supplementary information

A green protocol for the one-pot synthesis of 3,4-disubstituted isoxazole-5(4H)-ones using modified β-Cyclodextrin as a catalyst

Mahdieh Tajbakhsh a, Mohammad Reza Naimi-Jamal a, *, Saeed Balalaie b, Mohadeseh Rezaeian a

a. Research Laboratory of Green Organic Synthesis & Polymers, Department of Chemistry, Iran University of Science and Technology, P.O. Box 16846–13114 Tehran, Iran

b. Peptide Chemistry Research Institute, K. N. Toosi University of Technology, P. O. Box 15875-4416, Tehran, Iran

*Corresponding author E-mail: naimi@iust.ac.ir

Table of Content

FT-IR spectra of some products (4a, 4e, 4k, 4l) …………………………………………….……(S2-S5)

1H-NMR spectra of some products (4a, 4k) …………………………………………………………(S6-S7)

FT-IR spectrum of the reused catalyst…………………………………………………………………S8

Figure S1: FT-IR spectrum of product 4a

Figure S2: FT-IR spectrum of product 4e

Figure S3: FT-IR spectrum of product 4k

Figure S4: FT-IR spectrum of product 4l

Figure S5: 1H-NMR spectrum of product 4a

Figure S6: 1H-NMR spectrum of product 4k

Figure S7: FT-IR spectrum of the reused catalyst