Supplementary information

Miscibility and Ternary Diagram of Aqueous Polyvinyl alcohols with Different Degrees of Saponification

Junhyuk Kim1,‡, Shohei Ishikawa2,‡,*, Mitsuru Naito3, Xiang Li4, Ung-il Chung1, and Takamasa Sakai2,*

1Department of Bioengineering, Graduate School of Engineering, The University of Tokyo, 7-3-1 Hongo, Bunkyo-ku, Tokyo 113-8656, Japan

2Department of Chemistry & Biotechnology, School of Engineering, The University of Tokyo, Tokyo 113-8656, Japan

3Department of Materials Engineering, Graduate School of Engineering, The University of Tokyo, 7-3-1, Hongo, Bunkyo-ku, Tokyo 113-8656, Japan

4Faculty of Advanced Life Science, Hokkaido University, Sapporo 001–0021, Japan

‡These authors contributed equally to this work.

*Corresponding authors:

(S.I.) ishikawa@gel.t.u-tokyo.ac.jp

(T.S.) sakai@gel.t.u-tokyo.ac.jp

Figure S1. Chemical structure of PVAs. The degree of polymerization is 550, shown as n. The DSs are 74, 82, 88, and 98 mol%, implying that the ratios of x and y are 74:26, 82:18, 88:12, and 98:2, respectively.

Figure S2. 1H-NMR spectra of PVA98. a = δ 1.60 (m, 2H, CH2), b = δ 3.92 (m, 1H, CH), c = δ 2.00 (m, 3H, CH3).

Figure S3. 1H-NMR spectra of PVA88. a = δ 1.60 (m, 2H, CH2), b = δ 3.92 (m, 1H, CH), c = δ 2.00 (m, 3H, CH3).

Figure S4. 1H-NMR spectra of PVA82. a = δ 1.60 (m, 2H, CH2), b = δ 3.92 (m, 1H, CH), c = δ 2.00 (m, 3H, CH3).

Figure S5. 1H-NMR spectra of PVA74. a = δ 1.60 (m, 2H, CH2), b = δ 3.92 (m, 1H, CH), c = δ 2.00 (m, 3H, CH3).

Figure S6. GPC trace of PVA98 (black), PVA88 (red), PVA82 (blue), and PVA74 (orange). These traces were normalized so that the elution curves had the same peak intensity.