Stabilizing High-Humidity Perovskite Solar Cells with MoS2 Hybrid HTL

Puteri Nor Aznie Fahsyar 1,2*, Norasikin Ahmad Ludin2*, Noor Fadhilah Ramli2, Puteri Intan Zulaikha2, Suhaila Sepeai2, Ahmad Shah Hizam Md Yasir3

1Clean Technology Impact Laboratory, Taylor’s University, Selangor, Malaysia

2Solar Energy Research Institute, University Kebangsaan Malaysia, Selangor, Malaysia

3Faculty of Resilience, Rabdan Academy, Abu Dhabi, United Arab Emirates

*Corresponding authors: puteri.syedmahadzir@taylors.edu.my; sheekeen@ukm.edu.my

Supplementary documents

Fig. S1. MoS2 preparation using liquid exfoliation and solvent exchange process.

Fig. S2. Absorbance spectra of exfoliated MoS2 in NMP and IPA

Table S1. The values of all parameters of Raman peak shift.

| Sample | E12g (cm-1) | A1g (cm-1) | A1g -E12g (cm-1) | Thickness(nm) |
| --- | --- | --- | --- | --- |
| M1 | 381.6 | 404.6 | 23.0 | 9 |
| M2 | 381.1 | 405.1 | 24.0 | 29 |
| M3 | 380.6 | 405.6 | 25.0 | 45 |
| M4 | 380.1 | 406.5 | 26.4 | 65 |

Table S2. Summary of the bandgap for different concentrations of MoS2.

| Sample | Eg, eV |
| --- | --- |
| M0 | 1.59 |
| M1 | 1.59 |
| M2 | 1.58 |
| M3 | 1.60 |
| M4 | 1.61 |

Table S3. The values of all parameters of the fitted curves in the Nyquist plot.

| Sample | RS (Ω) | CPE1 (F) | RCT (Ω) | CPE2 (F) | RRec (Ω) |
| --- | --- | --- | --- | --- | --- |
| M0 | 72.67 | 7.948x10-7 | 223.27 | 5.440x10-5 | 368.7 |
| M1 | 62.46 | 9.159x10-7 | 280.7 | 9.101x10-4 | 1026 |
| M2 | 45.81 | 2.310x10-7 | 183.4 | 1.720x10-4 | 3983.5 |
| M3 | 111.22 | 6.847x10-8 | 390.4 | 5.430x10-5 | 874.6 |
| M4 | 145.58 | 1.184x10-6 | 588.56 | 1.523x10-4 | 5944 |

Table S4. Photovoltaic-performance parameters for M0 samples under 1 sun illumination (AM 1.5G, 100 mW cm−2) for PSC device at reverse scan direction.

| Time (hours) | Jsc (mA/cm2) | Voc (V) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| 0 | 16.6 | 0.92 | 0.54 | 8.3 |
| 24 | 15.8 | 0.83 | 0.54 | 7.1 |
| 48 | 15.0 | 0.80 | 0.52 | 6.3 |
| 72 | 14.3 | 0.77 | 0.38 | 4.2 |
| 96 | 10.6 | 0.70 | 0.27 | 2.0 |
| 120 | 8.1 | 0.61 | 0.24 | 1.2 |

Table S5. Photovoltaic-performance parameters for M1 samples under 1 sun illumination (AM 1.5G, 100 mW cm−2) for PSC device at reverse scan direction.

| Time (hours) | Jsc (mA/cm2) | Voc (V) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| 0 | 16.8 | 0.94 | 0.54 | 8.7 |
| 24 | 16.0 | 0.89 | 0.53 | 7.5 |
| 48 | 15.6 | 0.82 | 0.53 | 6.8 |
| 72 | 13.8 | 0.76 | 0.50 | 5.1 |
| 96 | 13.1 | 0.72 | 0.49 | 4.7 |
| 120 | 10.6 | 0.66 | 0.46 | 3.2 |

Table S6. Photovoltaic-performance parameters for M2 samples under 1 sun illumination (AM 1.5G, 100 mW cm−2) for PSC device at reverse scan direction.

| Time (hours) | Jsc (mA/cm2) | Voc (V) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| 0 | 17.2 | 0.97 | 0.57 | 9.5 |
| 24 | 16.8 | 0.91 | 0.57 | 8.7 |
| 48 | 15.7 | 0.87 | 0.57 | 7.9 |
| 72 | 15.2 | 0.82 | 0.57 | 7.1 |
| 96 | 14.8 | 0.78 | 0.56 | 6.5 |
| 120 | 14.0 | 0.68 | 0.55 | 5.2 |

Table S7. Photovoltaic-performance parameters for M3 samples under 1 sun illumination (AM 1.5G, 100 mW cm−2) for PSC device at reverse scan direction.

| Time (hours) | Jsc (mA/cm2) | Voc (V) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| 0 | 14.5 | 0.97 | 0.53 | 7.6 |
| 24 | 13.7 | 0.95 | 0.53 | 7.0 |
| 48 | 12.6 | 0.92 | 0.51 | 5.9 |
| 72 | 11.5 | 0.88 | 0.49 | 5.0 |
| 96 | 11.2 | 0.86 | 0.49 | 4.9 |
| 120 | 10.8 | 0.81 | 0.49 | 4.6 |

Table S8. Photovoltaic-performance parameters for M4 samples under 1 sun illumination (AM 1.5G, 100 mW cm−2) for PSC device at reverse scan direction.

| Time (hours) | Jsc (mA/cm2) | Voc (V) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| 0 | 14.2 | 0.97 | 0.50 | 6.9 |
| 24 | 13.1 | 0.94 | 0.49 | 6.0 |
| 48 | 12.4 | 0.90 | 0.47 | 5.1 |
| 72 | 11.9 | 0.87 | 0.47 | 4.9 |
| 96 | 10.9 | 0.85 | 0.47 | 4.5 |
| 120 | 10.5 | 0.84 | 0.47 | 4.3 |