Supplementary table 1. Viable cell count (Log CFU/mL) of C. albicans and S. mutans in dual-species biofilms formed on polymethylmethacrylate discs after exposure to test agents for 3 and 15 minutes and untreated control (N = 81).
	Groups
	Viable cell count (Log CFU/mL)

	
	C. albicans
	
	S. mutans

	
	3-minute
	
	15-minute
	
	3-minute
	
	15-minute

	
	Median
	Min
	Max
	
	Median
	Min
	Max
	
	Median
	Min
	Max
	
	Median
	Min
	Max

	2% CHX
	0.00
	0.00
	3.56
	
	0.00
	0.00
	3.76
	
	4.62
	0.00
	6.61
	
	0.00
	0.00
	4.31

	Compound 1
	4.62
	3.00
	6.02
	
	0.00
	0.00
	0.00
	
	6.61
	2.49
	7.15
	
	0.00
	0.00
	0.00

	Polident
	6.26
	6.10
	6.79
	
	0.00
	0.00
	4.92
	
	6.60
	5.92
	6.88
	
	0.00
	0.00
	0.00

	DW
	6.23
	6.17
	6.53
	
	6.05
	5.11
	6.12
	
	7.14
	6.98
	7.25
	
	6.59
	6.00
	7.11

	Control
	6.21
	5.61
	6.48
	
	6.21
	5.61
	6.48
	
	6.85
	6.48
	7.13
	
	6.85
	6.48
	7.13

	Biofilm assays were performed in triplicate in 3 independent experiments (n = 9).
CFU/mL: colony forming unit per milliliter; Min: minimum; Max: maximum; DW: distilled water; CHX: Chlorhexidine gluconate.
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