Supplementary Data

- Design Parameters of the Layers

Table S1 shows the design parameters of the three perovskite materials, two zinc ETLs and three HTLs used in this study to model the different PSC structures.

Table S1. Design Parameters of Materials

|  | ZnO | CdZnS | FAPbI3 | MASnI3 |
| --- | --- | --- | --- | --- |
| Thickness (nm) | 150 | 150 | 400 | 400 |
| Bandgap (eV) | 3.3 | 3.2 | 1.51 | 1.3 |
| Electron Affinity (eV) | 4.1 | 4.2 | 4 | 4.17 |
| Dielectric Permittivity | 9 | 9.12 | 6.6 | 8.2 |
| CB Effective Density of State(cm-3) | 4X1018 | 1.5X1018 | 1.2X1019 | 1X1018 |
| VB Effective Density of State(cm-3) | 1X1019 | 1.8X1019 | 2.9X1018 | 1X1018 |
| Electron Mobility (cm2/Vs) | 100 | 250 | 2.7 | 1.6 |
| Hole Mobility (cm2/Vs) | 25 | 40 | 1.8 | 1.6 |
| Donor Density ND (cm-3) | 1X1016 | 1X1016 | 1X109 | 1X1014 |
| Acceptor Density NA (cm-3) | - | - | 1X109 | 1X1014 |
|  | MAGeI3 | CBTS | CNTS | CZTS |
| Thickness (nm) | 400 | 150 | 150 | 150 |
| Bandgap (eV) | 1.9 | 1.9 | 1.74 | 1.45 |
| Electron Affinity (eV) | 3.98 | 3.6 | 3.87 | 4.5 |
| Dielectric Permittivity | 10 | 5.4 | 9 | 9 |
| CB Effective Density of State(cm-3) | 1x1016 | 2.2X1018 | 2.2X1018 | 2.2X1018 |
| VB Effective Density of State(cm-3) | 1x1015 | 1.8X1019 | 1.8X1019 | 1.8X1019 |
| Electron Mobility (cm2/Vs) | 16.2 | 30 | 11 | 60 |
| Hole Mobility (cm2/Vs) | 10.1 | 10 | 11 | 20 |
| Acceptor Density NA (cm-3) | 1x109 | - | - | - |
| Acceptor Density NA (cm-3) | 1x109 | 1X1015 | 1X1016 | 1X1018 |

Table S2 shows the work function values of the different materials that can be utilized as electrodes in the PSCs

.

Table S2.

| Materials | Al | Cu | Ag | Fe | C | Au | Pd | Ni | Pt |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ∅ (eV) | 4.3 | 4.65 | 4.7 | 4.8 | 5 | 5.1 | 5.3 | 5.5 | 5.65 |

- SCAPS-1D Equations

The poison equation governs the electric field of a p-n junction (E) and the charge density (ρ) in the semiconductor material and is given by:

|  | ∂2φ∂2x=-∂E∂x=-ρεS=-q εS [p-n ND+x- NA-± Ndef(x) | (1) |
| --- | --- | --- |

Where φ = electrostatic potential, q = elementary charge, εS= relative permittivity, n & p = electron and hole density respectively, are ND+ = donor density, NA- = acceptors density, and Ndef = defect density due to trapped charged carriers.

The continuity equation governs the generation, recombination, drift and diffusion mechanism of charge carrier concentration and is given by:

|  | ⅆpnⅆt=Gp-pn-pn0τp + pnμpdξdx+ μpξⅆpnⅆx+ Dpⅆ2pnⅆx2 | (2) |
| --- | --- | --- |
|  | ⅆnpⅆt=Gn-np-np0τn + npμndξdx+ μnξⅆnpⅆx+ Dnⅆ2npⅆx2 | (3) |

WhereGn, Gp = generation rate of charge carriers, ξ = electric field, μn & μp = carrier mobilities, Dn & Dp = carrier diffusion coefficient, τn& τp = carrier lifetime.

Carrier transport occurs by drift and diffusion and is given by:

|  | Jn=qnμnE+qDn ∂n∂x | (4) |
| --- | --- | --- |
|  | Jp=qnμpE+qDp ∂p∂x | (5) |

Where Jn and Jp = carriers’ current densities.

Open circuit Voltage:

|  | VOC= nkTq[ln⁡(ILIO+1)] | (6) |
| --- | --- | --- |

Where  kTq = thermal voltage, IL = light-generated current and IO = saturation current.

Fill Factor:

|  | FF=PmaxPt=Vmax ImaxVOC ISC | (7) |
| --- | --- | --- |

Power Conversion Efficiency:

|  | PCE=VOC ISC FFPin | (8) |
| --- | --- | --- |

- Band Offset Values

Figure S1 shows the conduction band offset and valance band offset formed by the different charge transport layers with the three distinct perovskite materials.

Figure S1. VBO and CBO of CTL with the Perovskites.

- Optimized Thickness Values

Figure S2 shows the effect of the zinc ETLs and absorber thickness on the performance of the PSC. While S2 show the effect of kesterite HTLs on the performance.

Figure S2. Effect of zinc ETLs and absorber thickness on the performance of the PSC

Figure S3. Effect of Kesterite HTLs and absorber thickness on the performance of the PSC