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	Cell type/response
	Score

	
	0
	1
	2
	3
	4

	Collagen Formation / Deposition
	0
	Collagen formation occupying up to 10% of the defect 
	Collagen formation occupying from 11 to 20% of the defect
	Collagen formation occupying from 20 to 30% of the defect
	Collagen formation occupying more than 35% of the defect

	Fibrosis 
	0
	Minimal narrow band along the defect 
	Mild thick band along the defect
	Moderate thick band along the defect
	Extensive marked thick band along the defect

	Non-Trabecular Bone formation (healing)
	None to minimal non-trabecular bone around the defect edges
	Minimal to slight non-trabecular bone around the defect edges (< 10% of defect length, approximated). Non or minimal focal isolated bone formation at the defect


	Minimal to slight non-trabecular bone around the defect edges (10- 33% of defect length, approximated). Minimal to slight focal isolated bone formation at the defect

	Minimal to slight non-trabecular bone around the defect edges (>33% of defect length, approximated). Slight to moderate focal to multifocal isolated bone formation at the defect

	Severe non-trabecular bone formation and complete defect healing. 

	Trabecular Bone Formation including cavity with bone marrow 
	Absence 
	Minimal focal presence of trabecular bone at the defect 
	Mild focal to multifocal presence of trabecular bone at the defect
	Moderate multifocal presence of trabecular bone at the defect
	Severe multifocal presence of trabecular bone at the defect

	Amount of bone graft occupying the defect
	0
	Up to 10% of the defect
	From 11 to 20% of the defect
	From 20 to 30% of the defect
	More than 30% of the defect 




