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	Treatment 
	Sample ID
 
	Host Reaction
	Additional Parameters

	
	
	Polymorphonuclear cells
	Lymphocytes
	Plasma cells
	Macrophages
	Giant cells
	Necrosis
	Subtotal (x2)
	 Hemorrhage
	Neovascularization
	Hemosiderin 
	Edema
	Subtotal 
	Total Host Reaction 
	Non-Trabecular Bone (healing)
	Trabecular Bone Formation
	Fibrosis 
	Collagen 
	Bone Graft Amount

	BG
	8L
	0
	3
	0
	3
	0
	0
	12
	0
	2
	0
	0
	2
	14
	0
	0
	n.a*
	n.a*
	2

	
	8R
	0
	1
	0
	3
	0
	0
	8
	0
	3
	0
	0
	3
	11
	1
	0
	n.a*
	n.a*
	2

	
	9L
	0
	2
	0
	3
	0
	0
	10
	0
	2
	2
	0
	4
	14
	0
	0
	n.a*
	n.a*
	4

	
	27L
	1
	3
	0
	2
	0
	0
	12
	2
	3
	0
	0
	5
	17
	0
	0
	n.a*
	n.a*
	2

	
	11R
	1
	3
	0
	3
	0
	0
	14
	4
	2
	4
	0
	10
	24
	0
	0
	n.a*
	n.a*
	2

	cBG
	25L
	0
	2
	0
	2
	0
	0
	8
	2
	2
	1
	0
	5
	13
	2
	1
	n.a*
	n.a*
	1

	
	25R
	1
	2
	0
	3
	0
	0
	12
	3
	2
	2
	0
	7
	19
	0
	0
	n.a*
	n.a*
	1

	
	26R
	1
	3
	0
	2
	0
	0
	12
	1
	2
	1
	0
	4
	16
	0
	0
	n.a*
	n.a*
	1

	
	26L
	0
	2
	0
	1
	0
	0
	6
	2
	3
	1
	0
	6
	12
	1
	0
	n.a*
	n.a*
	1

	
	27R
	n.a**
	n.a**
	n.a**
	n.a**
	n.a**
	n.a**
	n.a
	n.a**
	n.a**
	n.a**
	n.a**
	n.a
	n.a
	1
	0
	n.a*
	n.a*
	n.a



n.a.: not applicable 
n.a.*: Collagen formation / deposition cannot be separated from fibrosis as of the used collagen tape. 
n.a.**: Cellularity not visible. 
Additional Remarks:
25R - Focal adherence of fibrous tissue to the brain.
27R - Section slightly to the side. Scoring was adapted to reflect less central sectioning level of the defect, as the defect diameter/distance will be less and the healing is more prominent on the sides. 


