Supplemental Information for: Production and purification of 43Sc and 47Sc from enriched [46Ti]TiO2 and [50Ti]TiO2 targets

Shelbie J. Cingoranellia,b, Jennifer L. Bartelsb, Pavithra H. A. Kankanamalagec, C. Shaun Lovelessb, David A. Rotschc,d Suzanne E. Lapia,b*

aDepartment of Chemistry, University of Alabama at Birmingham

bDepartment of Radiology, University of Alabama at Birmingham

cPhysics Division, Argonne National Laboratory

dRadioisotope Science and Technology Division, Oak Ridge National Laboratory

* Corresponding author; E-mail: lapi@uab.edu. Telephone (205) 975-8689. Address 1924 6th Ave. S., WTI 310F, Birmingham, AL 35244.

Table of Contents

  - Relevant characteristics of 68Ga, 177Lu and 43,44g,47Sc

  - Radionuclides produced from proton bombardment of natTi targets

  - Isotopic purity of enriched materials

  - Certificate of Analysis of enriched materials

  - Cross section measurements of 46Ti(p,α)43Sc and 50Ti(p,α)47Sc

  - Cross sections of proton induced reactions on natTi

  - Schematic of the radioscandium purification method

  - Inductively Coupled Plasma-Mass Spectrometry

  - Radiolabeling conditions and iTLC

  - Phantom dimension

  - Average radioactivity per elution of purification

  - Enriched 46Ti and 50Ti recovery

  - The apparent molar activity curves for [43Sc]Sc-DOTA and [47Sc]Sc-DOTA

  - Relevant characteristics of 68Ga, 177Lu and 43,44g,47Sc

Table S1: Characteristics of the radioisotopes of Ga, Lu and Sc.1,2

| Radioisotope | Half-life | [β+/-] mean energy (keV) | Additional γ (branching ratio %) |
| --- | --- | --- | --- |
| 68Ga | 68 min | 829.5 (88.9%): [β +] | 1077.3 (3.22) |
| 43Sc | 3.9 h | 476.0 (88.1%): [β +] | 372.9 (22.5) |
| 44gSc | 3.9 h | 632.0 (94.3%): [β +] | 1157.0 (99.9) |
| 177Lu | 6.6 d | 133.6 (100.0%): [β -] | 112.9 (6.23) & 208.4 (10.4) |
| 47Sc | 3.3 d | 162.0 (100.0%): [β -] | 159.3 (68.3) |

  - Radionuclides produced from proton bombardment of natTi targets

Table S2: Products from proton irradiation of natTi.1-3

| Isotope | Nuclear reaction | Half-life | Decay mode | Key gamma rays |
| --- | --- | --- | --- | --- |
| 43Sc | 46Ti(p,α)43Sc | 3.9 h | β+ | 372 (22.5%) |
| 44gSc | 47Ti(p,α)44gSc | 3.9 h | β+ | 1157 (99.9%) |
| 44mSc | 47Ti(p,α)44mSc | 58.6 h | IT : 98.8% ε: 1.2% | 271 (86.74%) |
| 46Sc | 47Ti(p,2p)46Sc 49Ti(p,α)46Sc 50Ti(p,n+α)46Sc | 83.7 d | β- | 889 (99.98%) 1120(99.98%) |
| 47Sc | 48Ti(p,2p)47Sc 50Ti(p,α)47Sc | 3.9 d | β- | 159 (68.3%) |
| 48Sc | 49Ti(p,2p)48Sc | 48.6 h | β+ | 175 (7.48%) |
|  |  |  |  | 983 (100%) |
|  |  |  |  | 1037 (97.6%) |
|  |  |  |  | 1212 (2.38%) |
|  |  |  |  | 1312 (100%) |
| 48V | 48Ti(p,n)48V 49Ti(p,2n)48V | 15.9 d | β+ | 944 (7.87%) 983 (98.98%) |
|  |  |  |  | - (98.2%) |

c. Isotopic purity of enriched materials

| Table S3: The isotopic enrichment of [46Ti]TiO2 and [50Ti]TiO2. All materials were provided by the National Isotope Development Center, USA. |  |  |
| --- | --- | --- |
| Enrichment of xTiO2 |  |  |
| XTi Isotope | Isotopic Abundance in [46Ti]TiO2 | Isotopic Abundance in [50Ti]TiO2 |
| 46 | 96.84 | 1.69 |
| 47 | 0.5 | 1.29 |
| 48 | 2.33 | 12.51 |
| 49 | 0.16 | 1.41 |
| 50 | 0.16 | 83.1 |

- Isotopic purity of enriched materials

Table S4: The Certificates of Analysis (CoA) of [46Ti]TiO2 and [50Ti]TiO2, measured in ppm. Both the materials and the CoA were provided by the National Isotope Development Center, USA.

| Element: ppm | 46Ti | 50Ti | Element: ppm | 46Ti | 50Ti | Element: ppm | 46Ti | 50Ti |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ag | <50 | <50 | Mg | <100T | <100T | Lanthanides and Actinides |  |  |
| Al | <100T | <200T | Mn | <100 | <100 | Ce | <1000 | <1000 |
| Au | <500 | <500 | Mo | <100 | <100 | Dy | <1000 | <1000 |
| B | <100T | <100T | Na | <=100 | 1000 | Er | <50 | <50 |
| Ba | <100 | <100 | Nb | <500 | <500 | Eu | <50 | <50 |
| Be | <10 | <10 | Ni | <100 | <200 | Gd | <200 | <200 |
| Bi | <200 | <200 | Pb | <200 | <200 | Ho | <500 | <500 |
| Ca | <100 | 100 | Pt | <500 | <500 | La | <200 | <200 |
| Cd | <500 | <500 | Rb | <200 | <20 | Lu | <50 | <50 |
| Co | <100 | <200 | Sb | <500 | <500 | Nd | <500 | <500 |
| Cr | <100 | <200 | Si | 300 | <=100 | Pr | <500 | <500 |
| Cs | <500 | <500 | Sn | <100 | <200 | Sm | <500 | <500 |
| Cu | 200 | 200 | Sr | <100 | <100 | Tb | <500 | <500 |
| Fe | <100 | 500 | Ta | <500 | <500 | Y | <50 | <50 |
| Ga | <200 | <200 | Te |  | <500 | Yb | <20 | <20 |
| Ge | <200 | <200 | Ti | M | M | Tm | <500 | <500 |
| Hf | <500 |  | V | <100 | <200 |  |  |  |
| Hg | <500 | <500 | W | <500 | 1000 |  |  |  |
| In | <500 |  | Zn | <2000 | <500 |  |  |  |
| K | <100 | <100 | Zr | <200T | <200 |  |  |  |
| Li | BUFFER* | <50 |  |  |  |  |  |  |

*Was added during analysis. No values were obtained.

Where: M is major; T is trace; <= less than/equal; < is less than, nd is not detected; and elements listed without values were not detected or less than 10 ppm.

e. Cross section measurements of 46Ti(p,α)43Sc and 50Ti(p,α)47Sc

Figure S1: Excitation function for 46Ti(p,α)43Sc with the red lines indicating the relevant energy range during bombardment at 18 MeV (A).4-6. Excitation function for 50Ti(p,α)47Sc with the red lines indicating the relevant energy range during bombardment at 24 MeV(B).6,7

f. Cross sections of nuclear reactions from proton irradiation on natTi.

Figure S2: Representative cross sections of nuclear reactions occurring during 0-30 MeV proton irradiations on natTi targetes.4,5,7 Cross sections were imported from EXFOR and used to calculate the theoretical yields during irradiations as well as determine the optimal bombardment parameters. (A) 43Sc production via 46Ti(p,α) 43Sc. (B) 44g/mSc production  via 47Ti(p,α)44g/mSc. (C) The production of 47Sc via 48Ti(p,2p)47Sc and 50Ti(p,α)47Sc. (D) 48Sc production via 49Ti(p,2p)48Sc. (E) 48V production via 48Ti(p,n)48V. (F) Production of 46Sc from 49Ti(p,α)46Sc, 47Ti(p,2p)46Sc and 50Ti(p,n+α)46Sc.

g. Schematic of the radioscandium purification method

Figure S3: Optimized radioscandium purification method. Flow Through (FT) is the dissolved target solution. E1-E3 are three different washes for the removal of impurities as well as column conditioning. E4-E6 are the radioscandium elution fractions.

- Inductively Coupled Plasma – Mass Spectrometry (ICP-MS)

Table S5: The list of monitored elements for each target material used and separation performed.

| Transition metals |  | Lanthanides and Actinides |  | Other |
| --- | --- | --- | --- | --- |
| Sc | Fe | Ce | Dy | Al |
| Ti | Co | Pr | Ho | Ge |
| V | Ni | Nd | Er | Ga |
| Cr | Cu | Sm | Tm | Pb |
| Mn | Zn | Eu | Yb | Ca |
| Zr | W | Gd | Lu |  |
| Nb | Ta | Tb | U |  |

- Radiolabeling conditions and iTLC

1,4,7,10-tetraazacyclododecana-1,4,7,10-tetraacetic acid (DOTA) was dissolved in 0.25 M ammonium acetate buffer, pH 4.5, to produce a 10 mg/mL concentration stock. This was further diluted in the same buffer to final volumes of 100 µL with DOTA concentrations provided in Table S6. Subsequently, either 43Sc, 3.7 MBq (100 µCi) or 47Sc, 2.3 MBq (62.5 µCi) was added to the vials, which were incubated at 95 oC for 30 min. The resulting samples were spotted onto iTLC-SG paper (Agilent) and the paper was developed in 1 M citric acid. The iTLC strips were analyzed on an AR-2000 instrument using Winscan software (Eckert and Ziegler). In the analysis, the DOTA complex exhibited an RF of 0.65, while free 4xSc migrated with the solvent front, as illustrated in Figure S4. To determine the apparent molar activity, the EC50 value of the DOTA titration was used to calculate the µmol for total binding. The average activity used for each vial, adjusted for decay, was then divided by this value.

| Table S6: The serial dilution of DOTA. |  |  |  |
| --- | --- | --- | --- |
| Vial | Volume buffer | Serial dilution volume | Final concentration of DOTA(nmol) |
| 1 | 135 | 15 µL from 10 mg/mL stock | 247 |
| 2 | 100 | 50 µL from 1 | 82.4 |
| 3 | 100 | 50 µL from 2 | 27.5 |
| 4 | 100 | 50 µL from 2 | 9.16 |
| 5 | 100 | 50 µL from 4 | 3.05 |
| 6 | 100 | 50 µL from 5 | 1.02 |
| 7 | 100 | 50 µL from 6 | 0.34 |
| 8 | 100 | 50 µL from 7 | 0.11 |
| 9 | 100 | 50 µL from 8 | 0.04 |
| 10 | 100 | 50 µL from 9 | 0.01 |
| Discard | 0 | 50 µL from 10 | 0.00 |

Figure S4: The radio-iTLC of [47Sc]Sc-DOTA at 0.24 μmol DOTA concentration, RF = 0.65 (A). The radio-iTLC of free [47Sc]ScCl3 in 0.1 M HCl, RF = 1. (B) The red lines mark the origin at 10 mm and solvent front at 140 mm.

- PET phantom dimensions

Figure S5: Schematic of the rod alignment and rod diameter of the phantom used for PET resolution comparison of three radionuclides: 18F, 43Sc and 68Ga. The dashed line represents intensity plot line that was drawn to gather the Full-width at half-maximum data.

A phantom composed of PMMA with rod diameters of 1.2, 1.6, 2.4, 3.2, 4.0 and 4.8 mm with a height of 3.4 cm, with the alignment represented in figure S5. The insert diameter was 4.4 cm, the cylinder outside diameter was 5 cm, the cylinder inside diameter was 4.5 cm, and the cylinder inside height was 6.3 cm.

- Average activity per elution of purification

Table S7: Average activity per elution for a 1.5 hour bombardment (n=3) on [46Ti] and 4 hour bombardment (n=3) on [50Ti], where DT stands for Dissolved Target and FT stands for Flow-through

| Target | [46Ti]TiO2 |  |  |  | [50Ti]TiO2 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Elutions | 43Sc MBq (mCi) | SD | 48V in MBq (μCi) | SD | 47Sc MBq (mCi) | SD | 48V in MBq (μCi) | SD |
| DT | 510 | 21.8 (0.59) | 2.51 | 0.29 (7.7) | 52.17 | 2.35 (0.06) | 8.29 | 4.29 (116) |
|  | (13.8) |  | (67.6) |  | (1.42) |  | (224) |  |
| FT | 27.8 | 6.29 (0.17) | 0.93 | 0.09 (2.3) | 1.95 | 0.72 (0.02) | 5.76 | 3.48 (94.1) |
|  | (0.75) |  | (25) |  | (0.05) |  | (156) |  |
| E1 | 4.07 | 2.59 (0.07) | 1.55 | 0.58 (15.7) | 0.18 | 0.14 (<0.01) | 1.69 | 0.132 (8.85) |
|  | (0.11) |  | (41.9) |  | (<0.01) |  | (45.5) |  |
| E2 | 15.17 | 1.48 (0.4) | 1.18 | 0.22 (5.8) | 0.26 | 0.34 (0.01) | 2.04 | 0.24 (6.62) |
|  | (0.41) |  | (32) |  | (0.01) |  | (55.1) |  |
| E3 | 1.85 | 0.74 (0.02) | 0 | 0 0 | 0.08 | 0.02 (<0.01) | 0.04 | 0.34 (0.94) |
|  | (0.05) |  | 0 |  | (<0.01) |  | (0.09) |  |
| E4 | 473 | 4.44 (0.12) | 0 | 0 0 | 47.8 | 6.3 (0.11) | 0 | 0 0 |
|  | (12.8) |  | 0 |  | (1.27) |  | 0 |  |
| E5 | 3.7 | 2.96 (0.08) | 0 | 0 0 | 1.32 | 0.54 (0.01) | 0 | 0 0 |
|  | (0.1) |  | 0 |  | (0.04) |  | 0 |  |
| E6 | 4.81 | 0 0 | 0 | 0 0 | 0.19 | 0.08 (<0.01) | 0 | 0 0 |
|  | (0.13) |  | 0 |  | (0.01) |  | 0 |  |

- Enriched 46Ti and 50Ti recovery

Figure S6: The percent recovery of the enriched [50Ti]TiO2 target for each run cycle, consisting of bombardment, processing, and recycling (A). The percent recovery for enriched [46Ti]TiO2 target for each run cycle, consisting of bombardment, processing, and recycling (B).

- The apparent molar activity curves for [43Sc]Sc-DOTA and [47Sc]Sc-DOTA

Figure S7: The apparent molar activity curve for the complexation of [43Sc]Sc-DOTA, where the complexation is represented by % complex as a function of the concentration of DOTA (A). The apparent molar activity curve for the complexation of [47Sc]Sc-DOTA, where the complexation is represented by % complex as a function of the concentration of DOTA (B).

Reference

1	NuDat 2.8. Brookhaven National Laboratory website. https://nndc.bnl.gov/nudat2/. Data extracted June 2, 2021. Accessed January 1, 2022

2	Chernysheva, M. et al. Accelerator Production of Scandium Radioisotopes: Sc-43, Sc-44, and Sc-47. Curr Radiopharm 14, 359-373, doi:10.2174/1874471014999210112205535 (2021).

3	Loveless, C. S. et al. Cyclotron Production and Separation of Scandium Radionuclides from Natural Titanium Metal and Titanium Dioxide Targets. Journal of Nuclear Medicine 62, 131-136, doi:10.2967/jnumed.120.242941 (2021).

4	Carzaniga, T. S. et al. Measurement of (43)Sc and (44)Sc production cross-section with an 18MeV medical PET cyclotron. Appl Radiat Isot 129, 96-102, doi:10.1016/j.apradiso.2017.08.013 (2017).

5	Levkovski, V. N. Cross sections of medium mass nuclide activation (A=40-100) by medium energy protons and alpha-particles (E=10-50 MeV). Atomnaya Energiya 69, 180 (1991).

6	Otuka, N. et al. Towards a More Complete and Accurate Experimental Nuclear Reaction Data Library (EXFOR): International Collaboration Between Nuclear Reaction Data Centres (NRDC). Nuclear Data Sheets 120, 272-276, doi:https://doi.org/10.1016/j.nds.2014.07.065 (2014).

7	Gadioli, E., Gadioli Erba, E., Hogan, J. J. & Burns, K. I. Emission of alpha particles in the interaction of 10–85 MeV protons with48,50Ti. Zeitschrift für Physik A Atoms and Nuclei 301, 289-300, doi:10.1007/BF01421692 (1981).