Supplementarny materials.

# Bioactive and biodegradable cotton fabrics produced via synergic effect of plant extracts and essential oils in chitosan coating system

# Bolesław Szadkowski1,*, Magdalena Śliwka-Kaszyńska2, Anna Marzec1,*

1Institute of Polymer and Dye Technology, Faculty of Chemistry, Lodz University of Technology, Stefanowskiego 16, 90-537 Lodz, Poland

2Department of Organic Chemistry, Faculty of Chemistry, Gdansk University of Technology, Narutowicza 11/12, 80-233 Gdansk, Poland

*boleslaw.szadkowski@p.lodz.pl and anna.marzec@p.lodz.pl

Figure S1. FTIR spectra of the studied cotton fabrics.

Figure S2. N1s XPS spectra of the studied cotton fabrics.

| Sample name | %N |
| --- | --- |
| CF | 0.5 |
| CF/CS | 1.2 |
| CF/CS/AV/CEO | 1.1 |

Table S1. Nitrogen elemental analysis of the studied cotton fabrics obtained from XPS experiment.