Microwave-Assisted Synthesis, Characterization and in vitro Biomedical Applications of Hibiscus rosa-sinensis Linn.-mediated Carbon Quantum Dots

Shweta Yalshetti1, Bothe Thokchom1, Santosh Mallikarjun Bhavi1, Sapam Riches Singh1, Sneha R. Patil1, B. P. Harini2, Mika Sillanpää3, J. G. Manjunatha4, B. S. Srinath5, Ramesh Babu Yarajarla1*

1Drosophila and Nanoscience Research Laboratory, Department of Applied Genetics, Karnatak University, Dharwad, Karnataka 580003, India.

2Department of Zoology, Bangalore University, Bangalore, Karnataka 560056, India.

3Department of Biological and Chemical Engineering, Aarhus University, Norrebrogade 44, 8000 Aarhus C, Denmark.

4Department of Chemistry, FMKMC College, Mangalore University Constituent College, Madikeri, Karnataka 571201, India.

5Department of Microbiology and Biotechnology, Bangalore University, Bangalore, Karnataka 560056, India.

*Corresponding author:  Ramesh Babu Yarajarla

Drosophila and Nanoscience Research Laboratory, Department of Applied Genetics, Karnatak University, Dharwad, Karnataka 580003, India

E-mail: rameshy@kud.ac.in

Figure S1: MTT assay images of L929 cells treated with different concentrations of CQDs and plant extract, with cisplatin as standard control; PE stands for plant extract

Figure S2: MTT assay images of HaCaT cells treated with different concentrations of CQDs along with bar graph. Bars represent mean ± SD (nsp > 0.05, n = 4)

Figure S3: Flow cytometry dot plots (FSC vs SSC and Annexin V-FITC vs PI) of unstained, Annexin V-FITC only stained, PI only stained, control (untreated) and CQDs treated HaCaT cells

Figure S4: Scratch wound healing of untreated and 250 g mL-1 CQDs treated HaCaT cells after 24 h and its respective graph. Bars represent mean ± SD, n = 3

Figure S5: Colony counting assay: colonies of B. cereus and K. pneumoniae after 12 h culture with specific concentrations of CQDs, PE and 50 g mL-1 kanamycin. PE = plant extract; (100), (125) and (150) represent the concentration of CQDs and plant extract in g mL-1

Table S1: Cytotoxicity of CQDs against L929 cells compared with plant extract

| Sample | Concentration (g mL-1) | Cytotoxicity test by MTT assay |  |
| --- | --- | --- | --- |
|  |  | Cell viability (%) | IC50 (g mL-1) |
| CQDs | 100 | 76.12 ± 0.1064 | 314.01 |
|  | 200 | 62.58 ± 0.6385 |  |
|  | 300 | 49.51 ± 0.0461 |  |
|  | 400 | 41.85 ± 0.0532 |  |
|  | 500 | 28.08 ± 0.0355 |  |
| Plant extract | 100 | 78.80 ± 0.1596 | 356.02 |
|  | 200 | 67.95 ± 0.0320 |  |
|  | 300 | 55.37 ± 0.2483 |  |
|  | 400 | 43.92 ± 0.4966 |  |
|  | 500 | 35.19 ± 0.5676 |  |
| Cisplatin | 15 | 45.02 ± 0.1064 | - |

The results were analysed using one-way ANOVA (p < 0.05) and are expressed as mean ± SEM, n = 3

Table S2: Data of wound closure analyzed using ImageJ

| Cell | Label | Area (unit2) | Area % | Width (unit) | Standard deviation (unit) | Wound Closure % |
| --- | --- | --- | --- | --- | --- | --- |
| L929 | Untreated 0 h | 0.625 | 10.006 | 0.246 | 0.019 | 0 |
|  | Untreated 12 h | 0.62 | 9.919 | 0.245 | 0.011 | 0.8 |
|  | Untreated 24 h | 0.618 | 9.896 | 0.242 | 0.011 | 1.12 |
|  | Standard 0 h | 0.928 | 14.847 | 0.371 | 0.02 | 0 |
|  | Standard 12 h | 0.54 | 8.645 | 0.221 | 0.045 | 41.81034 |
|  | Standard 24 h | 0.003 | 0.053 | 0.023 | 0.023 | 99.67672 |
|  | Plant Extract 0 h | 0.921 | 14.737 | 0.365 | 0.031 | 0 |
|  | Plant Extract 12 h | 0.886 | 14.173 | 0.357 | 0.04 | 3.800217 |
|  | Plant Extract 24 h | 0.86 | 13.76 | 0.346 | 0.033 | 6.623236 |
|  | CQDs 0 h | 0.764 | 12.223 | 0.306 | 0.028 | 0 |
|  | CQDs 12 h | 0.374 | 5.983 | 0.156 | 0.048 | 51.04712 |
|  | CQDs 24 h | 0.001 | 0.016 | 0.015 | 0.012 | 99.87 |
| HaCaT | Untreated 0 h | 1075006 | 10.915 | 411.555 | 122.306 | 0 |
|  | Untreated 24 h | 680623 | 6.911 | 266.628 | 105.242 | 36.6866 |
|  | CQDs 0 h | 1349017 | 13.697 | 490.372 | 56.709 | 0 |
|  | CQDs 24 h | 289011 | 2.934 | 189.878 | 87.412 | 78.5761 |

Table S3: Percentage wound closure observed in L929 Cell line

| Cell line | Treatment | Concentration (In µg mL-1) | Wound Closure at 12 h (%) | Wound Closure at 24 h (%) |
| --- | --- | --- | --- | --- |
| L929 | Untreated | 0 | 0.8 | 1.12 |
|  | Standard Ascorbic Acid | 15 | 41.81 | 99.68 |
|  | Plant Extract | 35.60 | 3.8 | 6.62 |
|  | Carbon Quantum Dots | 31.40 | 51.05 | 99.87 |
| HaCaT | Untreated | 0 | - | 39.45 |
|  | Carbon Quantum Dots | 250 | - | 57.59 |

Table S4: Anti-inflammatory effect of CQDs compared with plant extract and aspirin

| Sample | Concentration (g mL-1) | Anti-inflammatory assay by protein denaturation |  |
| --- | --- | --- | --- |
|  |  | % of inhibition | IC50 (g mL-1) |
| CQDs | 50 | 23.78 ± 2.2001 | 106.20 |
|  | 100 | 35.15 ± 2.8596 |  |
|  | 150 | 56.51 ± 3.3064 |  |
|  | 200 | 73.65 ± 3.5299 |  |
|  | 250 | 89.42 ± 3.7487 |  |
| Plant extract | 50 | 18.28 ± 2.9017 | 187.28 |
|  | 100 | 33.09 ± 3.3459 |  |
|  | 150 | 48.68 ± 3.0251 |  |
|  | 200 | 60.32 ± 3.6843 |  |
|  | 250 | 73.33 ± 2.3999 |  |
| Aspirin | 50 | 35.47 ± 2.1572 | 93.41 |
|  | 100 | 54.04 ± 2.7353 |  |
|  | 150 | 67.61 ± 3.0314 |  |
|  | 200 | 78.47 ± 3.1401 |  |
|  | 250 | 94.03 ± 2.908 |  |

The results were analysed using one-way ANOVA (p < 0.05) and are expressed as mean ± SEM, n = 3

Table S5: Antibacterial activity of CQDs and plant extract

| Bacteria | Zone of Inhibition (in mm) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Kanamycin (50 g) | CQDs |  |  | Plant extract |  |  |
|  |  | 100g | g | 150g | 100g | g | 150g |
| Bacillus cereus | 24.08 ± 0.3700 | 19.20 ± 0.4580 | 22.56 ± 0.6537 | 24.91 ± 1.2581 | 15.21 ± 0.2890 | 18.62 ± 0.8875 | 18.75 ± 0.1230 |
| Klebsiella pneumoniae | 23.82 ± 0.4966 | 16.77 ± 0.0261 | 19.96 ± 0.0367 | 22.57 ± 0.7426 | 13.86 ± 0.5754 | 15.45 ± 0.3685 | 16.99 ± 0.1363 |

The results are expressed as mean ± SEM, n = 3