Supporting information

Selective Recovery of Pyrolyzates of Biodegradable (PLA, PHBH) and Common Plastics (HDPE, PP, PS) During Co-pyrolysis Under Slow Heating

Wakana Adachi1, Shogo Kumagai1,2 *, Zhuze Shao1, Yuko Saito1, Toshiaki Yoshioka1

1 Graduate School of Environmental Studies, Tohoku University, 6-6-07 Aoba, Aramaki-aza, Aoba-ku, Sendai, Miyagi 980-8579, Japan

2 Graduate School of Engineering, Tohoku University, 6-6-07 Aoba, Aramaki-aza, Aoba-ku, Sendai, Miyagi 980-8579, Japan

*Corresponding author. E-mail address: kumagai@tohoku.ac.jp (S. Kumagai).

Table S1 The summary of start, end, and peak-top temperatures of all the samples obtained by DTG

| Plastics | Temperature [°C] |  |  |
| --- | --- | --- | --- |
|  | Ts*1 | Tf*2 | Tp*3 |
| PLA | 325 | 378 | 368 |
| PHBH | 273 | 298 | 294 |
| HDPE | 458 | 499 | 484 |
| PP | 422 | 478 | 465 |
| PS | 386 | 444 | 417 |
| *1 Temperature at DTG = 5 wt%/min after weight loss start, *2 Temperature at DTG = 5 wt%/min before weight loss finish, *3 Temperature at the maximum DTG |  |  |  |

Table S2 The peak-top temperatures of all the samples obtained by EGA-MS (TIC)

| Samples | 1st peak temperature [°C] | 2nd peak temperature [°C] |
| --- | --- | --- |
| PLA | 364 |  |
| PHBH | 293 |  |
| HDPE | 478 |  |
| PP | 457 |  |
| PS | 411 |  |
| PLA10HDPE90 | 362 | 479 |
| PLA20HDPE80 | 357 | 476 |
| PLA50HDPE50 | 363 | 478 |
| PLA10PP90 | 356 | 457 |
| PLA20PP80 | 361 | 458 |
| PLA50PP50 | 362 | 457 |
| PLA10PS90 | 370 | 413 |
| PLA20PS80 | 370 | 414 |
| PLA50PS50 | 363 | 414 |
| PHBH10HDPE90 | 289 | 479 |
| PHBH20HDPE80 | 290 | 477 |
| PHBH50HDPE50 | 289 | 477 |
| PHBH10PP90 | 290 | 455 |
| PHBH20PP80 | 289 | 459 |
| PHBH50PP50 | 288 | 456 |
| PHBH10PS90 | 290 | 413 |
| PHBH20PS80 | 286 | 411 |
| PHBH50PS50 | 293 | 411 |

Figure S1 TG (a) and DTG (b) curves of PLA20HDPE80, PLA20PP80, and PLA20PS80.

Figure S2 TG (a) and DTG (b) curves of PLA10HDPE90, PLA10PP90, PLA10PS90

Figure S3 TG (a) and DTG (b) curves of PHBH20HDPE80, PHBH20PP80, PHBH20PS80

Figure S4 TG (a) and DTG (b) curves··of PHBH10HDPE90, PHBH10PP90, PHBH10PS90

Figure S5 TIC and EICs of PLA+HDPE

Figure S6 TIC and EICs of PLA+PP

Figure S7 TIC and EICs of PLA+PS

Figure S8 TIC and EICs of PHBH+HDPE

Figure S9 TIC and EICs of PHBH+PP

Figure S10 TIC and EICs of PHBH+PS