## Efficient arsenic removal from water using iron-impregnated low-temperature biochar derived from henequen fibers: Performance, mechanism, and LCA analysis

Xu Liao1, Raúl Miranda Avilés2,3*, Alma Hortensia Serafin Muñoz4, Diana Olivia Rocha Amador5, Rebeca Yasmin Perez Rodriguez6, Jesús Horacio Hernández Anguiano7, Carmen Julia Navarro8, Xiaoxiao Zha1, Daniela Moncada3, María de Jesús Puy Alquiza2, Pooja Vinod Kshirsagar2, Yanmei Li2*

1Doctoral Program of Water Science and Technology, Engineering Division, University of Guanajuato, Guanajuato, Guanajuato. 36000, México. (x.liao@ugto.mx, x.zha@ugto.mx)

2Department of Mining, Metallurgy and Geology Engineering, University of Guanajuato, Guanajuato, Guanajuato. 36020, México. (yanmeili@ugto.mx, rmiranda@ugto.mx, yosune.puy155@gmail.com, pv.kshirsagar@ugto.mx)

3Laboratory for Research and Characterization of Minerals and Materials, University of Guanajuato, Guanajuato, Guanajuato. 36020, México. (qmoncadas@gmail.com)

4Department of Civil Engineering, University of Guanajuato, Guanajuato, Guanajuato. 36000, México (sermuah@ugto.mx)

5Pharmacy Department, University of Guanajuato, Guanajuato, Guanajuato. 36000, México. (drochaa@ugto.mx)

6Chemistry Department, University of Guanajuato, Guanajuato, Guanajuato. 36000, México. (rebeca.perez@ugto.mx)

7Department of Geomatics and Hydraulic Engineering, University of Guanajuato, Guanajuato, Guanajuato. 36000, México. (horacio.hernandez@ugto.mx)

8Faculty of Engineering, University Autonomous of Chihuahua, Chihuahua, Chihuahua, 31000, México. (cjnavarro@uach.mx)

*Corresponding authors: 1. yanmeili@ugto.mx, 2. rmiranda@ugto.mx

Abstract:  The present study aims to investigate the low-energy consumption and high-efficiency removal of arsenic from aqueous solutions. The designed adsorbent Fe/TBC was synthesized by impregnating iron on torrefaction henequen fibers. Isothermal adsorption experiments indicated maximum adsorption capacities of 7.30 mg/g and 8.98 mg/g for arsenic(V) at 25.0 °C and 40.0 °C, respectively. The interference testing showed that elevated levels of pH, HCO3- concentration, and humic acid content in the solution could inhibit the adsorption of arsenic by Fe/TBC. Characterization of the adsorbent before and after adsorption using FTIR and SEM-EDS techniques confirmed arsenic adsorption mechanisms, including pore filling, electrostatic interaction, surface complexation, and H-bond adhesion. Column experiments were conducted to treat arsenic-spiked water and natural groundwater, with effective treatment volumes of 550 mL and 8792 mL, respectively. Lastly, the life cycle assessment (LCA) using OpenLCA 2.0.3 software was performed to treat 1 m3 of natural groundwater as the functional unit. The results indicated relatively significant environmental impacts during the Fe/TBC synthesis stage. The global warming potential resulting from the entire life cycle process was determined to be 0.8 kg CO2-eq. The results from batch and column experiments, regeneration studies, and LCA analysis indicate that Fe/TBC could be a promising adsorbent for arsenic(V).

Key words: Arsenic adsorption, CO2 emission, Regeneration, Torrefaction biochar, Water treatment

Fundamental characteristics, specific cations and anions of the natural groundwater sample from a well in Guanajuato.

| Items | Value |
| --- | --- |
| Coordinates | Latitude 20°48՛24˝ Longitude 101°42՛47˝ |
| Temperature (°C) | 30.5 |
| pH | 7.6 |
| EC (uS/cm) | 502.00 |
| TDS (mg/L) | 321.28 |
| Ca2+ (mg/L) | 36.67 |
| Mg2+ (mg/L) | 5.49 |
| Na+ (mg/L) | 79.12 |
| K+ (mg/L) | 4.04 |
| HCO3- (mg/L) | 290.00 |
| Cl- (mg/L) | 3.51 |
| SO42- (mg/L) | 51.77 |
| As (ug/L) | 24.10 |

LCA inventory data for the whole processes of LCA analysis.

| Processes | Inventory | Value | Unit | Note |
| --- | --- | --- | --- | --- |
| TBC preparation | Input |  |  |  |
|  | Electricity | 1.8 | MJ | low voltage |
|  | Tap water | 2000 | g |  |
|  | Deionized water | 500 | g |  |
|  | Transport | 500 | kg*km | freight train |
|  | Biomass | 467 | g | The torrefaction production efficiency of henequen fiber is 73%. |
|  | Output |  |  |  |
|  | Wastewater | 2 | L | CUTOFF Disposal, unspecified to waste water treatment |
|  | Waste heat | 1.8 | MJ | The electrical energy assumed diminished as heat to atmosphere. |
|  | TBC | 341 | g |  |
| Fe/TBC synthesis | Input |
|  | Electricity | 1.4 | MJ | low voltage |
|  | Iron chloride | 818 | g | inorganic chemicals |
|  | Nitric acid | 304 | g | with 98% HNO3 |
|  | Tap water | 2000 | g |  |
|  | Deionized water | 1500 | g |  |
|  | TBC | 341 | g |  |
|  | Output |
|  | Wastewater | 2 | L | CUTOFF Disposal, unspecified to waste water treatment |
|  | Waste heat | 1.4 | MJ | The electrical energy assumed diminished as heat to atmosphere. |
|  | Fe/TBC | 341 | g |  |
| Groundwater treatment | Input |  |  |  |
|  | Electricity | 8.71 | MJ | low voltage |
|  | Pump & Use Well Water | 1 | m3 | Groundwater from Guanajuato |
|  | Fe/TBC | 341 | g |  |
|  | Output |
|  | Tap water | 1000 | kg | As-free water |
|  | Spent adsorbent | 341 | g | CUTOFF Disposal, carbon black, to residual material landfill |

XRF analysis outcomes of major elemental composition of TBC, Fe/TBC and  Fe/TBC after adsorption with As.

| Biochars | Mg (mg/kg) | Cl (mg/kg) | Fe (mg/kg) | As (mg/kg) | O (mg/kg) | Na (mg/kg) |
| --- | --- | --- | --- | --- | --- | --- |
| TBC after HNO3 treatment | 789 | 126 | 33.3 | ND | 981000 | 10800 |
| Fe/TBC | 2890 | 18100 | 41600 | ND | 883000 | 44000 |
| Fe/TBC with As loaded | 2090 | 4710 | 48600 | 494 | 905000 | 28300 |

BET surface area, average pore diameter and total volume in pores of TBC and Fe/TBC.

| Biochars | SBET (m2/g) | Average pore diameter (nm) | Vtotal (cm3/g) |
| --- | --- | --- | --- |
| TBC before HNO3 treatment | 1.3894 | 7.9101 | 0.00177 |
| TBC after HNO3 treatment | 0.5173 | 13.2754 | 0.00122 |
| Fe/TBC | 2.2317 | 8.9771 | 0.00391 |
| As-loaded Fe/TBC | 1.1056 | 6.7150 | 0.00158 |

Adsorption kinetics model parameters obtained from experiments.

| Temperature | PFO model |  |  |  | PSO model |  |  |  | Elovich model |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | k1 | qe | R2 | RMSE | k2 | qe | R2 | RMSE | a | b | R2 | RMSE |
|  | min-1 | mg/g |  |  | g/mg/min | mg/g |  |  | mg/g/min | g/mg |  |  |
| 25 °C | 0.080 | 0.361 | 0.719 | 0.054 | 0.312 | 0.384 | 0.853 | 0.039 | 0.256 | 18.7 | 0.977 | 0.016 |
| 40 °C | 0.074 | 0.376 | 0.805 | 0.049 | 0.260 | 0.404 | 0.903 | 0.034 | 0.206 | 17.2 | 0.974 | 0.018 |

Adsorption isotherm model parameters obtained from experiments.

| Temperature | Langmuir model |  |  |  | Freundlich model |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qm | KL | R2 | RMSE | KF | n | R2 | RMSE |
| 25 °C | 7.30 | 0.311 | 0.903 | 0.734 | 2.12 | 2.85 | 0.934 | 0.606 |
| 40 °C | 8.98 | 0.490 | 0.903 | 1.696 | 2.98 | 2.95 | 0.966 | 0.564 |

Thomas model parameters obtained from column experiments.

| Influent | Thomas model |  |  |
| --- | --- | --- | --- |
|  | q0 (ug/g) | KTH (L/mg) | R2 |
| As-spiked water | 366 | 9.59 | 0.977 |
| Natural groundwater | 10832 | 0.30 | 0.973 |

Environmental impact analysis results for 1 m3 As-contaminated groundwater treatment.

| Impact category | Result | Reference unit |
| --- | --- | --- |
| Fine particulate matter formation | 0.000399002 | kg PM2.5-eq |
| Fossil resource scarcity | 0.085850958 | kg oil-eq |
| Freshwater ecotoxicity | 0.002499829 | kg 1,4-DCB-eq |
| Global warming | 0.860574772 | kg CO2-eq |
| Human carcinogenic toxicity | 0.004618957 | kg 1,4-DCB-eq |
| Human non-carcinogenic toxicity | 0.104753422 | kg 1,4-DCB-eq |
| Ozone formation, Human health | 0.001060343 | kg NOx-eq |
| Ozone formation, Terrestrial ecosystems | 0.001069592 | kg NOx-eq |
| Terrestrial acidification | 0.002005846 | kg SO2-eq |
| Terrestrial ecotoxicity | 0.260790247 | kg 1,4-DCB-eq |

Illustration of strategy for preparation of Fe/TBC composites.

System boundary and inputs/outputs of assembling Fe/TBC to treat 1 m3 of As-contaminated groundwater.

XRD patterns of TBC.

XRD patterns of Fe/TBC.

Zeta potential of Fe/TBC as a function of pH.

- Adsorption mechanism of Fe/TBC for As removal from water bodies.

Sankey diagram of global warming impact across the entire LCA processes.