Supporting Information

Nanomechanical Mapping of PLA Hydroxyapatite Composite Scaffolds Links Surface Homogeneity to Stem Cell Differentiation

Sonthikan Sitthisang1, Xunan Hou2, Alongkot Treetong3, Xin Xu2, Weilin Liu2, Chaobin He2,4*, Udom Sae-Ueng5*, Supansa Yodmuang1,6*

This PDF file includes

Figures S1 and Table S1

Figure S1.

The viability of hADMSCs cultured on P10 and P20 scaffolds after 4 weeks. The non-seeded scaffold serves as the control group. All data are expressed as mean ± SD (n = 3)

Table S1 PrestoBlue™ Assay data showing the viability of hADMSCs cultured on P10 and P20 scaffolds after 4 weeks. Absorbance values at wavelengths 570 nm and 600 nm and the calculated difference (570 nm - 600 nm) are provided. The non-seeded scaffold serves as the control group (n = 3).

|  | Absorbance at wavelength: 570 nm |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| scaffold | n = 1 | n = 2 | n = 3 |  |  |
| Non-seeded scaffold P10 P20 | 0.573 | 0.575 | 0.574 |  |  |
|  | 0.566 | 0.553 | 0.572 |  |  |
|  | 0.546 | 0.540 | 0.572 |  |  |
|  | Absorbance at wavelength: 600 nm |  |  |  |  |
| scaffold | n = 1 | n = 2 | n = 3 |  |  |
| Non-seeded scaffold P10 P20 | 0.567 | 0.569 | 0.570 |  |  |
|  | 0.439 | 0.418 | 0.434 |  |  |
|  | 0.486 | 0.476 | 0.512 |  |  |
|  | Subtraction of absorbance 570 nm - 600 nm |  |  |  |  |
| scaffold | n = 1 | n = 2 | n = 3 | Mean | SD |
| Non-seeded scaffold P10 P20 | 0.006 | 0.006 | 0.004 | 0.005 | 0.001 |
|  | 0.127 | 0.135 | 0.139 | 0.134 | 0.006 |
|  | 0.060 | 0.064 | 0.060 | 0.061 | 0.003 |