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Figure S1. 
The viability of hADMSCs cultured on P10 and P20 scaffolds after 4 weeks. The non-seeded scaffold serves as the control group. All data are expressed as mean ± SD (n = 3)



Table S1 PrestoBlue™ Assay data showing the viability of hADMSCs cultured on P10 and P20 scaffolds after 4 weeks. Absorbance values at wavelengths 570 nm and 600 nm and the calculated difference (570 nm - 600 nm) are provided. The non-seeded scaffold serves as the control group (n = 3).

	
	Absorbance 
at wavelength: 570 nm
	 
	 

	scaffold
	n = 1
	n = 2
	n = 3
	
	

	Non-seeded scaffold
P10
P20
	0.573
	0.575
	0.574
	
	

	
	0.566
	0.553
	0.572
	
	

	
	0.546
	0.540
	0.572
	
	

	
	Absorbance
at wavelength: 600 nm
	
	

	scaffold
	n = 1
	n = 2
	n = 3
	
	

	Non-seeded scaffold
P10
P20
	0.567
	0.569
	0.570
	
	

	
	0.439
	0.418
	0.434
	
	

	
	0.486
	0.476
	0.512
	
	

	
	Subtraction of absorbance 
570 nm - 600 nm
	
	

	scaffold
	n = 1
	n = 2
	n = 3
	Mean
	SD

	Non-seeded scaffold
P10
P20
	0.006
	0.006
	0.004
	0.005
	0.001

	
	0.127
	0.135
	0.139
	0.134
	0.006

	
	0.060
	0.064
	0.060
	0.061
	0.003
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