Supplementary file

Pharmacokinetics of pulmonary indacaterol in rat lung using molecular imprinting solid-phase extraction coupled with RP-UPLC

Mohamed Tarek1, 2, Nermine S. Ghoniem3*, Maha A. Hegazy4, Hebatallah A. Wagdy1, 2**

1Pharmaceutical Chemistry Department, Faculty of Pharmacy, The British University in Egypt (BUE), Cairo, Egypt.

2Health Research Center of Excellence; Drug Research and Development Group, Faculty of Pharmacy, The British University in Egypt, Cairo, Egypt.

3Analytical Chemistry Department, Faculty of Pharmacy, Cairo University, Kasr-El Aini Street, 11562 Cairo, Egypt.

4Pharmaceutical Chemistry Department, Faculty of Pharmacy, Future University in Egypt, Cairo 11835, Egypt.

* Corresponding Author

Nermine S. Ghoniem

Department of Analytical Chemistry, Faculty of Pharmacy, Cairo University.

E-mail address: nermine.ghoniem@pharma.cu.edu.eg

** Corresponding Author

Hebatallah A. Wagdy

Department of Pharmaceutical Chemistry, Faculty of Pharmacy, The British University in Egypt.

E-mail address: Hebatallah.wagdy@bue.edu.eg

List of tables

Table S1: Intra-day and inter-day accuracy and precision of the LLOQ and QCs of indacaterol

Table S2: Stability of the lung samples spiked with indacaterol standard under different conditions.

Table S3: Extraction recovery of indacaterol from lung samples.

Table S4: Effect of solvent on the rebinding of indacaterol to the polymer.

Table S5: Binding kinetics of indacaterol polymer.

Table S6: KD and Qmax, for lower and higher affinity binding sites of the MIP at equilibrium conditions.

Table S7: Adsorption isotherms parameters for MIP.

Table S8: Binding selectivity of the prepared polymer.

List of figures

Fig. S1.: Calibration curve of indacaterol in lung tissue sample in the concentrations ranging from 0.10 to 100.0 µg mL-1 using salbutamol as IS.

Fig. S2: Binding kinetics of indacaterol polymer.

Fig. S3: (a) Scatchard plot and (b) Freundlich and (c) Langmuir adsorption isotherms models for molecular imprinting polymer.

Fig. S4: Fourier transform infrared spectra of (a) extracted molecular imprinting polymer, (b) non-imprinted polymer, (c) indacaterol and (d) non-extracted molecular imprinting polymer.

Fig. S5: Effect of polymer weight on the loading % of indacaterol.

Fig. S6: Effect of different concentrations of indacaterol on the % loaded to molecular imprinting solid-phase extraction cartridge.

Fig. S7: Effect of type of loading solvent on the % loaded of indacaterol to molecular imprinting solid-phase extraction cartridge.

Fig. S8: Effect of type of washing solvent on the % washed of indacaterol from molecular imprinting solid-phase extraction cartridge.

Fig. S9: Effect of type of eluting solvent on the % eluted of indacaterol from molecular imprinting solid-phase extraction cartridge.

Fig. S10: Recovery of (a) indacaterol, glycopyrronium and mometasone mixture of concentration 40.0 µg mL-1 from molecular imprinting polymer and non-imprinting polymer after loading, (b) washing with 1.0 mL acetonitrile: water (20 :80; by volume) and (c) elution with 1.0 mL methanol: acetic acid (90: 10; by volume) using 20.0 mg of indacaterol polymer.

Fig. S11: Recovery of (a) indacaterol and salbutamol mixture of concentration 40.0 µg mL-1 from molecular imprinting polymer and non-imprinting polymer after loading, (b) washing with 1.0 mL acetonitrile: water (20 :80; by volume) and (c) elution with 1.0 mL methanol: acetic acid (90: 10; by volume) using 20.0 mg of indacaterol polymer.

| Table S1: Intra-day and inter-day accuracy and precision of the LLOQ and QCs of indacaterol |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Concentration (µg mL-1) | Intra-day accuracy % R* | Inter-day accuracy % R* | Intra-day precision % RSD* | Inter-day precision % RSD* |
| LLOQ | 0.10 | 112.00 | 113.05 | 4.34 | 5.02 |
| QCL | 0.30 | 106.00 | 107.12 | 2.14 | 3.53 |
| QCM | 35.00 | 104.58 | 105.32 | 2.04 | 3.21 |
| QCH | 70.00 | 101.36 | 102.17 | 1.95 | 2.19 |
| *Average of 6 determinations |  |  |  |  |  |

| Table S2: Stability of the lung samples spiked with indacaterol standard under different conditions |  |
| --- | --- |
| Item | % deviation from fresh sample |
| Short-term stability |  |
| LLOQ | -11.30±3.50 |
| QCL | -5.74±2.25 |
| QCM | -4.14±2.61 |
| QCH | -2.89±1.94 |
| Auto-sampler stability |  |
| LLOQ | -12.05±4.20 |
| QCL | -5.98±2.58 |
| QCM | -4.02±2.34 |
| QCH | -1.71±2.67 |
| Freeze and thaw stability |  |
| LLOQ | -13.26±4.85 |
| QCL | -4.80±3.26 |
| QCM | -4.30±2.81 |
| QCH | -2.20±2.25 |
| Long-term stability |  |
| LLOQ | -13.10±5.89 |
| QCL | -4.40±3.88 |
| QCM | -3.90±2.22 |
| QCH | -3.28±1.32 |
| % Deviation: (% R of stability samples - % R of fresh samples/ % R of fresh samples) × 100. |  |

| Table S3: Extraction recovery of indacaterol from lung samples |  |  |
| --- | --- | --- |
|  | Concentration (µg mL-1) | % R±SD* |
| LLOQ | 0.10 | 111.58±4.98 |
| QCL | 0.30 | 105.28±2.54 |
| QCM | 35.00 | 103.73±2.08 |
| QCH | 70.00 | 100.71±1.86 |
| *Average of 6 determinations |  |  |

| Table S4: Effect of solvent on the rebinding of indacaterol to the polymer |  |  |  |
| --- | --- | --- | --- |
| Type of solvent | QMIP (µg g-1)* | QNIP (µg g-1)* | IF* |
| Acetonitrile | 9840±0.86 | 2172±0.74 | 4.53±0.12 |
| Methanol | 3285±0.42 | 1314±0.36 | 2.50±0.06 |
| Ethanol | 3420±0.67 | 1352±0.33 | 2.53±0.34 |
| Water | 928±0.21 | 890±0.60 | 1.04±0.39 |
| Chloroform | 22±0.32 | 23±0.22 | 0.96±0.10 |
| Di-chloromethane | 12±0.36 | 13.10±0.47 | 0.92±0.11 |
| Dimethyl sulfoxide | 8±0.54 | 8.52±0.66 | 0.94±0.12 |
| *Average of three times ± SD |  |  |  |

| Table S5: Binding kinetics of indacaterol polymer |  |  |  |
| --- | --- | --- | --- |
| Time (min) | QMIP (µg g-1)* | QNIP (µg g-1)* | IF* |
| 5 | 758±0.98 | 195±0.36 | 3.89±0.62 |
| 15 | 1245±0.24 | 318±0.54 | 3.92±0.3 |
| 30 | 3014±0.47 | 752±0.72 | 4.01±0.25 |
| 60 | 5065±0.35 | 1248±0.36 | 4.06±0.01 |
| 120 | 9840±0.86 | 2172±0.74 | 4.53±0.12 |
| 240 | 6512±0.75 | 1637±0.11 | 3.98±0.64 |
| 360 | 3125±0.36 | 783±0.25 | 3.99±0.11 |
| 480 | 1542±0.21 | 398±0.36 | 3.87±0.15 |
| 1080 | 1024±0.36 | 272±0.82 | 3.76±0.46 |
| 1200 | 945±0.87 | 244±0.75 | 3.87±0.12 |
| 1440 | 942±0.21 | 240±0.47 | 3.92±0.26 |
| *Average of three times ± SD |  |  |  |

| Table S6: KD and Qmax, for lower and higher affinity binding sites of the MIP at equilibrium conditions |  |  |
| --- | --- | --- |
|  | Line 1: high affinity region | Line 2: low affinity region |
| Linear regression line equation | y=−0.9708x+4499.9 | y=0.0691x+218.39 |
| R2 | 0.9857 | 0.9825 |
| Equilibrium dissociation constant KD (μg) | 1.03±0.12 | 14.47±0.67 |
| Maximum binding sites Qmax (μg g-1) | 4635±0.13 | 3160±0.32 |

| Table S7: Adsorption isotherms parameters for MIP. |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Freundlich |  |  | Langmuir |  |  |
| KF (µg1-1/n mL1/n g-1) | n | R2 | Qmax (µg g-1) | KL (mL µg -1) | R2 |
| 171.5 | 1.1 | 0.9342 | 10000 | 0.043 | 0.8287 |

| Table S8: Binding selectivity of the prepared polymer |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Concentration (µg mL-1) | Competitive binding between indacaterol, glycopyrronium and mometasone to indacaterol polymer |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Indacaterol |  |  |  |  | Glycopyrronium |  |  |  | Mometasone |  |  |  |
|  | QMIP (µg g-1)* | QNIP (µg g-1)* |  | IF* |  | QMIP (µg g-1)* | QNIP (µg g-1)* | IF* |  | QMIP (µg g-1)* | QNIP (µg g-1)* |  | IF* |
| 40.0 | 6247±0.36 | 1671±0.66 |  | 3.73±0.3 |  | 45±0.21 | 43±0.61 | 1.05±0.4 |  | 51±0.91 | 50±0.42 |  | 1.02±0.4 |
|  | Competitive binding between indacaterol and salbutamol to indacaterol polymer |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Indacaterol |  |  |  |  |  | Salbutamol |  |  |  |  |  |  |
|  | QMIP (µg g-1)* |  | QNIP (µg g-1)* |  | IF* |  | QMIP (µg g-1)* |  | QNIP (µg g-1)* |  |  | IF* |  |
|  | 6252±0.35 |  | 1654±0.61 |  | 3.78±0.26 |  | 94±0.54 |  | 92±0.68 |  |  | 1.02±0.14 |  |
| *Average of three times ± SD |  |  |  |  |  |  |  |  |  |  |  |  |  |

Fig. S1

NIP

MIP

Fig. S2

Low affinity binding region

High affinity binding region

a

c

b

Fig. S3

c

a

b

d

Fig. S4

Fig. S5

Fig. S6

Fig. S7

Fig. S8

Fig. S9

a

b

c

Fig. S10

c

b

a

Fig. S11