Supporting information

Facile Fabrication of Zn0.6Cd0.4S/ZnO/g-C3N4 dual Z-scheme heterostructure with Enhanced Performance under Visible Light: An Experimental and Theoretical Study

Yuqi Dong1, Qing-an Qiao1*, Ruping Wang1, Yueyue Yang1, Honglan Cai1*, Hongwei Gao2

1 School of Chemistry and Materials Science, Ludong University, Yantai 264025, PR China

2 School of Life Science, Ludong University, Yantai 264025, PR China

Table S1 Specific surface area, pore size and pore volume analysis of prepared samples

| Samples | SBET (m2/g) | Pore volume(cm3/g) | Average pore size(nm) |
| --- | --- | --- | --- |
| Zn0.6Cd0.4S | 45.8612 | 0.087020 | 22.8148 |
| g-C3N4 | 7.2868 | 0.017385 | 20.7587 |
| Z0.6C0.4S /ZnO/CN-35% | 70.8393 | 0.169922 | 22.7369 |

Fig S1 XRD patterns of Zn0.6Cd0.4S

Fig S2 Mott-Schottky curves of (a) Zn0.6Cd0.4S, (b) g-C3N4, (c)ZnO

Fig S3. Photocatalytic degradation of pollutants spectra: (a)MB (CMB: 20 mg/L, pH: 7, catalysts dose: 0.6g/L, irradiation time:90 min), (b)RhB (CRhB: 20 mg/L, pH: 7, catalysts dose: 0.6g/L, irradiation time:60 min), (c-d) TC (CTC: 20 mg/L, pH: 7, catalysts dose: 0.3 g/L, irradiation time:30 min)

Fig S4 Electronic band structures, total density of states (TDOS) and projected density of states (PDOS) of (a-b) Zn0.6Cd0.4S, (c-d) ZnO, (e-f) g-C3N4

* Corresponding authors:

E-mail addresses: qiaoqa@ldu.edu.cn (Qing-an Qiao), hognlancai74@ldu.edu.cn(Honglan Cai)