Supporting Information

Surface modification of MXene using cationic CTAB surfactant for adsorptive elimination of cefazolin antibiotic from water

Jafar Abdi a, b, *, Golshan Mazloom c, Yeojoon Yoon d

a Faculty of Chemical and Materials Engineering, Shahrood University of Technology, 3619995161 Shahrood, Iran

b Center for International Scientific Studies and Collaborations, Tehran, Iran

c Department of Chemical Engineering, Faculty of Engineering, University of Mazandaran, 47416-13534 Babolsar, Iran

d Department of Environmental and Energy Engineering, Yonsei University, Wonju, Republic of Korea

Corresponding authors (*):

Jafar.abdi@shahroodut.ac.ir  (J. Abdi)

Evaluation of the kinetic and isotherm models quality

The quality and reliability of the kinetic and isotherm models were assessed using different statistical techniques described as follows:

1. The average absolute relative deviation of the model results from the experimental values was calculated by the average absolute relative error (AARE):

AARE%=100ni=1nX(i)model-X(i)expX(i)exp

2. The root mean square error (RMSE), which indicates the error dispersion, is calculated by:

RMSE=i=1n(Ximodel-X(i)exp)2n12

3. The dispersion of data is investigated by the standard deviation of errors (STD), which can be calculated using:

STD=1ni=1nXimodel-X(i)model2)12

4. The coefficient of determination R2 which assigns the accuracy of the predictions. The R2 value close to 1 determines that the estimation of experimental data is more accurate.

R2=1-i=1nX(i)model-X(i)exp2i=1nX(i)model-X(i)exp2

Fig. S1. EDS spectrum and elemental mapping of CTAB@MXene.

(b)

(a)

Fig. S2. Non-linear kinetic plots for CFZ adsorption onto CTAB@MXene.

Fig. S3. Non-linear adsorption isotherm plots for CFZ adsorption onto CTAB@MXene.

Fig. S4. TOC removal rates and adsorption efficiencies observed via UV-Vis for CFZ removal.

Table S1. The results of TOC analysis from the remaining CFZ solution after different adsorption cycles under the optimized conditions.

| Sample | [TOC]0 (mg/L) |
| --- | --- |
| Pure water | 5.21 |
| First cycle | 11.7 |
| Second cycle | 13.8 |
| Third cycle | 14.6 |
| Forth cycle | 15.2 |