Physiochemical characterization and biological evaluation of amorphous solid dispersions of erlotinib HCl; better chemotherapeutic efficacy

K.P. Safna Hussan 1,2,3*, Thekkekara D Babu1, M. Shahin Thayyil4, T.S. Sreeshma5, A. Archana1

1Amala Cancer Research Centre, Amalanagar P O, Thrissur 680 555 Kerala, India.

2Micro/Nano Technology Center, Tokai University, Hiratsuka-shi, Kanagawa 259-1292, Japan

3Ayurgreen Scientifica Research Institute LLP, Ayurgreen Campus, Edappal, Malappuram 679 582, Kerala, India

4Department of Physics, University of Calicut, Malappuram-673635, Kerala, India.

5Department of Veterinary Biochemistry, College of Veterinary and Animal Sciences, Mannuthy, Thrissur, India

Corresponding Authors

*Safna Hussan K.P, yfm4476@tokai.ac.jp, safnahussain2@gmail.com

# X-Ray Diffraction

## 1.1. Optimum Concentration:

In this study, we developed an amorphous solid dispersion of erlotinib HCl using several polymers of PVP-K30, PEG 4000, and their blend in a 10:90 weight ratio of drug:polymer configuration. In which ERL+PEG exhibits enhanced solubility, bioavailability and anticancer efficacy in invitro and in vivo studies. The ideal drug: polymer concentration is 10:90 because when drug loading in the formulation is increased, ERL's propensity to recrystallize increases. The XRD pattern for different weight ratio of ERL+PEG is emphasizing the crystalline peaks of ERL is hiking upon increasing drug concentration, which is clearly depicted in the Figure below. Such recrystallisation adversely effects their solubility and bioavailability ,  rendering the effort useless.

Fig 1S. Powder X-ray diffraction patterns of ERL and amorphous solid dispersion of ERL with PEG 4000 at different weight ratios

Fig 2S. Powder X-ray diffraction patterns of ERL, PEG 4000 and amorphous solid dispersion of ERL with PEG 4000 (at the weight ratio 10:90).

The excipient PEG-4000 showed two sharp peaks for crystallinity at 19.36˚ and 23.72˚. The characteristic peaks of ERL were found to diminish in the formulations, however the crystalinity peaks of PEG 4000 were retained.

# FTIR Spectroscopy

| Wavenumber (cm-1) |  |  |  | Functional groups [24][25][7][26][27] |
| --- | --- | --- | --- | --- |
| ERL | ERL+PEG | ERL+PVP | ERL+PEG+PVP |  |
|  | 1721 |  |  |  |
| 1666 | 1642 | 1648 | 1658 | C=O- bending |
| 1603 |  |  |  | C=C stretching |
| 1539 |  |  |  | C=N stretching |
| 1479 | 1470 | 1467 | 1464 | CH2 sym. deformation vibration |
| 1386 | 1346 | 1346 | 1349 | C-H sym. deformation vibration |
| 1301 | 1279 | 1282 | 1288 | NCO stretching vibration |
| 1183 | 1252 | 1237 | 1243 | C-N stretching vibrations |
| 1146 | 1107 | 1110 | 1116 | COCN stretching vibration |
| 1086 |  |  |  | -COCN stretching vibration |
| 1035 |  |  |  | C=O stretching |
| 947 | 949 | 955 | 967 | C-H out-of-plane deformation vibration |
| 893 | 840 | 840 | 840 | C-C skeleton vibration |
| 793 |  |  | 753 | C-O-C stretching vibration |
| 709 |  |  |  | N-H deformation vibrations |
| 679 |  |  | 653 | N-H out-of-plane bending vibrations |
| 588 | 588 | 588 | 577 | C-C skeleton vibration |

Tab S1. Prominent FTIR peaks for neat and amorphous binary dispersion of AMB with selected polymers

# DPPH Assay

Fig 3S. DPPH radical scavenging activities of various concentrations of polymers PVP K -30 and PEG 4000.

The DPPH scavenging activity of different concentrations of base polymers PVP K -30 and PEG 4000 were evaluated and depicted in Figure 3.S.  Both polymers have negligible activity even at higher concentration.

# Hydroxyl Radical Assay

Fig 4S. Hydroxyl radical scavenging activities of various polymers PVP K and PEG  concentrations.

In addition, the hydroxyl scavenging activity of different concentrations of base polymers PVP K -30 and PEG 4000 were evaluated and depicted in Figure 4.S in supplementary material.  Both polymers have negligible activity even at higher concentration.