Supplementary data for

Engineering Nitrogen and Oxygen Functionalities in Naturally Sourced Activated Carbon for Multicomponent Gas Adsorption

Xiupeng Chenga, †, Zhipeng Qiea, b, †, *, Huaizhong Xiangc,d, Zhongbao Liua, Limingxin Zonga, Wenqi Hea, Xinxin Pie, Hassan Alhassawic, Peiyao Caoa, Guang Yanga, Shuangshuang Gaoa

a College of Mechanical and Energy Engineering, Beijing University of Technology, Beijing 100124, China

b Chongqing Research Institute of Beijing University of Technology, Chongqing 401121, China

c Department of Chemical Engineering, The University of Manchester, Manchester M13 9PL, UK

d Department of Chemistry, Queen Mary University of London, London E1 4NS, UK

e College of Mechanical and Electrical Engineering, Qingdao University, Qingdao 266071, China

Corresponding Author’s email: qiezhipeng@bjut.edu.cn (Z.Q.)

† These authors contributed equally to this work.

Fig. S1. XPS K2p spectra of (a) AC, ( (b) NAC-600, (c) NAC-750 and (d) NAC-900.

Fig. S2. CO2 curves of adsorption capacity versus time (a) AC, (b) NAC-600, (c) NAC-750, (d) NAC-900 and (e) 3D comparison chart of .

Fig. S3. CO2 adsorption isotherms of (a) AC, ( (b) NAC-600, (c) NAC-750 and (d) NAC-900.

Table.S1. Fitting parameters of CO2 adsorption isotherms

|  | Langmuir |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qm | KL | R2 | KF | n | R2 |
| AC | 96 | 0.05 | 0.996 | 9.95 | 1.93 | 0.999 |
| NAC-600 | 98.97 | 0.048 | 0.999 | 9.89 | 1.9 | 0.994 |
| NAC-750 | 98.5 | 0.049 | 0.994 | 9.98 | 1.91 | 0.999 |
| NAC-900 | 85.6 | 0.042 | 0.998 | 7.2 | 1.79 | 0.999 |

Fig. S4. H2O curves of adsorption capacity versus time (a) AC, ( (b) NAC-600, (c) NAC-750 ,(d) NAC-900 and(e) 3D comparison chart of .

Fig. S5. C7H8 curves of adsorption capacity versus time (a) AC, ( (b) NAC-600, (c) NAC-750 ,(d) NAC-900 and(e) 3D comparison chart of .

Fig. S6. Recyclability of NAC-600 during CO2 and toluene adsorption/desorption test